** USE WHEN SPECIFIED IN THE MATERIALS DESIGN REPORT **

** USE WHEN THE PROJECT INCLUDES ANY OF THESE SECTIONS OF THE SPECIFICATIONS: SECTIONS 208, 306, 412, 810, 913, AND 915 **

** USE WHEN THE PROJECT INLCUDES CONSTRUCTION OF NEW BRIDGES OR NEW RETAINING WALLS **

(1014GEOSYN, 07/18/24)

SECTION 1014 	GEOSYNTHETICS:

1014-1		General Requirements: of the Standard Specifications is revised to read:

Certificates of Analysis, conforming to the requirements of Subsection 106.05 of the specifications, shall be submitted.

Geosynthetic materials, excluding biaxial geogrid, must be on the DataMine list for geotextiles and geosynthetics on the AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) website. The product line evaluation report from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) shall be provided to the Engineer prior to use on the project.

Fibers, yarns, and filaments used in the manufacture of geotextile fabric, and the threads used in joining by sewing, shall consist of long-chain synthetic polymers, composed at least 95 percent, by weight, of polyolefins or polyesters. They shall be formed into a stable network such that the filaments or yarns retain their dimensional stability relative to each other, including selvages.

Geosynthetic materials shall be furnished in protective covers capable of protecting the materials from harmful environmental conditions such as ultraviolet rays, abrasion, extreme heat, and water. Storage of the materials shall be in a manner that prevents damage, contamination, or deterioration.

Geotextile fabric shall be resistant to chemical attack, rot, and mildew, and shall have no tears or defects which will adversely alter its physical properties.

All numeric values in the following tables, except for apparent opening size (AOS), represent minimum average roll values (MARV) in the weaker principal direction. Numeric values for (AOS) represent maximum average roll values.

Woven slit film geosynthetics will not be allowed for use in Subsections 1014-5, 1014-6, 1014-7, and 1014-9 of the specifications.