*                          USE STORED SPECIFICATION 109PAVSM WHEN AN                  *

*           INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE                *

*                            PAVEMENT SMOOTHNESS IS SPECIFIED IN THE                              *

*                                       MATERIALS DESIGN REPORT                                                   *

*		USE IN CONJUNCTION WITH STORED SPECIFICATION 1001MATL	   *

*		FILL IN THE FOLLOWING (SHOWN IN RED TEXT):				   *

*			407-3		SPREAD RATE			(1 place)    *

*						PERCENTAGE (LEVELING)	(1 place)    *

*						THICKNESS			(1 place)    *

*			407-3.03		TYPE OF ASPHALT BINDER	(1 place)    *

(407ADMIX, 07/18/24)

SECTION 407	ASPHALTIC CONCRETE FRICTION COURSE:

407-3			Materials:  of the Standard Specifications is modified to add:

For comparative purposes, quantities shown in the bidding schedule have been calculated based on the following data:

| Spread Rate (lb./ sq. yd.) | XXX |  |
| --- | --- | --- |
| Asphalt Cement, % | 6.0 (6.5 when PG TR+ is used) |  |
| Mineral Admixture, % | 1.0 |  |

The estimated target spread rate specified above includes XX percent for leveling to provide a minimum XX inch thickness above the leveling thickness.

407-3.03		Bituminous Material:  the first paragraph of the Standard Specifications is revised to read:

Asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005.  The type of asphalt binder shall be PG XXXX.

407-7.04(A)		General Requirements:  the second paragraph of the Standard Specifications is revised to read:

All wheels and tires of compactors shall be wetted with water, or if necessary soapy water, or a release agent in order to prevent the sticking of asphaltic concrete. All other equipment surfaces shall be treated when necessary with a release agent. Only release agents evaluated through AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) are acceptable for use. The results from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) testing, when tested in accordance with AASHTO T 383, shall conform to the requirements shown in the table below.

407-7.04(A)		General Requirements:  the second row of the “Release Agent Test – Requirement” table of the Standard Specifications is hereby deleted: