*                          USE STORED SPECIFICATION 109PAVSM WHEN AN                           *

*              INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE              *

*               PAVEMENT SMOOTHNESS IS SPECIFIED IN THE MATERIALS DESIGN        *

*                                                                REPORT.                                                              *

**               WHEN PAVEMENT SMOOTHNESS INCENTIVES/DISINCENTIVES               **

**                           ARE SPECIFIED IN THE MATERIALS DESIGN REPORT,                    **

**              EDIT THIS STORED SPECIFICATION TO INCLUDE THE REVISION               **

**                          TO SUBSECTION 409-3.01 (SECOND PARAGRAPH).                          **

*	FILL IN THE FOLLOWING (SHOWN IN RED TEXT):					    *

*		409-2		UNIT WEIGHT	(1 place)	    *

*		409-2.02		TYPE OF ASPHALT BINDER		(1 place)	    *

(409ACMS, 07/18/24)

SECTION 409	ASPHALTIC CONCRETE (MISCELLANEOUS STRUCTURAL):

409-2			Materials:  of the Standard Specifications is modified to add:

The bidding schedule quantity of asphaltic concrete is based on an estimated unit weight of XXX pounds per cubic foot.

409-2.02		Bituminous Material:  the first paragraph of the Standard Specifications is revised to read:

Asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005 of the specifications.  The type of asphalt binder shall be PG XXXX.

(When pavement smoothness incentives/disincentives are

specified in the Materials Design Report, use the following

revision to the second paragraph of Subsection 409-3.01 and change to black text;

otherwise delete this revision of the second

paragraph from this stored specification.)

409-3.01		General:  the first sentence of the second paragraph of the Standard Specifications is revised to read:

Smoothness of the final pavement surface shall be tested, and payment for smoothness made, in accordance with Subsection 109.13 of the specifications.  In addition to the requirements of Subsection 109.13 of the specifications, the following requirements shall also be met:

409-3.01		General:  the ninth paragraph of the Standard Specifications is revised to read:

All wheels and tires of compactors shall be wetted with water, or if necessary soapy water, or a release agent in order to prevent the sticking of asphaltic concrete. All other equipment surfaces shall be treated when necessary with a release agent. Only release agents evaluated through AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) are acceptable for use. The results from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) testing, when tested in accordance with AASHTO T 383, shall conform to the requirements shown in the table below.

409-3.01		General:  the second row of the “Release Agent Test – Requirement” table of the Standard Specifications is hereby deleted: