*                           USE STORED SPECIFICATION 109PAVSM WHEN AN                           *

*              INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE               *

*                                 PAVEMENT SMOOTHNESS IS SPECIFIED IN                                   *

*                                          THE MATERIALS DESIGN REPORT                                          *

*	USE IN CONJUNCTION WITH THE FOLLOWING:					    *

*	BID ITEM:						9240170			    *

*	STORED SPECIFICATIONS:				924CQC			    *

*								        1001MATL			    *

*	FILL IN THE FOLLOWING (SHOWN IN RED TEXT):					    *

*	417-1		TYPE OF MIX	(1 Place)	    *

*	TABLE 417-1	EFFECTIVE VOIDS	(1 Place)	    *

*	TABLE 417-1 (NOTE 3)	RATIO MINIMUM VALUE	(1 Place)	    *

*	TABLE 417-1 (NOTE 4)	NUMBER OF GYRATIONS	(3 Places)	    *

*	417-3	UNIT WEIGHTS	(As needed)	    *

*	PERCENTAGES	(As needed)	    *

*	417-3.03(B) 	TYPE OF ASPHALT BINDER	(1 place)	    *

(417SHRP, 07/18/24)

SECTION 417	ASPHALTIC CONCRETE (END PRODUCT) SHRP VOLUMETRIC MIX:

417-1			Description: the last paragraph of the Standard Specifications is revised to read:

The type of asphaltic concrete shall be XXXXXXX mix.

417-2			Asphaltic Concrete Mix Design Criteria: “Effective Voids”, Note 3 and Note 4 in Table 417-1 of the Standard Specifications are revised to read:

| TABLE 417-1 ASPHALTIC CONCRETE MIX DESIGN CRITERIA |  |  |
| --- | --- | --- |
| Criteria | Requirements |  |
|  | 1/2” Mix | 3/4” Mix |
| Effective Voids: %, Range | X.X 0.2 |  |
| Notes: |  |  |
| (3) The ratio of the mix design composite gradation target for the No. 200 sieve, including mineral admixture, to the effective asphalt content shall be within the range specified below: X.X to 1.2 |  |  |
| (4) For purposes of design, the number of gyrations shall be XXX (N-design). The calculated density of the specimens at XXX gyrations (N-initial) shall be less than 89.0 percent of the maximum theoretical density. The density of the specimens at XXX gyrations (N-max) shall be less than 98.0 percent of the maximum theoretical density. |  |  |

417-3			Materials: of the Standard Specifications is modified to add:

For comparative purposes, quantities shown in the bidding schedule have been calculated based on the following data:

(In the following table, use only the columns called for

in the Materials Design Report.)

|  | 1/2” Mix | 3/4” Mix |
| --- | --- | --- |
| Unit Weight, (lb./cu. ft.) | XXX | XXX |
| Asphalt Cement, % | X.X | X.X |
| Mineral Admixture, % | 1.0 | 1.0 |

417-3.03(B)	Virgin Bituminous Material: the first paragraph of the Standard Specifications is revised to read:

Virgin asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005.  The type of virgin asphalt binder shall be PG XXXXX or, if RAP is used in the mixture, the virgin asphalt binder shall be as required to meet the blending requirements in Subsection 417-3.03(C) and Arizona Test Method 833.

417-6			Construction Requirements:  the twelfth paragraph of the Standard Specifications is revised to read:

All wheels and tires of compactors shall be wetted with water, or if necessary soapy water, or a release agent in order to prevent the sticking of asphaltic concrete. All other equipment surfaces shall be treated when necessary with a release agent. Only release agents evaluated through AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) are acceptable for use. The results from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) testing, when tested in accordance with AASHTO T 383, shall conform to the requirements shown in the table below:

417-6			Construction Requirements:  the second row of the “Release Agent Test – Requirement” table of the Standard Specifications is hereby deleted:

417-9(E)		Acceptability: of the Standard Specifications is modified to add:

The contractor may submit a written proposal without an engineering analysis for Engineer’s evaluation and approval, that a mixture properties lot with a PT value lower than 50 on gradation and/or asphalt cement content be allowed to remain in place if the application of a Self-Directed Target Change as outlined in Subsection 417-4 of the specifications would bring the PT value to 50 or greater. This written request shall also include the proposed revised PT calculations. Upon Engineer’s verification and approval of the request, the material shall remain in place at the maximum negative pay factor(s) specified in this Subsection for the mixture properties lot in reject.