*                    USE WHEN SPECIFIED IN THE MATERIALS DESIGN REPORT                  *

*                          USE STORED SPECIFICATION 109PAVSM WHEN AN                           *

*              INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE              *

*                                                      PAVEMENT SMOOTHNESS                                          *

*                                  IS SPECIFIED IN THE MATERIALS DESIGN REPORT.                   *

**               WHEN PAVEMENT SMOOTHNESS INCENTIVES/DISINCENTIVES               **

**                            ARE SPECIFIED IN THE MATERIALS DESIGN REPORT,                   **

**              EDIT THIS STORED SPECIFICATION TO INCLUDE THE REVISION               **

**                          TO SUBSECTION 409-3.01 (SECOND PARAGRAPH).                          **

*	FILL IN THE FOLLOWING (SHOWN IN RED TEXT):					    *

*		409-2		UNIT WEIGHT	(1 place)	    *

*		409-2.02		TYPE OF ASPHALT BINDER		(1 place)	    *

(409AGGR 06/19/25)

SECTION 409	ASPHALTIC CONCRETE (MISCELLANEOUS STRUCTURAL):  the title and text of the Standard Specifications is revised to read:

SECTION 409	ASPHALTIC CONCRETE (MISCELLANEOUS STRUCTURAL-SPECIAL MIX):

409-1			Description:

The work under this section shall consist of constructing Asphaltic Concrete (Miscellaneous Structural-Special Mix), hereinafter asphaltic concrete, by furnishing all materials, mixing at a plant, hauling and placing a mixture of aggregate materials, reclaimed asphalt pavement (RAP) if used, mineral admixture, and bituminous material (asphalt cement) to form a pavement course or to be used for other specified purposes, in accordance with the details shown on the project plans and the requirements of the specifications, and as directed by the Engineer.

The contractor shall acquire and make all arrangements for a source or sources of material, furnish a mix design which will meet the design criteria specified hereinafter, and provide all the equipment, materials, and labor necessary to complete the work.

## 409-2	Materials:

The bidding schedule quantity of asphaltic concrete is based on an estimated unit weight of XXX pounds per cubic foot.

### 409-2.01	Mineral Aggregate:

Mineral aggregate shall conform to the following requirements when tested in accordance with the applicable test methods.

| Mineral Aggregate Characteristics | Test Method | Requirement |
| --- | --- | --- |
| Combined Bulk Oven Dry Specific Gravity | Arizona Test Method 251 | 2.350 - 2.850 |
| Combined Water Absorption | Arizona Test Method 251 | 0 – 3.0% |
| Abrasion | # AASHTO T 96 | 100 Rev., Max 9% 500 Rev., Max 40% |
| Sand Equivalent | AASHTO T 176 (After thoroughly sieving the sample, no additional cleaning of the fines from the plus No. 4 material is required.) | Minimum 55 |
| Fractured Coarse Aggregate Particles | AASHTO T 335 | Minimum 85% with at least two fractured faces and minimum 92% with at least one fractured face (plus No. 4 material) |
| Uncompacted Void Content | AASHTO T 304 Method A | Minimum 45.0% |
| Carbonates (1) | Arizona Test Method 238 | Maximum 20% |
| (1): Testing for carbonates only applies if either of the following conditions exist: |  |  |
| (a) The asphaltic concrete is the designed final pavement surface normally used by traffic. (b) The asphaltic concrete, temporary or otherwise, will be subject to traffic for more than 60 days. |  |  |

The gradation will be determined in accordance with AASHTO T 11 and AASHTO 27, and shall conform to the requirements given below.

| Mix Design Grading Limits |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sieve Size | Percent Passing |  |  |  |
|  | 1/2 Inch Mix |  | 3/4 inch Mix |  |
|  | Without Admixture | With Admixture | Without Admixture | With Admixture |
| 1-1/4 Inch | --- | --- | --- | --- |
| 1 Inch | --- | --- | 100 | 100 |
| 3/4 Inch | 100 | 100 | 90-100 | 90-100 |
| 1/2 Inch | 90 - 100 | 90-100 | --- | --- |
| 3/8 Inch | 67 - 82 | 67 - 82 | 62 - 77 | 62 - 77 |
| No. 8 | 40 - 48 | 41 - 49 | 37 - 46 | 38 - 47 |
| No. 40 | 10 - 18 | 11 - 19 | 10 - 18 | 11 - 19 |
| No. 200 | 1.5 - 4.5 | 2.5 – 6.0 | 1.5 - 4.5 | 2.5 - 6.0 |

Fine mineral aggregate shall be obtained from crushed gravel or crushed rock.  All uncrushed material passing the No. 4 sieve shall be removed prior to the crushing, screening, and washing operations necessary to produce the specified gradation.  The contractor shall notify the Engineer a minimum of 48 hours in advance of crushing the material to be used as mineral aggregate, so all crushing operations can be inspected.  Existing stockpile material which has not been inspected during crushing will not be permitted for use unless the contractor is able to document to the Engineer's satisfaction that the mineral aggregate has been crushed.  Any material inspected by the Department as crushed material for the project shall be separated from the contractor’s other stockpiles and reserved for use throughout the project duration.

The contractor may blend uncrushed fine aggregate up to a maximum of 15 percent of the total aggregate, provided that the composite of uncrushed fine aggregate and crushed fine aggregate meets the requirement for uncompacted void content.  The uncrushed fine aggregate shall be 100 percent passing the 1/4 inch and not contain more than 4.0 percent passing the No. 200 sieve.  Should the contractor modify the method of producing either the uncrushed or crushed fine aggregate, the Engineer shall be immediately notified and the materials sampled and tested for determination of uncompacted void content.

### 409-2.02	Bituminous Material:

Asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005 of the specifications.  The type of asphalt binder shall be PG XXXX.

The percent of asphalt cement used shall be based on the weight of total mix (asphalt cement, mineral aggregate, and mineral admixture).

The contractor shall provide the laboratory mixing and compaction temperature ranges to the mix design laboratory for each PG asphalt binder used for mix design purposes.  The laboratory mixing temperature range is defined as the range of temperatures where the un-aged asphalt binder has a rotational viscosity of 0.17 ± 0.02 Pascal·seconds, measured in accordance with AASHTO T 316.  The laboratory compaction temperature range is defined as the range of temperatures where the un-aged asphalt binder has a rotational viscosity of 0.28 ± 0.03 Pascal·seconds, measured in accordance with AASHTO T 316.  The testing required in AASHTO T 316 shall be performed at 275 degrees F and 350 degrees F, and a viscosity-temperature curve developed in accordance with ASTM D2493.  The viscosity-temperature curve shall be included in the mix design report.  For PG asphalt binders that have a maximum laboratory mixing temperature exceeding 325 degrees F or a maximum laboratory compaction temperature exceeding 300 degrees F, the laboratory mixing and compaction temperature ranges shall be specified in writing by the asphalt binder supplier.  The laboratory mixing and compaction temperature ranges, as well as the actual laboratory mixing and compaction temperatures used, shall be reported on the mix design.  The contractor shall ensure that the asphalt binder supplier information required in this paragraph is provided to all appropriate parties in a timely manner, and that copies are included in the mix design report.  The laboratory mixing and compaction temperatures are for mix design purposes only.  Field mixing and compaction temperatures are specified in Subsection 409-3 of the specifications.

### 409-2.03	Mineral Admixture:

Mineral admixture shall be either Portland cement, blended hydraulic cement, or hydrated lime conforming to the following requirements:

| Material | Requirement |
| --- | --- |
| Portland Cement, Type I or II | ASTM C150 |
| Blended Hydraulic Cement, Type IP or 1L | ASTM C595 |
| Hydrated Lime | ASTM C1097 |

The mineral admixture content shall be 2.0 percent, by weight, of the mineral aggregate.  However, a minimum of 1.0 percent mineral admixture may be used if the contractor submits test information showing a lowered percentage of mineral admixture produces mix design results for Index of Retained Strength of at least 60 percent (70 percent if the average elevation of the project is above 3,500 feet) and a Minimum Wet Strength of 150 psi when tested in accordance with Arizona Test Method 802.

The certification and acceptance of Portland cement, blended hydraulic cement, and hydrated lime shall be in accordance with ADOT Materials Practice and Procedure Directive No. 13, "Certification and Acceptance of Hydraulic Cement, Fly Ash, Natural Pozzolan, Silica Fume, and Lime".

### 409-2.04	Mix Design:

Utilizing mineral aggregate which has been crushed, processed, separated, and stockpiled, a mix design shall be formulated and submitted by the contractor to the Engineer.  The mineral aggregate samples used for mix design purposes shall be representative of aggregate materials to be used during production.

The mix design shall be based on the mix design criteria and other requirements specified herein, utilizing asphalt cement and mineral admixture of the type and from the sources proposed for use in the production of asphaltic concrete.

Mix designs shall be developed utilizing a minimum ratio of three (3) for the lift thickness to nominal maximum aggregate size.

The mix design shall be prepared by or under the direct supervision of a professional engineer experienced in the development of mix designs and mix design testing.  Reclaimed asphalt pavement (RAP) may be used in the mixture if properly designed per Arizona Test Method 833.  Limits for the usage of RAP shall be per ADOT Materials Practice and Procedure Directive No. 20, “Guidance on the Use of Reclaimed Asphalt Pavement (RAP) in Asphaltic Concrete”.  The mix design engineer shall meet the requirements given in ADOT Materials Practice and Procedure Directive No. 4, “Asphaltic Concrete Mix Design Proposals and Submittals”.  The mix design shall be provided in a format that clearly indicates all the mix design requirements and shall be sealed, signed, and dated by the mix design engineer.

The mix design shall be prepared by a mix design laboratory that has met the requirements of ADOT Materials Practice and Procedure Directive No. 19, “ADOT System for the Evaluation of Testing Laboratories”.

If approved by the Engineer, as an alternative to meeting the mix design requirements specified herein, a mix design meeting the requirements of the specifications for a Section 416 Asphaltic Concrete (End Product) (1/2 inch Special Mix), Section 416 Asphaltic Concrete (End Product) (3/4 inch Special Mix), Section 417 Asphaltic Concrete (SHRP) (End Product) (1/2 inch Mix), or Section 417 Asphaltic Concrete (SHRP) (End Product) (3/4 inch Mix) may be substituted for use.  The type of asphalt binder used in the alternative mix design must be the same as that specified in Subsection 409-2.02 of the specifications.  The alternative mix design may include reclaimed asphalt pavement (RAP) if properly designed per Arizona Test Method 833.  If a mix design meeting the requirements of Section 417 is used, the number of gyrations for N-design used in the alternative mix design must be at least that which would be specified at the location where the Asphaltic Concrete (Miscellaneous Structural-Special Mix) is to be placed.  The lift thickness for the alternative mix design shall conform to the following table:

| Alternative Mix Design | Minimum Lift Thickness |
| --- | --- |
| Section 416 (1/2 Inch Special Mix) | 1-1/2 Inches |
| Section 416 (3/4 inch Special Mix) | 2 inches |
| Section 417 (1/2 inch Mix) | 2 inches |
| Section 417 (3/4 inch Mix) | 2-1/2 inches |

The contractor may propose the use of a mix design that has been developed for a previous project.  The proposed mix design shall meet the requirements of these specifications.  The contractor shall provide evidence that the type and source of bituminous material, the type of mineral admixture, and the source and methods of producing mineral aggregate, and RAP material if applicable, have not changed since the formulation of the previous mix design.  The contractor shall also provide current test results for all specified characteristics of the mineral aggregate, and RAP material if applicable, proposed for use.  The Engineer will determine if the previously used mix design is suitable for the intended use and if the previous use of the mix design was satisfactory to the Department.  The Engineer will either approve or disapprove the proposed mix design.  Should the Engineer disapprove the use of the previously used mix design, the contractor shall prepare and submit a new mix design proposal in accordance with the requirements of these specifications.

A previously used mix design older than two years from the date it was formulated, sealed, signed, and dated shall not be allowed for use.  Once approved for use on a project, a previously used mix design may be used for the duration of that project.

Test results used in the formulation of the mix design must be from testing performed no earlier than 45 days prior to the date the mix design is signed by the mix design engineer.  Historical abrasion values may be supplied on sources provided the testing was conducted within the past two years.

The mix design shall be submitted to the Engineer under a cover letter signed by an authorized representative of the contractor.

A copy of the mix design and representative samples of the mineral aggregate, mineral admixture, and asphalt cement used in the mix design shall be submitted to the Engineer for calibration of the ignition furnace, and for the determination of sand equivalent, fractured coarse aggregate particles, and uncompacted void content.  The Engineer shall witness the sampling of the mineral aggregate.  The mix design and samples shall be submitted to the Engineer at least five working days prior to the start of asphaltic concrete production.

The sand equivalent, fractured coarse aggregate particles, and uncompacted void content shall meet the requirements specified in Subsection 409-2.01 of the specifications.  Additional testing of the uncrushed and crushed fine aggregate for uncompacted void content will be required if the method of producing either fine aggregate is modified.

If the mineral aggregate fails to meet the requirements specified herein, asphaltic concrete production shall not commence, and the contractor shall either submit a revised mix design which is representative of the materials produced or correct the deficiencies in the aggregate stockpiles.

The mix design shall meet the following criteria when tested in accordance with the requirements of the following test methods:

| ## Criteria | ## Requirement | Arizona Test Method |
| --- | --- | --- |
| 1. Voids in Mineral Aggregate: %, Range | 15.0 – 18.0 | (See Note ) |
| 2. Effective Voids: %, Range | 3.8 – 4.2 | (See Note ) |
| 3. Absorbed Asphalt: %, Range | 0 – 1.0 | (See Note ) |
| Note: For mixes without RAP, Arizona Test Method 815. For mixes with RAP, Arizona Test Method 833. |  |  |

The contractor may make self-directed target changes to the approved mix design within the limits shown below.  Requests for self-directed target value changes shall be made in writing and acknowledged by the Engineer prior to start of production.  Self-directed target changes shall meet contract requirements for mix design criteria and grading limits.

| MEASURED CHARACTERISTICS | ALLOWABLE SELF-DIRECTED TARGET VALUE CHANGES |  |
| --- | --- | --- |
| Gradation (sieve size): |  |  |
| 3/8 inch No. 8 No. 40 No. 200 | 4% from mix design target value 4% from mix design target value 2% from mix design target value 0.5% from mix design target value |  |
| Asphalt Cement Content | +0.2% from mix design target value |  |
| Effective Voids | None |  |

The contractor may propose target value changes to the approved mix design for the Engineer’s approval.  The Engineer will determine if the proposed target value change will result in mix production that meets the contract requirements for mix design criteria and grading limits.  For acceptance purposes, target value changes will not be retroactive.

In no case shall the approval of mix design changes relieve the contractor of the responsibility for the results obtained by the use of such approved changes.

### 409-2.05	Sampling and Testing:

Sampling and testing the materials and mixture for quality control purposes shall be the contractor's responsibility. The contractor shall perform sufficient testing to assure that mineral aggregate and asphaltic concrete are produced which meet all specified requirements.

For acceptance purposes, samples of the asphaltic concrete shall be taken by the contractor, under the observation of the Engineer, at random locations designated by the Engineer.  A minimum of one sample shall be taken for each 500 tons of asphaltic concrete.  Samples shall be taken in accordance with the requirements of the plate method in AASHTO R 97.  The Engineer will immediately take custody of the samples.  The material will be tested by the Engineer for the following properties:

| Test Property | Test Method |
| --- | --- |
| Asphalt Cement Content | AASHTO T 308 (for both Non-RAP and RAP mixes) (See Note) |
| Gradation |  |
| Marshall Density | AASHTO R 68 |
| Maximum Theoretical Density | AASHTO T 209 |
| Effective Voids | AASHTO T 269 |
| Note: A new calibration of the ignition furnace shall be performed for each mix design, and at any other time the Engineer directs. |  |

## 409-3	Construction Requirements:

### 409-3.01	General:

All courses of asphaltic concrete shall be compacted as required, smooth and true to the required lines, grades, and dimensions.

(When pavement smoothness incentives/disincentives are

specified in the Materials Design Report, use the following

revision to the second paragraph of Subsection 409-3.01 and change to black text;

otherwise delete this revision of the second

paragraph from this stored specification.)

Smoothness of the final pavement surface shall be tested, and payment for smoothness made, in accordance with Subsection 109.13 of the specifications.  In addition to the requirements of Subsection 109.13 of the specifications, the following requirements shall also be met:

- The surface of the final lift of asphaltic concrete placed under this section of the specifications shall be tested and shall not vary by more than 1/8 inch from the lower edge of a 10-foot straightedge when it is placed in the longitudinal direction (including across transverse joints), and when it is placed in the transverse direction across longitudinal joints;

- The surface of any lift of asphaltic concrete placed under this section of the specifications, other than the final lift, shall be tested and shall not vary by more than 1/4 inch from the lower edge of a 10-foot straightedge when it is placed in the longitudinal direction (including across transverse joints), and when it is placed in the transverse direction across longitudinal joints; and

- All deviations exceeding the specified tolerances above shall be corrected by the contractor, to the satisfaction of the Engineer.

The asphaltic concrete hot plant shall conform to the requirements of Section 403 of the specifications.

The moisture content of the asphaltic concrete immediately behind the paver shall not exceed 0.5 percent.  The moisture content will be determined in accordance with the requirements of AASHTO T 329.

Asphaltic concrete shall be placed only when the temperature of the surface on which the asphaltic concrete is to be placed is at least 65 degrees F.

At any time, the Engineer may require that the work cease or that the work day be reduced in the event that weather conditions, either existing or expected, are anticipated to have an adverse effect upon the asphaltic concrete.

All wheels and tires of compactors shall be wetted with water, or if necessary soapy water, or a release agent in order to prevent the sticking of asphaltic concrete. All other equipment surfaces shall be treated when necessary with a release agent. Only release agents evaluated through AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) are acceptable for use. The results from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) testing, when tested in accordance with AASHTO T 383, shall conform to the requirements shown in the table below:

| RELEASE AGENT TEST | REQUIREMENT |
| --- | --- |
| Asphalt Stripping Test Diluted Non-Diluted (Full Strength) | No Stripping No Stripping |
| Asphalt Performance Test | Less than or equal to 10.0% after the third cycle |

Release agents which degrade, dissolve, or in any way damage the bituminous material shall not be used.  Diesel fuel shall not be used as a release agent.

Asphaltic concrete immediately behind the laydown machine shall be in a thoroughly mixed, free-flowing, and workable condition, be free of lumps and crusts, and have a minimum temperature of 275 degrees F.

All courses of asphaltic concrete shall be placed and finished by means of self-propelled paving machines except under certain conditions or at certain locations where the Engineer deems the use of self-propelled paving machines impractical.

The speed of the paving machine shall be coordinated with the production of the plant and an adequate number of trucks for hauling asphaltic concrete shall be available in order to achieve, as far as practical, a continuous operation.

Self-propelled paving machines shall spread the mixture within the specified tolerances, without segregation or tearing, true to the line, grade, and crown indicated on the project plans.  Pavers shall be equipped with hoppers and augers which will distribute the mixture uniformly in front of adjustable screeds.

Pavers shall be equipped with a screed for the full width being paved, heated if necessary, and capable of spreading and finishing all courses of asphaltic concrete.

Pavers shall be equipped with automatic screed controls with sensors for either or both sides of the paver, capable of sensing grade from an outside reference line, sensing the transverse slope of the screed, and providing the automatic signals which operate the screed to maintain the desired grade and transverse slope.

Failure of the control system to function properly shall be cause for the suspension of the placing of asphaltic concrete.

The base or subgrade upon which asphaltic concrete is to be placed shall be prepared and maintained in a firm condition until asphaltic concrete is placed.  It shall not be frozen or excessively wet.

Before asphaltic concrete is placed, the surface to be paved shall be cleaned of all objectionable material and tacked with bituminous material in accordance with the requirements of Section 404 of the specifications.

Longitudinal joints of each course shall be staggered a minimum of 1 foot with relation to the longitudinal joint of any immediate underlying course.  Longitudinal joints shall be located within 1 foot of the center of a lane or within 1 foot of the centerline between two adjacent lanes.

The contractor shall schedule its paving operations to minimize exposed longitudinal edges.  Unless otherwise approved by the Engineer, the contractor shall limit the placement of asphaltic concrete courses, in advance of adjacent courses, to one shift of asphaltic concrete production.  The contractor shall schedule its paving operations in such a manner to eliminate exposed longitudinal edges over weekends or holidays.

### 409-3.02	Compaction:

Compaction shall consist of an established sequence of coverage using specified types of compactors.  A pass shall be defined as one movement of a compactor in either direction.  Coverage shall be the number of passes as are necessary to cover the entire width being paved.

The rolling sequence, the type of compactor to be used and the number of coverages required shall be as follows:

| Rolling Sequence | Type of Compactor |  | No. of Coverages |  |
| --- | --- | --- | --- | --- |
|  | Option No. 1 | Option No. 2 | Option No. 1 | Option No. 2 |
| Initial | Static Steel | Vibrating Steel | 1 | 1 |
| Intermediate | Pneumatic Tired | Vibrating Steel | 2 - 6* | 2 - 4* |
| Finish | Static Steel | Static Steel | 1 - 3 | 1 - 3 |
| Note: * Based on the roller pattern which exhibits the best performance. |  |  |  |  |

The Engineer shall select the option for compaction and, when pneumatic-tired compactors are used, will designate the tire pressure.

Steel wheel compactors shall not be used in the vibratory mode for courses of 1 inch or less in nominal thickness nor when the temperature of the asphaltic concrete falls below 180 degrees F.  Steel wheel compactors shall weigh not less than 8 tons.

Initial and intermediate compaction shall be completed before the temperature of the asphaltic concrete falls below 200 degrees F.  All edges shall be rolled with a pneumatic tired compactor, or other methods approved by the Engineer, while the mixture is still hot.

Compaction will be deemed to be acceptable on the condition that the asphaltic concrete is compacted using the type of compactors specified, ballasted and operated as specified and with the number of coverages of the compactors as specified.

### 409-3.03	Acceptance:

Asphaltic concrete will be accepted complete in place unless the result of any test varies from the contractor’s mix design target value (TV) as follows:

| Test Property | Allowable Variation from Target Value |  |
| --- | --- | --- |
| Gradation (Sieve sizes) |  |  |
| 3/8 inch | TV –10.0 | TV + 10.0 |
| No. 8 | TV – 8.0 | TV + 8.0 |
| No. 40 | TV – 6.0 | TV + 6.0 |
| No. 200 | TV – 2.5 | TV + 2.5 |
| Asphalt Cement Content | TV – 0.60 | TV + 0.70 |
| Effective Voids | TV –2.5 | TV + 2.0 |

Within 25 days after receiving notice of any failing test result(s), the contractor may submit a written proposal to accept the material represented by the failing test result(s), in place, at a reduction in cost.  If the failing test result(s) are only on Asphalt Cement Content and/or Effective Voids, the reduction in cost will be $5.00 per ton.  If the failing test result(s) are only on Gradation, the reduction in cost will be $3.00 per ton.  If the failing test result(s) are on Asphalt Cement Content and/or Effective Voids, and also on Gradation, the reduction in cost will be $5.00 per ton.  The proposal shall contain an engineering analysis of the anticipated performance (i.e. reduction in serviceability, in years) of the asphaltic concrete if left in place.  The engineering analysis shall also detail the potential root cause of the problem, any proposed corrective action, and the anticipated effect of such corrective action on the performance.  The engineering analysis shall only include acceptance or referee test results, as applicable to the standard specifications. The engineering analysis shall include the expected additional cost to the Department (over original performance life) to maintain the pavement at an acceptable condition. The engineering analysis shall include supporting information such as pictures of the area, control charts, plant and field records, etc. The engineering analysis shall be performed by an independent professional engineer, who is not an employee of the contractor or materials supplier, experienced in asphaltic concrete testing and the development of asphaltic concrete mix designs.

Within three working days, the Engineer will determine whether or not to accept the contractor’s proposal.  If the proposal is accepted, the asphaltic concrete shall remain in place, at a reduction in cost per ton, as described above, and any necessary corrective action shall be performed at no additional cost to the Department.  If the proposal is not accepted, the asphaltic concrete shall be removed at no additional cost to the Department and replaced with asphaltic concrete meeting the requirements of these specifications.

The contractor may request that a sample with a failing test result(s) on gradation and/or asphalt cement content be allowed to remain in place without the completion of an engineering analysis if the application of a self-directed target value change as outlined in section 409-2.04 would have brought the failing test result(s) to within the specified tolerances. This proposal must be made to the Engineer in writing with justification. Once accepted, the material will be allowed to remain in place at the maximum negative pay factor(s). Maximum negative are defined as a minus $3.00 per ton for mixture properties lots in reject for Gradation only, minus $5.00 per ton for mixture properties lots in reject for Asphalt Cement Content and/or Effective Voids only, and minus $5.00 per ton for mixture properties lots in reject for Asphalt Cement Content and/or Effective Voids and also Gradation.

If the asphaltic concrete, represented by failing test results, is used as temporary pavement which will be removed prior to, or after, the completion of construction, the Engineer reserves the right to waive the engineering analysis and accept the material in place, at a cost reduction described above, provided the temporary pavement maintains the functionality of the intended use for the duration of the project.

## 409-4	Method of Measurement:

Asphaltic concrete will be measured by the ton for the mixture actually used, which will include the weight of mineral aggregate, bituminous material, and mineral admixture.  Measurement will include any weight used in construction of intersections, turnouts, curbs, spillways and spillway inlets, ditches, catch basin entrances, median strips, sidewalks, or other miscellaneous items or surfaces.

## 409-5	Basis of Payment:

### 409-5.01	General:

The accepted quantities of asphaltic concrete, measured as provided above, will be paid for at the contract unit price per ton for the bituminous mixture complete in place.

No direct payment will be made for the bituminous material and mineral admixture in the asphaltic concrete, or the bituminous material for tack coat and application of tack coat, the price being considered as included in the price paid for asphaltic concrete.

Asphaltic concrete may be measured, by volume, upon the execution of a supplemental agreement which will specify the manner in which the volume is determined.  The volume will include the volume of mineral aggregate, bituminous material, mineral admixture, and any necessary blending material.

### 409-5.02	Reduction for Noncompliance:

A reduction in payment to the contractor for asphaltic concrete will be made for asphalt cement (bituminous material) that do not meet the requirements of Section 1005 as determined by corresponding test results.  Adjustments in payment will be made in accordance with the requirements of Table 1005-1.