*                           USE STORED SPECIFICATION 109PAVSM WHEN AN                           *

*              INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE               *

*                                 PAVEMENT SMOOTHNESS IS SPECIFIED IN                                   *

*                                          THE MATERIALS DESIGN REPORT                                          *

*	USE IN CONJUNCTION WITH THE FOLLOWING:					    *

*		BID ITEM:							9240170			    *

*		STORED SPECIFICATIONS:			924CQC			    *

*									        1001MATL			    *

*	FILL IN THE FOLLOWING (SHOWN IN RED TEXT):					    *

*		416-3			UNIT WEIGHTS				(As Needed)		    *

*					PERCENTAGES				(As Needed)		    *

*		416-3.03(B)	TYPE OF ASPHALT BINDER		(1 place)		    *

(416ACES, 02/20/25)

SECTION 416	ASPHALTIC CONCRETE – END PRODUCT

416-1			Description: the second paragraph of the Standard Specifications is revised to read:

Reclaimed asphalt pavement (RAP), as defined in Subsection 416-3.04 of the specifications, may be used in the mixture provided all requirements of the specifications are met. References to the use of RAP in this section apply only if RAP is utilized as part of the mixture. ADOT Materials Practice and Procedure Directive No. 20, “Guidance on the Use of Reclaimed Asphalt Pavement (RAP) in Asphaltic Concrete”, shall be used in conjunction with the requirements of the specifications.

416-2			Asphaltic Concrete Mix Design Criteria: of the Standard Specifications is revised to read:

Mix designs shall be developed utilizing a minimum ratio of three (3) for the lift thickness to nominal maximum aggregate size.

Mix designs shall be developed by the contractor on the basis of the following criteria and tested in accordance with the requirements of the following test methods:

| Criteria |  |  | Requirements |  |  |  | Arizona Test |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1/2” Mix |  | 3/4” Mix | Base Mix | Method |
| 1. Voids in Mineral Aggregate: %, Range |  |  | 15.5 - 18.5 |  | 15.0 - 18.0 | 14.5 - 17.0 | Note (2) |
| 2. Effective Voids: %, Range |  |  | 4.0 ± 0.2 |  | 4.0 ± 0.2 | 4.0 ± 0.2 | Note (2) |
| 3. Absorbed Asphalt: %, Range |  |  | 0 - 1.0 |  | 0 - 1.0 | 0 - 1.0 | Note (2) |
| 4. Index of Retained Strength: %, Minimum |  |  | 60 (Note 1) |  | 60 (Note 1) | 60 (Note 1) | Note (3) |
| 5. Wet Strength: psi, Minimum |  |  | 150 |  | 150 | 150 | Note (3) |
| 6. Stability: pounds, Minimum |  |  | 2,000 |  | 2,000 | 3,000 | Note (2) |
| 7. Flow: 0.01-inch, Range |  |  | 8 - 16 |  | 8 - 16 | 8 - 16 | Note (2) |
| 8. Mix Design Grading Limits |  |  |  |  |  |  | 201 |
|  | Percent Passing |  |  |  |  |  |  |
| Sieve Size | 1/2 inch Mix |  |  | 3/4 inch Mix |  | Base Mix |  |
|  | Without Admix. | With Admix. |  | Without Admix. | With Admix. | Without Admix. | With Admix. |
| 1-1/4 inch |  |  |  |  |  | 100 | 100 |
| 1 inch |  |  |  | 100 | 100 | 90 -100 | 90 - 100 |
| 3/4 inch | 100 | 100 |  | 90 - 100 | 90 - 100 | 85 - 95 | 85 - 95 |
| 1/2 inch | 90 - 100 | 90 - 100 |  | --- | --- | --- | --- |
| 3/8 inch | 67 - 82 | 67 - 82 |  | 62 - 77 | 62 - 77 | 57 - 72 | 57 - 72 |
| No. 8 | 40 - 48 | 41 - 49 |  | 37 - 46 | 38 - 47 | 32 - 42 | 33 - 43 |
| No. 40 | 10 - 18 | 11 - 19 |  | 10 - 18 | 11 - 19 | 8 - 16 | 9 - 17 |
| No. 200 | 1.5 - 4.5 | 2.5 - 6.0 |  | 1.5 - 4.5 | 2.5 - 6.0 | 1.5 - 3.5 | 2.5 - 5.0 |
| Notes: If the average elevation of the project is above 3,500 feet, the index of retained strength shall be a minimum of 70 percent. For mixes without RAP, Arizona Test Method 815. For mixes with RAP, Arizona Test Method 833. For mixes without RAP, Arizona Test Method 802 (as modified by Arizona Test Method 815). For mixes with RAP, Arizona Test Method 802 (as modified by Arizona Test Method 833). |  |  |  |  |  |  |  |

The ratio of the mix design composite gradation target for the No. 200 sieve including mineral admixture, to the effective asphalt content shall be within the range 0.7 to 1.3.

416-3			Materials: of the Standard Specifications is modified to add:

For comparative purposes, quantities shown in the bidding schedule have been calculated based on the following data:

(In the following two tables, use only the columns called for in the

Materials Design Report;  exclude all of either table if no

column is called for in the Materials Design Report.)

| Standard Mixes | 1/2” Mix | 3/4” Mix | Base Mix |
| --- | --- | --- | --- |
| Unit Weight, (lb./cu. ft.) | XXX | XXX | XXX |
| Asphalt Cement, % | X.X | X.X | X.X |
| Mineral Admixture, % | 1.0 | 1.0 | 1.0 |

| Special Mixes | 1/2” Mix | 3/4” Mix | Base Mix |
| --- | --- | --- | --- |
| Unit Weight, (lb./cu. ft.) | XXX | XXX | XXX |
| Asphalt Cement, % | X.X | X.X | X.X |
| Mineral Admixture, % | 1.0 | 1.0 | 1.0 |

416-3.03 (B)	Virgin Bituminous Material: the first paragraph of the Standard Specifications is revised to read:

Virgin asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005.  The type of virgin asphalt binder shall be PG XXXXX or, if RAP is used in the mixture, the virgin asphalt binder shall be as required to meet the blending requirements in Subsection 416-3.03(C) and Arizona Test Method 833.

416-4			Mix Design:  the fifth paragraph of the Standard Specifications is revised to read:

The contactor may propose the use of a mix design that has been developed for a previous project that is less than a year old with no additional requirements. The proposed mix design shall meet the requirements of these specifications. If the proposed mix design is greater than one year old but less than two years old, the contractor shall provide evidence that the type and source of bituminous material, the type of mineral admixture, and the source and methods of producing virgin mineral aggregate and RAP have not changed since the formulation of the previous mix design. The contractor shall also provide current test results for all specified characteristics of the mineral aggregate and RAP proposed for use. The Engineer will determine if the previously used mix design is suitable for the intended use and if the previous use of the mix design was satisfactory to the Department. The Engineer will either approve or disapprove the proposed mix design. Should the Engineer disapprove the use of the previously used mix design, the contractor shall prepare and submit a new mix design proposal in accordance with the requirements of these specifications.

416-4			Mix Design: the “Measured Characteristics – Allowable Self-Directed Target Changes” table of the Standard Specifications is revised to read:

| MEASURED CHARACTERISTICS | ALLOWABLE SELF-DIRECTED TARGET CHANGES |
| --- | --- |
| Gradation (sieve size): 3/8 Inch No. 8 No. 40 No. 200 | ±4% from the mix design target value ±4% from the mix design target value ±2% from the mix design target value None |
| Asphalt Cement Content | Within range of +0.4% to -0.2% from the mix design target value |
| Effective Voids | None |

416-6			Construction Requirements:  the twelfth paragraph of the Standard Specifications is revised to read:

All wheels and tires of compactors shall be wetted with water, or if necessary soapy water, or a release agent in order to prevent the sticking of asphaltic concrete. All other equipment surfaces shall be treated when necessary with a release agent. Only release agents evaluated through AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) are acceptable for use. The results from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) testing, when tested in accordance with AASHTO T 383, shall conform to the requirements shown in the table below.

416-6			Construction Requirements:  the second row of the “Release Agent Test – Requirement” table of the Standard Specifications is hereby deleted:

416-7.04(A)		General: the fifth paragraph of the Standard Specifications is revised to read:

The target values for gradation, Asphalt Cement Content, and Effective Voids are given in the contractor’s mix design.  The Upper Limits (UL) and Lower Limits (LL) of acceptable production of each of the measured characteristics are as follows:

| Measured Characteristics | LL (Note 1) | UL (Note 1) |
| --- | --- | --- |
| Gradation (Sieve size): 3/8 inch | TV - 8.0 | TV + 8.0 |
| No. 8 No. 40 No. 200 | TV - 8.0 TV - 5.0 TV - 2.0 | TV + 8.0 TV + 5.0 TV + 2.0 |
| Asphalt Cement Content | TV - 0.50 | TV + 0.50 |
| Effective Voids | TV - 2.0 | TV + 2.0 |
| Notes: - The limits are used in the statistical calculations for Quality Index. Acceptance is controlled by the variability of the produced material and every effort should be made to strive for the applicable target value (TV). |  |  |

416-7.05(B)		Courses Greater than 1 – 1/2 Inches in Nominal Thickness: of the Standard Specifications is revised to read:

Compaction control shall be the responsibility of the contractor. The number and types of rollers shall be the contractor's responsibility and shall be sufficient to meet these requirements.

All edges shall be rolled with a pneumatic tired compactor, or other methods approved by the Engineer, while the mixture is still hot.

A compaction lot shall be identical to the mixture properties lot described in Subsection 416-7.04 of the specifications. Lots encompassing more than one project shall be separated in accordance with Subsection 416-9(D) of the specifications. Each lot shall be tested for acceptance.

Twenty cores shall be taken for each lot by the contractor, under the observation of the Engineer. The Engineer will designate 10 random locations within the lot, and the contractor shall take two cores at each location; however, if more than one shift constitutes a lot, two cores shall be taken from a minimum of two random locations each shift, or as directed by the Engineer. The Engineer will save one core from each location for 15 days after written notification to the contractor of test results for the lot has been made. Randomly selected locations will be determined to the nearest 0.5 foot in the transverse direction and to the nearest foot in the longitudinal direction of the pavement course; however, the outside 1 foot of the unconfined pavement course will be excluded from testing as shown in ADOT Materials Practice and Procedure Directive (P.P.D.) No. 18, “Determining Sample Times and Locations for End Product Asphaltic Concrete”. Unless otherwise indicated in the project plans, shoulders shall be excluded from compaction lot testing on rehabilitation projects. Unless otherwise indicated in the project plans, placements without constant width including gore areas, tapers, and turn radii shall be excluded from compaction lot testing on all projects. P.P.D. No. 18 also addresses areas to be excluded relative to longitudinal joints. Areas excluded from testing will be compacted in accordance with Subsection 416-7.05(A) of the specifications. Cores shall be taken utilizing mechanical coring equipment in accordance with the requirements of Arizona Test Method 104. Cores shall be a minimum of 4 inches in diameter and shall be taken not later than two working days after placement of the asphaltic concrete. The cores shall be delivered to the Engineer immediately upon being taken. The bulk density of each core will be determined by the Engineer in accordance with the requirements of Arizona Test Method 415. The test results will be furnished to the contractor within four working days of receipt of cores by the Engineer. In areas where more than one lift is placed in the same lot, coring shall be accomplished through the full depth of the lifts after the final lift is placed, and the compaction density shall be based on the full depth of the lifts.

The target value for compaction shall be 5.5 percent in-place air voids. In-place air voids shall be determined in accordance with Arizona Test Method 424. The maximum theoretical density used in the determination of air voids will be the average of the four maximum theoretical densities determined for the lot in Subsection 416-7.04 of the specifications.

The Upper Limit (UL) is 8.0 percent in-place air voids and the Lower Limit (LL) is 3.0 percent in-place air voids. The Engineer will determine the PT for compaction in accordance with Subsection 416-9(I), and utilizing Table 416-1 of the specifications will determine the compaction pay factor.

In the event the contractor elects to question the core test results, the contractor may request referee testing in accordance with Subsection 416-9(J) of the specifications.

416-7.06		Smoothness and Surface Tolerances: of the Standard Specifications is revised to read:

Asphaltic concrete shall be compacted as required, smooth and true to the required lines, grades, and dimensions.

The Special Provisions may require the smoothness of the final pavement surface to be tested in accordance with Subsection 109.13 of the specifications.

Regardless of whether testing in accordance with Subsection 109.13 of the specifications is specified or not, the following requirements shall be met:

- The surface of any lift of asphaltic concrete placed under this section of the specifications, shall be tested and shall not vary by more than 1/4 inch from the lower edge of a 10-foot straightedge when it is placed in the longitudinal direction (including across transverse joints), and when it is placed in the transverse direction across longitudinal joints; and

All deviations exceeding the specified tolerances above shall be corrected by the contractor, to the satisfaction of the Engineer.

416-8(C)		Mineral Admixture: of the Standard Specifications is revised to read:

No separate measurement or payment will be made for mineral admixture, the cost being considered as included in the cost of the asphaltic concrete.

416-9			Basis of Payment: of the Standard Specifications is revised to read:

The accepted quantities of asphaltic concrete, measured as provided above, will be paid for at the contract unit price adjusted by the appropriate pay factors as hereinafter provided.

When Warm Mix Asphalt (WMA) technologies are used in the mixture, no separate payment will be made for WMA additives or technologies, necessary hot plant modifications, or other associated costs.

For the purpose of determining acceptability and appropriate pay factors, each unit of asphaltic concrete will be included in three separate lots: a “spread lot”, a “mixture properties lot”, and a “compaction lot”.  The total unit price for any unit of accepted asphaltic concrete will be the contract unit price, adjusted by the applicable spread lot pay factor, mixture properties lot pay factor, and compaction lot pay factor.

The contractor may request to place the first lot of each mix type as a test strip.  Requests to place a test strip shall be made in writing and acknowledged by the Engineer prior to start of production.  A test strip shall be limited to 1,000 tons and may only be placed on shoulders, ramps, cross roads, or other areas approved by the Engineer.  A test strip shall be excluded from the mixture properties lot pay factor and the compaction lot pay factor; however, all other provisions of Subsection 416-9 shall still apply to such areas.

The Engineer may exclude asphaltic concrete from the spread lot and from the spread lot pay factor calculations if the Engineer determines that the proposed use of the material or the existing surface conditions are not conducive to the use of spread lots.

The Engineer may exclude certain locations from the mixture properties lot and/or compaction lot and from the random sampling used in determining the mixture properties lot pay factor and/or the compaction lot pay factor should the Engineer determine that the location of the work precludes normal construction operations.

(A)		Spread Lot Pay Factor:

The spread lot pay factor will be determined in accordance with Subsection 416-7.03.  If the quantity in a spread lot is found to vary by more than + 5.0 percent from the required quantity, no payment will be made for the material which exceeds + 5.0 percent, including asphalt cement and mineral admixture.  If the quantity is found to vary by more than - 12.0 percent from the required quantity, the spread lot will be rejected.

(B)		Mixture Properties Lot Pay Factor:

The mixture properties lot pay factor shall be determined in accordance with the following procedure:

- The individual PT values and pay factors for Gradation, Asphalt Cement Content, and Effective Voids shall be determined as set forth in Subsection 416-7.04 of the specifications.

- A single pay factor shall be determined for Gradation and Asphalt Cement Content.  That pay factor shall be the lowest pay factor for the individual measured characteristics for Gradation and Asphalt Cement Content.

- If no individual PT value in (1) above is less than 50, the mixture properties lot pay factor shall be the sum of the pay factor determined in (2) above and the Effective Voids pay factor.  The negative pay factor for mixture properties shall not exceed $3.00 per ton.  If any individual PT value is less than 50, the lot is in reject and the provisions in Subsection 416-9(E) of the specifications shall apply.

(C)		Compaction Lot Pay Factor:

The compaction lot pay factor shall be determined as set forth in Subsection 416-7.05(B) of the specifications.

(D)		Determination of Lot Pay Factors on Contracts Involving Multiple Projects:

When more than one project is included in a single contract, placement during a shift or half shift of production may encompass more than one project.  In such case, the applicable spread lot pay factor, mixture properties lot pay factor, and compaction lot pay factor for each project shall be determined as follows:

(1)	Spread lot pay factors will be determined separately for each project utilizing the procedure set forth in Subsection 416-7.03 of the specifications.

(2)	The individual PT values and pay factors for Gradation, Asphalt Cement Content, and Effective Voids will be determined from the results of the random samples taken and tested in accordance with Subsection 416-7.04 of the specifications, regardless of which project(s) the samples fall within.

(3)	PT values and pay factors for compaction, for those areas subject to Subsection 416-7.05(B) of the specifications, shall be determined from separate sets of core samples for each project utilizing the procedure set forth in that Subsection.

(4)	The mixture properties lot pay factor shall be determined separately for each project in accordance with Subsection 416-9(B) of the specifications, utilizing the individual pay factors determined in (2) above.

(5)	The compaction lot pay factor shall be determined separately for each project in accordance with Subsection 416-9(C) of the specifications, utilizing the pay factor determined in (3) above.

(E)		Acceptability:

Asphaltic concrete included in any mixture properties lot possessing an individual PT value lower than 50 for Gradation, Asphalt Cement Content, or Effective Voids will be rejected. Asphaltic concrete included in any compaction lot possessing a PT value lower than 50 will be rejected.

Within 25 days, or as agreed upon by the Engineer, after receiving notice that a spread lot, mixture properties lot, or compaction lot of asphaltic concrete has been rejected by the Engineer, the contractor may submit a written proposal to accept the material in place at the applicable maximum negative pay factor(s). Maximum negative pay factors are defined as a minus $1.00 per ton for spread lots, minus $5.00 per ton for compaction lots, minus $3.00 per ton for mixture properties lots in reject for gradation only, minus $5.00 per ton for mixture properties lots in reject for Asphalt Cement Content and/or Effective Voids only, and minus $5.00 per ton for mixture properties lots in reject for Asphalt Cement Content and/or Effective Voids and also Gradation. Positive mixture properties lot pay factors become zero when the compaction lot is in reject and the material is allowed to be left in place. In addition, for any mixture properties lot that is in reject due to Asphalt Cement Content but allowed to remain in place, payment shall not be made for asphalt cement quantities in excess of the upper limit (UL) as determined in Subsection 416-7.04(A) of the specifications.

The proposal shall contain an engineering analysis of the anticipated performance (i.e. reduction in serviceability, in years) of the asphaltic concrete if left in place. The engineering analysis shall also detail the potential root cause of the problem, any proposed corrective action, and the anticipated effect of such corrective action on the performance. The engineering analysis shall only include acceptance or referee test results, as applicable to the standards specifications. The engineering analysis shall include the expected additional cost to the Department (over original performance life) to maintain the pavement at an acceptable condition. The engineering analysis shall include supporting information such as pictures of the area, control charts, plant and field records, etc. The engineering analysis shall be performed by an independent professional engineer experienced in asphaltic concrete testing and the development of asphaltic concrete mix designs. If a rejected mixture properties lot or a rejected compaction lot is submitted for referee testing by the contractor, the 25 days allowed to prepare an engineering analysis will begin upon notification of referee test results.

The contractor may submit a written proposal without an engineering analysis for Engineer’s evaluation and approval, that a mixture properties lot with a PT value lower than 50 on gradation and/or asphalt cement content be allowed to remain in place if the application of a Self-Directed Target Change as outlined in Subsection 416-4 of the specifications would bring the PT value to 50 or greater. This written request shall also include the proposed revised PT calculations. Upon Engineer’s verification and approval of the request, the material shall remain in place at the maximum negative pay factor(s) specified in this subsection for the mixture properties lot in reject.

Within three working days, the Engineer will determine whether or not to accept the contractor's proposal. If the proposal is not accepted, the asphaltic concrete shall be removed at no additional cost to the Department and replaced with asphaltic concrete meeting the requirements of these specifications. If the proposal is accepted, the asphaltic concrete shall remain in place at the applicable maximum negative pay factor(s), and any necessary corrective action shall be performed at no additional cost to the Department.

The Department reserves the right to suspend the work should any of the following conditions occur:

(1)	The occurrence of two or more rejected lots within any 10 consecutive production lots.

(2)	The occurrence of three consecutive negative mixture properties lot pay factors or three consecutive negative compaction lot pay factors.

(3)	The occurrence of five or more pay factors that are negative either for a mixture properties lot or for a compaction lot within any 10 consecutive production lots.

If the Department elects to suspend the work for any of these conditions, the contractor shall either submit a revised mix design in accordance with Subsection 416-4 of the specifications, or submit for the Engineer's approval a written engineering analysis.  The engineering analysis shall detail the course of action necessary to correct deficiencies in the contractor’s present production methods such that further production can be accomplished without excessive amounts of asphaltic concrete in penalty or rejection.  If approved by the Engineer, the revised mix design, or the course of action proposed in the engineering analysis, shall be implemented, and the work may continue.  Costs or delays due to the provisions of this subsection are not compensable.

(F)		Asphalt Cement:

(1)	Non-RAP Mixes:

Payment for asphalt cement will be made by the ton.  Adjustments in payment shall be made in accordance with the requirements of Subsection 1005-3.01 of the specifications.

(2)	Mixes Containing RAP:

When RAP is used in the mixture, payment for asphalt cement will be made by the ton for the total asphalt cement as determined in Subsection 416-8(B)(2) of the specifications.  Adjustments in payment shall be made in accordance with the requirements of Subsection 1005-3.01 of the specifications for the virgin binder only.

(G)		Smoothness:

When required in the Special Provisions, payment for smoothness shall be made in accordance with the requirements of Subsection 109.13 of the specifications.

(H)		Statistical Acceptance:

The “Total Percentage of Lot Within UL and LL (PT)” shall be determined in accordance with Subsection 109.11 of the Specifications.

Pay Factors (PF) shall be determined by entering Table 416-1 with PT.

| TABLE 416-1 PAY FACTORS |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Material Spread |  | Mixture Properties and Compaction |  |  |  |
| Negative Variance % | Pay Factor (Dollars per Ton) | PT | Pay Factors (Dollars per Ton) |  |  |
|  |  |  | Gradation and Asphalt Cement Content | Effective Voids | Compaction |
| 2.1 - 3.0 | - 0.10 | 100 | 0.00 | + 2.00 | + 2.00 |
| 3.1 - 4.0 | - 0.20 | 95 - 99 | 0.00 | + 1.00 | + 1.00 |
| 4.1 - 5.0 | - 0.30 | 90 - 94 | 0.00 | 0.00 | 0.00 |
| 5.1 - 6.0 | - 0.40 | 85 - 89 | 0.00 | - 0.25 | - 0.25 |
| 6.1 - 7.0 | - 0.50 | 80 - 84 | - 0.25 | - 0.50 | - 0.50 |
| 7.1 - 8.0 | - 0.60 | 75 - 79 | - 0.50 | - 0.75 | - 0.75 |
| 8.1 - 9.0 | - 0.70 | 70 - 74 | - 0.75 | - 1.00 | - 1.00 |
| 9.1 - 10.0 | - 0.80 | 65 - 69 | - 1.00 | - 1.25 | - 1.25 |
| 10.1 - 11.0 | - 0.90 | 60 - 64 | - 1.50 | - 1.50 | - 1.75 |
| 11.1 - 12.0 | - 1.00 | 55 - 59 | - 2.00 | - 2.00 | - 2.25 |
| More than 12.0 | Reject | 50 - 54 | - 2.50 | - 2.50 | - 3.00 |
|  |  | Less than 50 | Reject-See Subsection 416-9(E) |  |  |
| See Subsections 416-9(A) and (E) |  |  |  |  |  |

(I)		Mixture Properties Lot Referee Testing:

(1)	Referee Testing Performed for Mixture Properties Only:

Within 15 days after written notification to the contractor of test results for a particular mixture properties lot, the contractor may make a written request for referee testing.  The referee testing shall be performed by an independent approved laboratory designated by the Department.  The testing of the samples will be performed by the independent testing laboratory without knowledge of the specific project conditions such as the identity of the contractor or mix design laboratory, the test results by the Department, or the mix design targets for gradation and effective voids.  The asphaltic concrete samples previously saved will be tested for the following properties:

| Test Property | Test Method |  |
| --- | --- | --- |
| Asphalt Cement Content (See Note 1 below) | Arizona Test Method 427 (428 for RAP mixes) |  |
| Gradation |  |  |
| Marshall Density and Stability | Arizona Test Method 410 |  |
| Maximum Theoretical Density | Arizona Test Method 417 |  |
| Effective Voids | Arizona Test Method 424 |  |
| Note: (1) If a correction to the Asphalt Cement Content by ignition furnace testing is made in accordance with Subsection 416-7.04(B) of the specifications, or if RAP is used in the mixture, the Asphalt Cement Content shall not be subject to referee testing. |  |  |

The results of the referee testing will be binding on both the contractor and the Department.

Using the referee testing results, the Engineer will determine new PT’s for all characteristics, with the exception of Asphalt Cement Content if a correction to the ignition furnace value was made as specified in Subsection 416-7.04(B) of the specifications, or if RAP is used in the mixture.

When referee testing is performed on a mixture properties lot, the referee test result for the average maximum theoretical density will be used to determine a new PT for compaction.

The Department will pay for the referee testing; however, if the combined pay factor of the lot (mixture properties plus compaction) does not improve or is reduced, or if either the mixture properties lot or compaction lot remains in reject or is placed in reject, payment to the contractor for asphaltic concrete shall be reduced by the amount of the cost of the referee testing for the mixture properties of that particular lot.

(2)	Referee Testing Performed for Compaction Only:

Within 15 days after written notification to the contractor of test results for a particular compaction lot, the contractor may make a written request for referee testing.  The bulk density of each of the cores previously saved will be determined in accordance with the requirements of Arizona Test Method 415 by an independent testing laboratory designated by the Department.  The testing of the cores will be performed by the independent testing laboratory without knowledge of the specific project conditions, such as the identity of the contractor or mix design laboratory, or the test results by the Department.  The percent air voids will be determined in accordance with Arizona Test Method 424.  The maximum theoretical density used in the determination of air voids will be the average of the four maximum theoretical densities determined for the lot in Subsection 416-7.04 of the specifications.

The results of the referee testing will be binding on both the contractor and the Department.

When referee testing is performed on the compaction lot, the Engineer will determine a new PT for compaction using the referee testing results.

The Department will pay for the referee testing; however, if the pay factor of the compaction lot does not improve or is reduced, or the compaction lot remains in reject or is placed in reject, payment to the contractor for asphaltic concrete will be reduced by the amount of the cost of referee testing for the compaction of that particular lot.

(3)	Referee Testing Performed for Both Mixture Properties and Compaction:

When referee testing is performed, as described above, for both the mixture properties lot and the compaction lot, the Engineer will use the referee test results to determine new PT’s as specified in Subsections 416-9(I)(1) and 416-9(I)(2) of the specifications.

The Department will pay for the referee testing; however, if the combined pay factor of the lot (mixture properties plus compaction) does not improve or is reduced, or if either the mixture properties lot or compaction lot remains in reject or is placed in reject, payment to the contractor for asphaltic concrete shall be reduced by the amount of the cost of the referee testing for the mixture properties and compaction of that particular lot.