(706REFPMR, 11/21/24)

SECTION 706	RAISED PAVEMENT MARKERS:

706-2.02		Reflective Pavement Markers: the title and text of the Standard Specifications is revised to read:

706-2.02		Raised Retroreflective Pavement Markers:

The type of the raised retroreflective pavement markers shall be as shown on the plans.

Permanent raised retroreflective pavement markers shall conform to the performance requirements of ASTM D4280, Type A, B, or E, and shall meet the ASTM D4280 requirements for pavement markers with designation H for abrasion resistance and designation F for flexural strength. A list of approved permanent raised retroreflective pavement markers is shown on the Department’s Approved Products List. Copies of the most recent version of the APL are available on the internet from the ADOT Research Center, through its Product Evaluation Program.

Temporary raised retroreflective pavement markers  shall conform to the performance requirements of ASTM D4280, Type A, B, or E. Temporary raised retroreflective pavement markers, or permanent raised retroreflective pavement markers used as temporary, shall not be required to meet the ASTM D4280 designation H requirements for abrasion resistance.

706-2.03		Non-Reflective Pavement Markers and Reflectorized Dagmars: the title and text of the Standard Specifications is revised to read:

706-2.03		Non-Reflective Pavement Markers and Retroreflectorized Channel Markers:

Non-reflective pavement markers shall be of the following types:

| Type | Color |
| --- | --- |
| A | White |
| AY | Yellow |
| M | White |
| MY | Yellow |

Retroreflectorized Channel Markers shall be of the following types:

| Type | Color |
| --- | --- |
| J | White |
| JY | Yellow |

Non-reflective pavement markers and retroreflectorized channel markers shall consist of a heat-fired, vitreous ceramic base and a heat-fired, opaque glazed surface which will produce the required properties. Markers shall be produced from any suitable combination of intimately mixed clays, shales, flints, feldspars, or other inorganic material which will meet the properties herein required. Markers shall be thoroughly and evenly matured and free from defects which will affect appearance or serviceability.

The top surface of the marker shall be in reasonably close conformity with the configuration shown on the plans. Markers shall be convex and the radius of curvature shall be between 3-1/2 and 6 inches, except that the radius of the 1/2 inch nearest the edge may be less. All edges shall be rounded and any change in curvature shall be gradual. The top and sides shall be smooth and free of mold marks, pits, indentations, air bubbles, or other objectionable marks or discolorations.

Non-reflective pavement markers and retroflectorized channel markers shall meet the following requirements:

| Glaze Thickness: Inches | 0.005 Minimum |
| --- | --- |
| Moh Hardness: | 6 Minimum |
| Directional Reflectance: (White Only) Glazed Surface Body of Marker | 75 Minimum 70 Minimum |
| Yellowness Index: (White Only) Glazed Surface Body of Marker | 0.07 Maximum 0.12 Maximum |
| Color (Yellow Only): Purity: percent, range Dominant Wave Length: mu, range Total Luminous Reflectance (Y valve) | 75 - 96 579 - 585 0.41 Minimum |
| Compressive Strength: pounds | 1,500 Minimum |
| Water Absorption: percent | 2.0 Maximum |
| Autoclave | Glaze shall not spall, craze or peel |

Retroreflectorized channel markers shall have encapsulated lens reflectors conforming to standard manufacturing practices.

706-2.05		Bituminous Adhesive: of the Standard Specifications is revised to read:

The bituminous adhesive for pavement markers shall be a hot-melt adhesive, and shall conform to the requirements of ASTM D4280, Annex A1. A list of approved adhesives is shown on the Department’s Approved Products List (APL). Copies of the most current version of the APL are available on the internet from the ADOT Research Center, through its Product Evaluation Program.

706-4		Method of Measurement: of the Standard Specifications is revised to read:

Raised pavement markers will be measured as a unit for each marker furnished and placed.

706-5		Basis of Payment: of the Standard Specifications is revised to read:

The accepted quantities of raised pavement markers, measured as provided above, will be paid for at the contract unit price for the type designated in the bidding schedule, complete in place, including adhesive and surface preparation.