(1006PCC, 09/21/23)

SECTION 1006	PORTLAND CEMENT CONCRETE:

1006-2.01(A)	General: of the Standard Specifications is revised to read:

Cementitious material is defined as an inorganic material or a mixture of inorganic materials that sets and develops strength by chemical reaction with water by formation of hydrates and is capable of doing so under water.  In this specification, cementitious materials are defined as hydraulic cement (Portland cement, Portland-pozzolan cement or Portland-limestone cement) and supplementary cementitious materials (fly ash, natural pozzolan, or silica fume).

1006-2.01(B)	Hydraulic Cement: the first paragraph of the Standard Specifications is revised to read:

Hydraulic cement shall consist of Portland cement, Portland-pozzolan cement or Portland-limestone cement.

1006-2.01(B)	Hydraulic Cement: of the Standard Specifications is modified to add:

Portland-limestone cement shall conform to the requirements of ASTM C595 for blended hydraulic cement with moderate sulfate resistance, Type IL (MS).

1006-2.01(C)(2)	Flyash and Natural Pozzolan: of the Standard Specifications is revised to read:

Fly ash and natural pozzolan shall conform to the requirements of ASTM C618 for Class C, F, or N.

TABLE 1006-5	Design Criteria: the column heading of the third column of the Standard Specifications is revised to read:

|  |  | Cementitious Material Content: Lbs. per Cu Yd. Minimum - Maximum |  |  |
| --- | --- | --- | --- | --- |

1006-3.02(C)	Mix Design Submittal Requirements: the items (16) and (18) of the Standard Specifications are revised to read:

- Volume of each material measured to the nearest hundredth of a cubic foot;

- Total volume measured to the nearest hundredth of a cubic foot;

1006-7.02(A)	General: the fifth paragraph of the Standard Specifications is revised to read:

Concrete shall be sampled in accordance with ASTM C172 for acceptance testing of temperature, slump, unit weight and yield (when required) and air content (when required) as well as for fabrication of test cylinders for compressive strength determination at 28 days except that the concrete shall be sampled once during discharge at the middle portion of the batch. ASTM C172 includes sampling from stationary, paving and truck mixers, and from agitating and non-agitating equipment used to transport central-mixed concrete and from continuous mixing equipment as described in Specification ASTM C685/C685M. Sampling shall be at the point of discharge from truck mixers.  Sufficient care shall be taken to obtain a representative sample by diverting the entire stream of the concrete to prevent segregation. Samples shall be of sufficient size to perform all the required tests and fabricate the necessary test cylinders but in no case less than 1 cubic foot.

1006-7.02(B)	Class S and Class B Concrete: of the Standard Specifications is revised to read:

For Class S concrete with a compressive strength requirement less than 4000 psi, or Class B concrete, a strength test will consist of the average strength of two test cylinders.  However, if the compressive strengths of the two test cylinders differ by more than 10 percent from the average of the two, the strength test result shall be the cylinder with the highest compressive strength.

For Class S concrete with a compressive strength requirement equal to or greater than 4000 psi, or Class P concrete, the compressive strength of each sample shall be determined by averaging the results of the three test cylinders.  However, if the compressive strength of any one of the three test cylinders differs by more than 10 percent from the average of the three, its result shall be discarded and the compressive strength shall be the average of the remaining two cylinders.  Should the individual compressive strength of any two of the three remaining cylinders differ by more than 10 percent from the average of the three, the results will be discarded and the compressive strength shall be the strength of the remaining cylinder.

1006-7.03(A)(3)	Consistency: the third paragraph of the Standard Specifications is revised to read:

- When the concrete is pumped, samples for consistency will be taken as the concrete leaves the mixer.

TABLE 1006-10	Air Entrainment Requirements: the table of the Standard Specifications is revised to read:

| TABLE 1006-10 Air Entrainment Requirements |  |  |
| --- | --- | --- |
| Elevation | Air Entrainment Required | Required Air Content by Volume (%) |
| 3000 feet or above | Yes | 4 to 7 |
| Below 3000 feet | Contractor’s Option | ≤ 7 |