*** USE IF SPECIFIED IN THE MATERIALS DESIGN REPORT ***

*	USE IN CONJUNCTION WITH THE FOLLOWING:		           *

*		BID ITEM:							9240170			    *

*		STORED SPECIFICATIONS:			924CQC			    *

*									        1001MATL			    *

*									        104ENVIR			    *

* FILL IN THE FOLLOWING: 									     *

* Asphalt Concrete Mix type (1place) *

* SUBSECTION 1.0 *

* UNIT WEIGHT OF THE MIX (1 place) *

* SUBSECTION 3.0 *

* TYPE OF ASPHALT BINDER (1 place)  *

* SUBSECTION 3.03 *

(924SMA, 01/15/26)

ITEM 9240140 - MISCELLANEOUS WORK (STONE MATRIX ASPHALTIC CONCRETE):

ITEM 9240141 - MISCELLANEOUS WORK (STABILIZING ADDITIVE):

STONE MATRIX ASPHALTIC CONCRETE:

1.0			Description:

The work under these items shall consist of constructing Asphaltic Concrete Stone Matrix Asphalt (SMA), hereinafter asphaltic concrete, by furnishing all materials, mixing at a plant, hauling and placing a mixture of aggregate materials, mineral admixture, and bituminous material (asphalt cement) to form a pavement course or to be used for other specified purposes, in accordance with the details shown on the project plans and the requirements of the special provisions.

All stone matrix asphaltic concrete shall be placed as a surface course. Surface courses are defined as courses placed to serve either as the traffic course or as a surface upon which a finishing course is to be placed. Recycled Asphalt Pavement (RAP) shall not be allowed in Stone Matrix Asphalt (SMA).

The contractor shall acquire and make all arrangements for a source or sources of material, furnish a mix design which will meet the design criteria specified hereinafter, and provide all the equipment, materials, and labor necessary to complete the work.

(Use only the mix type called for In the Materials Design Report. And delete the other)

The type of asphaltic concrete shall be 1/2-inch mix or 3/8-inch mix.

2.0			Asphaltic Concrete Mix Design Criteria:

The Department will follow the Stone Matrix Asphalt mix design procedure contained in the AASHTO R 46, and the AASHTO M 325 except as revised herein.

Mix designs shall be developed by the contractor.  Each mix design shall meet the criteria in Table 1 and the grading requirements in Table 2 when tested in accordance with Arizona Test Method 815, with the noted exceptions.

| TABLE 1 ASPHALTIC CONCRETE MIX DESIGN CRITERIA |  |  |
| --- | --- | --- |
| Criteria | Requirements |  |
| Voids in Mineral Aggregate: % | 17.0 Minimum |  |
| Effective Voids: % | 4.0 +/-0.1 |  |
| Absorbed Asphalt: %, Range | 0 - 1.0 |  |
| Asphalt Binder Content: % | 6.0% Minimum (Lower Limit) |  |
| Draindown at Production Temperature,% | 0.3 Maximum |  |
| VCAMIX ,% | Less than VCADRC |  |
| TSR | 0.8 Minimum |  |
| Dust to Binder Ratio | 0.8 to 1.5 |  |
| Where: VCAMIX = Voids in Coarse Aggregate VCADRC= Dry-Rodded Voids in Coarse Aggregate TSR = Tensile strength ratio per T283 Notes: - Mix design laboratory compacted test specimens shall be prepared using a gyratory compactor in accordance with AASHTO T 312, except the mix design shall be determined at the Ndesign gyrations of 75 using the Superpave gyratory compactor. Ninitial and Nmax are not required for SMA design. - Refer to AASHTO R 46 for instructions on calculating VCAMIX and VCADRC. The dry- rodded VCA of the coarse aggregate is determined per AASHTO T 19. - The tensile strength ratio (TSR) of the SMA shall be at least 0.80, at 6.0 ± 1.0 percent air voids, when tested in accordance with AASHTO T 283. - Draindown sensitivity shall be determined on the SMA mixture in accordance with AASHTO T 305 at the anticipated plant-production temperature and shall not exceed 0.3 percent. |  |  |

| TABLE 2 MIX DESIGN GRADING LIMITS |  |  |
| --- | --- | --- |
| Sieve Size | 1/2 inch | 3/8 inch |
| 3/4 inch | 100 | 100 |
| 1/2 inch | 85 - 100 | 100 |
| 3/8 inch | 45 - 78 | 90 - 100 |
| No. 4 | 20 - 28 | 26 - 50 |
| No. 8 | 16 - 24 | 20 - 28 |
| No. 30 | 12 - 18 | 12 - 18 |
| No. 50 | 11 - 14 | 12 - 15 |
| No. 200 | 7 - 9 | 8 - 10 |

3.0			Materials:

For comparative/estimating purposes, quantities shown in the bidding schedule have been calculated based on the following data:

(In the following table, use only the columns called for In the Materials Design Report.)

|  | 1/2” MIX | 3/8” MIX |
| --- | --- | --- |
| Unit Weight, (lb./cu. ft.) | 144 | 144 |
| Asphalt Cement, % | 6.5 | 6.5 |
| Stabilizing Additive, % | 0.3 | 0.3 |

3.01			Mineral Aggregate:

(A)		General:

The contractor shall provide a source in accordance with the requirements of Section 1001 of the specifications.

Coarse mineral aggregate shall be 100% crushed gravel, crushed rock, or other approved inert material with similar characteristics, or a combination thereof, conforming to the requirements of this special provision.

Fine mineral aggregate shall be 100% crushed gravel or crushed rock.  All uncrushed material passing the No. 4 sieve shall be removed prior to the crushing, screening, and washing operations necessary to produce the specified gradation. The liquid limit for fine aggregate shall not exceed 25 and the fine aggregate shall conform to all the requirements of this special provision.

The contractor shall notify the Engineer a minimum of 48 hours in advance of crushing the material to be used as virgin mineral aggregate, so all crushing operations can be inspected.  Existing stockpile material which has not been inspected during crushing will not be permitted for use unless the contractor is able to document to the Engineer’s satisfaction that the virgin mineral aggregate has been crushed.  Any material inspected by the Department as crushed material shall be separated from the contractor’s other stockpiles and reserved for use throughout the project duration.

Should the contractor modify the method of producing either the uncrushed or crushed fine aggregate, the Engineer shall be immediately notified and the materials sampled and tested for determination of uncompacted void content.

The mineral admixture shall be added and thoroughly mixed with the mineral aggregate by means of a mechanical mixing device prior to the mineral aggregate and mineral admixture entering the dryer. The moisture content of the combined mineral aggregate shall be a minimum of 3 percent by weight of the aggregate during the mixing process

(B)		Mineral Aggregate Characteristics:

Aggregates shall be free of deleterious materials, clay balls, and adhering films or other material that prevent the thorough coating with the asphalt cement.

Mineral aggregate shall conform to the following requirements when tested in accordance with the applicable test methods:

| MINERAL AGGREGATE CHARACTERISTICS | TEST METHOD | REQUIREMENT |  |
| --- | --- | --- | --- |
| Combined Bulk Oven Dry Specific Gravity | Arizona Test Method 251 | 2.350 - 2.850 |  |
| Combined Water Absorption | Arizona Test Method 251 | 0 - 2% |  |
| Sand Equivalent | AASHTO T 176 (After thoroughly sieving the sample, no additional cleaning of the fines from the plus No. 4 material is required.) | Minimum 50 |  |
| Abrasion | AASHTO T 96 | 100 Rev., Maximum 9% 500 Rev., Maximum 30% |  |
| Fractured Coarse Aggregate Particles | AASHTO T 335 | Minimum 95% with at least two fractured faces and 100% with at one fractured face (plus No. 4 material) |  |
| Flat and Elongated Particles | ASTM D4791 (except test shall be performed on plus No. 4 material) | Maximum 10% (of the plus No. 4 material) 5:1 |  |
| Uncompacted Void Content | AASHTO T 304 Method A | Minimum 45.0% |  |
| Flakiness Index | Arizona Test Method 233 | Maximum 20% |  |
| Carbonates | Arizona Test Method 238 | Maximum 20% |  |
| Soundness (Sodium Sulfate) | AASHTO T 104 | Maximum 10% loss with five cycles |  |
| Plasticity Index | AASHTO T 90 | Non-Plastic |  |
| Notes: - Abrasion shall be performed separately on materials from each source of mineral aggregate. All sources shall meet the requirements for abrasion. - Testing for carbonates only applies if either of the following conditions exist: - The asphaltic concrete is the designed final pavement surface normally used by traffic. - The asphaltic concrete, temporary or otherwise, will be subject to traffic for more than 60 days. |  |  |  |

Tests on aggregates outlined above, except for abrasion, shall be performed on materials furnished for mix design purposes and composited to the mix design gradation.

3.02			Mineral Admixture:

Mineral admixture will be required. The amount used shall be minimum 1.0 percent, by weight of the mineral aggregate, unless testing demonstrates that additional admixture is required in order to meet the mix design criteria. A maximum of 2.0 percent admixture will be permitted.  The exact amount of admixture required shall be specified in the mix design. Mineral admixture shall be either Portland cement, blended hydraulic cement, or hydrated lime conforming to the following requirements:

| MATERIAL | REQUIREMENT |
| --- | --- |
| Portland Cement, Type I or II | ASTM C150 |
| Blended Hydraulic Cement, Type IP | ASTM C595 |
| Hydrated Lime | ASTM C1097 |

The certification and acceptance of Portland cement, blended hydraulic cement, and hydrated lime shall be in accordance with ADOT Materials Practice and Procedure Directive No. 13, "Certification and Acceptance of Hydraulic Cement, Fly Ash, Natural Pozzolan, Silica Fume, and Lime".

3.03			Bituminous Material:

Asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005 of the specifications.  The type of asphalt binder shall be PG XX-XX PM.

The contractor shall follow the recommendations of the supplier for laboratory mixing and compaction temperatures for mix design purposes.

3.04	 	    Mineral Filler:

Mineral filler shall consist of finely divided mineral matter such as crusher fines, rock dust, Class F fly ash, or Class N natural pozzolan meeting the requirements of ASTM C618. At the time of use, it should be sufficiently dry to flow freely and essentially free from agglomerations. Filler shall be free from organic impurities and have a plasticity index not greater than four. The mineral filler shall be added at the same point the asphalt cement is added to the aggregate.

Mineral filler shall meet the following grading requirements:

| SIEVE SIZE | PERCENT PASSING |
| --- | --- |
| No. 30 | 100 |
| No. 50 | 95 - 100 |
| No. 200 | 55 - 100 |

3.05		   Stabilizing Additive:

Stabilizing additives shall be made from virgin basalt, diabase, slag, or cellulose treated with a cationic sizing agent to enhance disbursement of the fiber as well as increase adhesion of the fiber surface with the asphalt binder and control draindown. The stabilizing additive shall conform to the requirements of AASHTO M 325.

A certificate of analysis meeting the requirements of Subsection 106.05 of the specifications with the manufacturer’s most recent test data conforming to the requirements shown in the table below shall be submitted along with mix design submittal. Certificate of Compliance conforming to the requirements of Subsection 106.05 of the specifications shall be submitted for each shipment of stabilizing additive.

| Mineral Fiber |  |
| --- | --- |
| Property Description: | Requirement |
| Dosage Rate: | 0.3 – 0.6% by weight of total mix |
| Average Fiber Length (Max.): | 0.25 inch |
| Average Fiber Thickness (Max.): | 0.0002 inch |
| Shot Content (ASTM C612) |  |
| Passing No. 60 Sieve: | 90 - 100% |
| Passing No. 230 Sieve: | 65 - 100% |
| Cellulose Fiber |  |
| Property Description: | Requirement |
| Dosage Rate: | 0.2 – 0.4% by weight of total mix |
| Using Alpine Sieve Analysis, Fiber Length (Max.): | 0.25 inch |
| Passing No. 100 Sieve: | 60 - 80% |
| Using a Mesh Screen Analysis |  |
| Ash Content: | 13 - 23% |
| Oil Absorption: | 4.0 - 6.0% |
| Moisture Content (Max.): | 5% |

3.06		        Warm Mix Asphalt Technologies:

Warm Mix Asphalt (WMA) technologies include plant water foaming processes, mineral additives, and chemical additives.  WMA technologies shall be approved prior to their use in accordance with Materials Practice and Procedure Directive No. 23, “Requirements for the Use of Warm Mix Asphalt (WMA) Technologies in Asphaltic Concrete”. Only ADOT approved Warm Mix Asphalt (WMA) technologies will be allowed. Refer to ADOT Approved Warm Mix Asphalt (WMA) Technologies List.

4.0			 Mix Design:

Utilizing mineral aggregate which has been crushed, processed, separated, and stockpiled, a mix design shall be formulated and submitted by the contractor to the Engineer. The mineral aggregate samples used for mix design purposes shall be representative of materials to be used during production.

The mix design shall be based on the mix design criteria and other requirements hereinbefore specified, utilizing asphalt cement, mineral admixture, mineral filler and stabilizing additive of the type and from the sources proposed for use in the production of asphaltic concrete.

The mix design shall be prepared by or under the direct supervision of a professional engineer experienced in the development of mix designs and mix design testing. The mix design engineer shall meet the requirements given in ADOT Materials Practice and Procedure Directive No. 4, “Asphaltic Concrete Mix Design Proposals and Submittals”.  The mix design shall be provided in a format that clearly indicates all the mix design requirements and shall be sealed, signed, and dated by the mix design engineer.

The mix design shall be prepared by a mix design laboratory that has met the requirements of ADOT Materials Practice and Procedure Directive No. 19, “ADOT System for the Evaluation of Testing Laboratories”.

The mix design shall contain as a minimum:

- The name and address of the testing organization and the person responsible for the   mix design testing.

- The specific location(s) of the source(s) of mineral aggregate.

- The supplier, refinery, type of asphalt cement and any modifiers including polymers.  The source and type of mineral admixture.  The percentage of asphalt

cement and mineral admixture to be used.

- The anticipated mineral aggregate gradation in each stockpile.

- Mix design gradation and mix test results from all trial gradations.  The mix design shall contain the mineral aggregate gradation, and also the gradation with mineral admixture.

- The results of all testing, determinations, etc., such as: specific gravity of each component, water absorption, sand equivalent, loss on abrasion, fractured coarse aggregate particles, flat and elongated particles, uncompacted void content, percent carbonates (if required), immersion compression results (Index of Retained Strength, wet and dry strengths), asphalt absorption, percent air voids, voids in mineral aggregate, and bulk density.

- Viscosity-temperature curve along with the laboratory mixing and compaction temperature ranges, as well as the actual laboratory mixing and compaction temperatures used. For modified binders follow the recommendations of the supplier.

When Warm Mix Asphalt (WMA) technologies are used in the mixture, the additional mix design requirements specified in Materials Practice and Procedure Directive No. 23, “Requirements for the Use of Warm Mix Asphalt (WMA) Technologies in Asphaltic Concrete”, shall also be included in the mix design.

Test results used in the formulation of the mix design shall be from testing performed no earlier than 45 days prior to the date the mix design is signed by the mix design engineer.  Historical abrasion values may be supplied on sources provided the testing was conducted within the past two years.

The mix design shall be submitted to the Engineer under a cover letter signed by an authorized representative of the contractor.

A copy of the mix design and representative samples of the materials used in the mix design shall be submitted to the Engineer for calibration of the ignition furnace, and for the determination of the sand equivalent, Abrasion, Fractured Coarse Aggregate Particles, Flat and Elongated Particles, Flakiness Index, Uncompacted Void Content and VCADRC.  Approximately 400 pounds of mineral aggregate and mineral filler (proportional to the mix design gradation), stabilizing additives, 2 gallons of asphalt cement, and 1 gallon of mineral admixture shall be submitted. The Engineer shall witness the sampling of the mineral aggregate. The mix design and samples shall be submitted to the Engineer at least five working days prior to the start of asphaltic concrete production.

The mineral aggregate shall meet the requirements specified in Subsection 3.01 of this specification.

If the mineral aggregate fails to meet the requirements specified herein, asphaltic concrete production shall not commence, and the contractor shall either submit a revised mix design which is representative of the materials produced or correct the deficiencies in the aggregate stockpiles.

The Engineer will review the mix design to assure that it contains all required information. If it does not, it will be returned within two working days of receipt of all samples and mix design information for further action and resubmission by the contractor.

If the contractor elects to change its source(s) of mineral aggregate or mineral filler or stabilizing additives, or adds or deletes the use of a stockpile(s) regardless of source, the contractor shall furnish the Engineer with a new mix design which meets the requirements specified hereinbefore.

If changes are made in the source or type of bituminous material, type of mineral admixture, stabilizing additives or mineral filler the contractor shall provide verification testing results.  Verification testing shall be performed at the original mix design asphalt content using the original mineral aggregate, the proposed bituminous material, and/or the proposed mineral admixture.  Three specimens shall be fabricated and tested for VCAMIX, bulk density, maximum theoretical density, and effective voids.  The percent effective voids shall be within ± 0.2 of the percent effective voids in the original design and also be within the current effective voids mix design specification limits. Verification testing results shall not replace target values shown in the original mix design.  All target values from the original design shall be used in future production with the exception of any self-directed target value changes that are requested.  The verification process does not ensure that the contractor can meet the target values during production.

In addition to the verification testing specified above, verification testing for TSR is also required.  If there is a change in the type of mineral admixture or mineral filler, TSR testing is required.

The contractor may make self-directed target changes to the approved mix design within the limits shown below.  Requests for self-directed target changes shall be made in writing and acknowledged by the Engineer prior to start of production for a lot.  Self-directed target changes shall meet contract requirements for mix design criteria and grading limits.

| MEASURED CHARACTERISTICS | ALLOWABLE SELF-DIRECTED TARGET CHANGES |
| --- | --- |
| Gradation (Sieve Size): |  |
| 3/8 inch | ± 4% from mix design target value |
| No. 4 | ± 3% from mix design target value |
| No. 8 | ± 3% from mix design target value |
| No. 50 | ± 2% from mix design target value |
| No. 200 | ± 0.5% from mix design target value |
| Asphalt Cement Content | ± 0.5% from mix design target value |
| Effective Voids | None |

The contractor may propose target changes to the approved mix design for the Engineer’s approval. The Engineer will determine if the proposed target change will result in mix production that meets the contract requirements for mix design criteria and grading limits. For acceptance purposes, target changes will not be retroactive.

In no case shall the approval of mix design changes relieve the contractor of the responsibility for the results obtained by the use of such approved changes.

Should a mix design prove unsatisfactory to the contractor during production, the contractor shall furnish the Engineer with a revised mix design. For acceptance purposes, the revised mix design will not be retroactive.

The contractor shall not change its methods of crushing, screening, washing, or stockpiling from those used during production of material used for mix design purposes without approval of the Engineer or without preparing a new mix design.

5.0			Contractor Quality Control:

The contractor shall perform the quality control measures described in Subsection 106.04(C) of the specifications.  At the weekly meeting, the contractor shall be prepared to explain and discuss how the following processes will be employed.

- Aggregate production, including crusher methods, pit extraction, and washing.

- Stockpile management, including stacking methods, separation technique, plant feed technique, stockpile pad thickness, and segregation prevention.

- Proportioning and plant control, including plant scale calibration, mix temperature control, storing method, and addition of admixture.

- Transporting and placing, including hauling distance and temperature control, segregation and non-uniform placement control, and joint placement and technique.

- Compaction, including types and weight of rollers, establishing and monitoring of roller patterns, and temperature controls.

- Feeding of mineral filler and fibers into the mix.

The contractor shall obtain samples and perform the tests specified in the following table:

| CONTRACTOR QUALITY CONTROL TESTING REQUIREMENTS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Type of Test |  | Test Method |  | Sampling Point |  | Minimum Testing Frequency |  |
| Virgin Mineral Aggregate |  |  |  |  |  |  |  |
| Gradation |  | AASHTO T 11, T 27 |  | Crusher Belt or Stockpile |  | 1 per stockpile per day |  |
| Sand Equivalent |  | AASHTO T 176 |  |  |  | 1 per 2000 Tons of total virgin aggregate (1) |  |
| Fractured Coarse Aggregate Particles |  | AASHTO T 335 |  |  |  |  |  |
| Uncompacted Void Content |  | AASHTO T 304 Method A |  |  |  |  |  |
| Asphaltic Concrete |  |  |  |  |  |  |  |
| Gradation | AASHTO T 11, T 27 or T 308 |  | Cold Feed, Hot Bins, Roadway, or Plant |  | 1 per 1000 Tons |  |  |
| Asphalt Content | AASHTO T 287, T 308 |  | Roadway or Plant |  | 1 per 1000 Tons |  |  |
| Voids | AASHTO T 312, T 166, T 209, T 269 |  | Roadway or Plant |  | 1 per 1000 Tons each day. Maximum of 4 per day. |  |  |
| Compaction | AASHTO T 355 |  | Roadway |  | 1 per 300 tons |  |  |
| VCAMIX less than VCADRC | AASHTO T 19 |  | Cold Feed and Roadway |  | 1 per 1000 Tons |  |  |
| Notes: |  |  |  |  |  |  |  |
| (1) Prior to the completion of the mix design, quality control tests on mineral aggregate shall be performed based on the anticipated percent use of each stockpile. Samples taken from individual stockpiles may be composited prior to performing the required tests, or testing may be performed on material from each stockpile and the composite test result for each required test determined mathematically. |  |  |  |  |  |  |  |

6.0			Construction Requirements:

The contractor shall be responsible for the proportioning of all materials, for the hauling, placing, loading, spreading, and finishing of asphaltic concrete, and for the applying of bituminous material, such as tack coats, prime coats, and provisional seals, all in accordance with the appropriate portions of the specifications.

The asphaltic concrete hot plant shall conform to the requirements of Section 403 of the Specifications.

The temperature of asphaltic concrete or mineral aggregate upon discharge from the drier shall not exceed 350 degrees F unless a higher temperature is recommended in writing by the asphalt binder supplier and approved by the Engineer.

A Material Transfer Vehicle (MTV) shall be used for placing the SMA on all travel lanes and may be used at the contractor’s option in other areas. The contractor shall not place more than one truckload of hot mix in a windrow in front of the MTV at any time. The contractor shall use a MTV with storage and remixing capabilities on all mainline construction. The MTV will independently remix and deliver mixture from the hauling Equipment to the paving Equipment.

The contractor shall furnish an MTV with the following capabilities:

- An unloading system to receive mixtures from the hauling Equipment.

- A minimum storage capacity of 13 tons with a remixing system in the MTV storage bin.

- A discharge conveyor to deliver the mixture to the paver hopper.

- The MTV system cannot exceed maximum legal loading on Structures.

- Pick-up machines, hopper inserts and Material transfer devices are not considered MTVs.

In the event the MTV malfunctions during paving operations, the contractor may finish the Day without the MTV. The Contractor shall not resume further mainline mix placement until the MTV is operational.

All courses of asphaltic concrete shall be placed and finished by means of self-propelled paving machines except under certain conditions or at certain locations where the Engineer deems the use of self-propelled paving machines impractical.

Self-propelled paving machines shall spread the mixture within the specified tolerances, without segregation or tearing, true to the line, grade, and crown indicated on the project plans.  Pavers shall be equipped with hoppers and augers which shall distribute the mixture uniformly in front of adjustable screeds.

Pavers shall be equipped with a screed for the full width being paved, heated if necessary, and capable of spreading and finishing all courses of asphaltic concrete.

Pavers shall be equipped with automatic screed controls with sensors for either or both sides of the paver, capable of sensing grade from an outside reference line, sensing the transverse slope of the screed, and providing the automatic signals which operate the screed to maintain the desired grade and transverse slope.

Failure of the control system to function properly shall be cause for the suspension of the placing of asphaltic concrete.

The base or subgrade upon which asphaltic concrete is to be placed shall be prepared and maintained in a firm condition until asphaltic concrete is placed. Asphalt paving mixtures shall not be placed when surfaces are wet or when the surface temperature is 55 degrees F or lower. When the surface temperature is between 40°F and 55°F, the contractor may elect to place asphaltic concrete mixture, at no additional cost to the Department, provided an approved warm-mix additive is used as a compaction aid. Placement of asphaltic concrete shall not be allowed when the surface temperature is below 40°F.

The contractor shall utilize an approved warm-mix additive, regardless of surface temperature, when the haul distance exceeds 50 miles.

At any time, the Engineer may require that the work cease or that the work day be reduced in the event that weather conditions, either existing or expected, are anticipated to have an adverse effect upon the asphaltic concrete.

All wheels and tires of compactors shall be wetted with water, or if necessary soapy water, or a release agent in order to prevent the sticking of asphaltic concrete. All other equipment surfaces shall be treated when necessary with a release agent. Only release agents evaluated through AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) are acceptable for use. The results from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) testing, when tested in accordance with AASHTO TP 102, shall conform to the requirements shown in the table below:

| RELEASE AGENT TEST | REQUIREMENT |  |
| --- | --- | --- |
| Asphalt Stripping Test Diluted Non-Diluted (Full Strength) | No stripping No stripping |  |
| Asphalt Performance Test | Less than or equal to 10.0% after the third cycle |  |

Release agents which degrade, dissolve, or in any way damage the bituminous material shall not be used.  Diesel fuel shall not be used as a release agent.

Longitudinal joints of each course shall be staggered a minimum of 1 foot with relation to the longitudinal joint of any immediate underlying course.

When surfacing courses are placed on 10 foot or wider shoulders which are to receive rumble strips, the contractor shall place any longitudinal joints approximately 1 foot away from the travel lane side of the rumble strip.

Longitudinal joints shall be located within 1 foot of the center of a lane or within 1 foot of the centerline between two adjacent lanes.  Joints shall be formed by a slope shoe or hot-lapped, and shall result in an even, uniform surface.

Before a surface course is placed in contact with a cold transverse construction joint, the cold existing asphaltic concrete shall be trimmed to a vertical face by cutting the existing asphaltic concrete back for its full depth of the lift and exposing a fresh face.  After placement and finishing of the new asphaltic concrete, both sides of the joint shall be dense and the joint shall be well sealed.  The surface in the area of the joint shall conform to the requirements hereinafter specified for surface tolerances when tested with the straightedge placed across the joint.

All holes where cores are taken shall be repaired within 48 hours after coring using a material approved by the Engineer.  All holes shall be in a dry condition prior to repair. The patching material shall be thoroughly compacted in the holes by the contractor.

The handling of asphaltic concrete shall at all times be such as to minimize segregation.  Any asphaltic concrete which displays segregation shall be removed and replaced.

Before asphaltic concrete is placed, the surface to be paved shall be cleaned of all objectionable material and tacked in accordance with the requirements of Section 404.  The cleaning of the surface, the tacking of the surface, and the type of bituminous material used shall be acceptable to the Engineer.  The amount of bituminous material used shall be as directed by the Engineer.

A light coat of bituminous material shall be applied to edges or vertical surfaces against which asphaltic concrete is to be placed.

The contractor shall schedule its paving operations to minimize exposed longitudinal edges.  Unless otherwise approved by the Engineer, the contractor shall limit the placement of asphaltic concrete courses, in advance of adjacent courses, to one shift of asphaltic concrete production.  The contractor shall schedule its paving operations in such a manner to eliminate exposed longitudinal edges over weekends or holidays.

The moisture content of the asphaltic concrete immediately behind the paver shall not exceed 0.5 percent.  The moisture content will be determined in accordance with AASHTO T 329.

When Warm Mix Asphalt (WMA) technologies are used, the contractor shall comply with the manufacturer’s recommendations for incorporating additives and WMA technologies into the mixture.  The contractor shall comply with the manufacturer’s recommendations regarding transporting, storage, and delivery of additives and water foaming processes.  The contractor shall maintain a copy of the manufacturer’s recommendations on file at the asphalt mixing plant and make those recommendations available for reference while using WMA technologies.

7.0			Acceptance:

7.01		         General:

In addition to the random acceptance samples taken from each lot, the Engineer may sample and reject material which appears to be defective.  Such rejected material shall not be used in the work.  The results of tests run on rejected material will not be included with the lot acceptance tests.

Acceptance will be on the basis of the following:

- Sand Equivalent;

- Fractured Coarse Aggregate Particles;

- Flakiness Index;

- Flat and Elongated Particles;

- Uncompacted Void Content;

- Material Spread;

- Plastic Index (PI) for Mineral Filler;

- Smoothness;

- VCAMIX;

- Gradation;

- Asphalt Cement Content;

- Effective Voids; and

- Compaction

7.02			Sand Equivalent, Fractured Coarse Aggregate Particles, Flakiness        			Index, Flat and Elongated Particles, and Uncompacted Void Content  			of Mineral Aggregate:

During asphaltic concrete production, the Engineer will obtain and test samples of material for the determination of the sand equivalent, fractured coarse aggregate particles, flat and elongated particles, flakiness index and uncompacted void content of mineral aggregate. Samples shall be obtained from the cold feed belt prior to the addition of mineral admixture, or from the stockpiles when sampling from the cold feed belt is not possible.

Mineral aggregate will be accepted if it meets the minimum requirements specified in Subsection 3.01 of this specification.

The plastic index (PI) for the mineral filler shall be determined in accordance with the requirements of AASHTO T 89 & T 90.

If the mineral aggregate fails to meet these requirements, operations shall cease and the contractor shall have the option of submitting a revised mix design conforming to the requirements of Subsection 4.0 of this specification or correcting deficiencies in the aggregate stockpiles.

7.03			Material Spread:

A spread lot shall be considered to be one-half shift of production.  Lots encompassing more than one project shall be separated in accordance with Subsection 9(D) of this specification.

The contractor shall record information pertaining to each spread lot on forms provided by the Engineer.  Information shall include the project number, date and period of time that each spread lot was placed, the spread lot number, beginning and ending station, the plans thickness, and tons placed in each lot.  Completed spread lot forms shall be signed by the contractor and given to the Engineer at the end of each shift.

The Engineer will calculate the quantity required in each spread lot using the mix design bulk density unless a request is made by the contractor to use a production bulk density.  If a request is made to use production bulk density, the first three non-rejected lots following the test lot will be used to determine the average production bulk density.  All lots placed prior to establishing the average production bulk density shall be calculated using the mix design bulk density.  For each new mix design used on the project, a new production bulk density may be requested by the contractor.  In addition, if conditions warrant during asphalt production, the contractor may request establishment of a new average production bulk density.  All requests to use a production bulk density shall be made in writing and approved by the Engineer prior to use.  The same procedure will be used for determining average production bulk density in all cases.  Changes to the bulk density for calculating spread quantities will not be retroactive.

The calculated quantity required in each spread lot will be compared to the actual quantity placed.  A lot will be considered to be acceptable, with a zero pay factor, if the actual quantity placed varies by no more than -2.0 to +5.0 percent from the required quantity.

If the quantity in a lot is found to vary from the required quantity by -2.1 to -12.0 percent, the appropriate pay factor will be determined in accordance with Table 3.  This pay factor will be utilized in determining the pay adjustment as outlined in Subsection 9.0 of this specification.

7.04			Gradation, Asphalt Cement Content, Effective Voids, and VCAMIX:

(A)		General:

A mixture properties lot shall be considered to be one shift's production.  In the event a shift’s production is less than 1200 tons, multiple shifts may be combined to form a lot.  When a lot consists of production from more than one shift, the following conditions apply: at least one sample shall be taken each shift, at least one sample shall be taken every 500 tons, and no mix design or target value changes shall be made within the lot.  If changes are made in the mix design or target values, new lots will be established.

Four samples of the asphaltic concrete shall be taken for each lot by the contractor, under the observation of the Engineer, at random locations designated by the Engineer.  Samples shall be collected by the contractor, under observation by the Engineer, in accordance with AASHTO R97 from windrows on the ground at the jobsite or from the back of trucks at the plant from an elevated rack. Samples shall be delivered to the Engineer immediately after being taken.  The minimum weight of the sample shall be 130 pounds.  The Engineer will split the sample and save one-half for 15 days after written notification to the contractor of test results for that lot has been made.  The material will be tested by the Engineer for the following properties:

| TEST PROPERTY | TEST METHOD |
| --- | --- |
| Asphalt Cement Content Gradation | AASHTO T 308 (See Note) |
| Gyratory Density | AASHTO T 312 |
| Maximum Theoretical Density | AASTHO T 209 |
| Effective Voids | AASHTO T 269 |
| VCAMIX | AASHTO T 19 (Refer to AASHTO R 46 for guidance) |
| Note: A new calibration of the ignition furnace shall be performed for each mix design, and at any other time the Engineer directs. |  |

Acceptance testing results will be furnished to the contractor within four working days of receipt of samples by the Engineer.

The target values for gradation, asphalt cement content, and effective voids are given in the contractor’s mix design.  The Upper Limits (UL) and Lower Limits (LL) of acceptable production of each of the measured characteristics are as follows:

| MEASURED CHARACTERISTICS FOR 1/2” AND 3/8” MIXES |  |  |
| --- | --- | --- |
| Gradation (Sieve Sizes) | LL | UL |
| 3/8 inch | TV – 5.0 | TV + 5.0 |
| No. 4 | TV – 4.0 | TV + 4.0 |
| No. 8 | TV – 3.0 | TV + 3.0 |
| No. 50 | TV – 3.0 | TV + 3.0 |
| No. 200 | TV – 2.0 | TV + 1.5 |
| Asphalt Cement Content | TV – 0.5 | TV + 0.5 |
| Effective Voids | TV –2.0 | TV + 2.0 |
| Note: The limits are used in the statistical calculations for Quality Index. Acceptance is controlled by the variability of the produced material and every effort should be made to strive for the center of the applicable Target Valve (TV). |  |  |

The Engineer will determine the PT for each measured characteristic in accordance with

Subsection 9(I) of this specification and utilizing Table 3 will determine the pay factor for each measured characteristic.

In the event the contractor elects to question the mixture property test results, the contractor may request referee testing in accordance with Subsection 9(J) of this specification.

(B)	Ignition Furnace Correction:

Ignition furnace corrections shall be made in accordance with the requirements of AASHTO T 308.

7.05			Compaction:

Compaction control shall be the responsibility of the contractor.  The number and types of rollers shall be the contractor's responsibility and shall be sufficient to meet the requirements specified herein.

Pneumatic-tired rollers will not be permitted.

Compactors shall be operated in accordance with the manufacturer’s recommendations. Compactors shall be designed and properly maintained so that they are capable of accomplishing the required compaction.

Steel wheel compactors shall weigh not less than 12 tons.

A compaction lot shall be identical to the mixture properties lot described in Subsection 7.04 of this specification.  Lots encompassing more than one project shall be separated in accordance with Subsection 9 (D) of this specification.  Each lot shall be tested for acceptance.

Twenty cores shall be taken for each lot by the contractor, under the observation of the Engineer.  The Engineer will designate 10 random locations within the lot, and the contractor shall take two cores at each location; however, if more than one shift constitutes a lot, two cores shall be taken from a minimum of two random locations each shift, or as directed by the Engineer.  The Engineer will save one core from each location for 15 days after written notification to the contractor of test results for the lot has been made. Randomly selected locations will be determined to the nearest 0.5 foot in the transverse direction and to the nearest foot in the longitudinal direction of the pavement course; however, the outside 1 foot of the unconfined pavement course will be excluded from testing as shown in ADOT Materials Practice and Procedure Directive (P.P.D.) No. 18, “Determining Sample Times and Locations for End Product Asphaltic Concrete”.  P.P.D. No. 18 also addresses areas to be excluded relative to longitudinal joints.  Cores shall be taken utilizing mechanical coring equipment in accordance with the requirements of AASHTO R 97.  Cores shall be a minimum of 4 inches in diameter and shall be taken not later than two working days after placement of the asphaltic concrete.  The cores shall be delivered to the Engineer immediately upon being taken.  The bulk density of each core will be determined by the Engineer in accordance with the requirements of AASHTO T 166.  The test results will be furnished to the contractor within four working days of receipt of cores by the Engineer.  In areas where more than one lift is placed in the same lot, coring shall be accomplished through the full depth of the lifts after the final lift is placed, and the compaction density shall be based on the full depth of the lifts.

The target value for compaction shall be 5.0 percent in-place air voids.  In-place air voids shall be determined in accordance with AASHTO T 269.  The maximum theoretical density used in the determination of air voids will be the average of the four maximum theoretical densities determined for the lot in Subsection 7.04 of this specification.

The Upper Limit (UL) is 8.0 percent in-place air voids and the Lower Limit (LL) is 2.5 percent in-place air voids.  The Engineer will determine the PT for compaction in accordance with Subsection 9(I) of this specification, and utilizing Table 3 will determine the compaction pay factor.

In the event the contractor elects to question the core test results, the contractor may request referee testing in accordance with Subsection 9(J) of this specification.

7.06			Smoothness and Surface Tolerances:

Asphaltic concrete shall be compacted as required, smooth and true to the required lines, grades, and dimensions.

The Special Provisions may require the smoothness of the final pavement surface to be tested in accordance with Subsection 109.13 of the specifications.

Regardless of whether testing in accordance with Subsection 109.13 of the specifications is specified or not, the following requirements shall be met:

- The surface of the final lift of asphaltic concrete placed under this section of the specifications shall be tested and shall not vary by more than 1/8 inch from the lower edge of a 10-foot straightedge when it is placed in the longitudinal direction (including across transverse joints), and when it is placed in the transverse direction across longitudinal joints.

- The surface of any lift of asphaltic concrete placed under this section of the specifications, other than the final lift, shall be tested and shall not vary by more than 1/4 inch from the lower edge of a 10-foot straightedge when it is placed in the longitudinal direction (including across transverse joints), and when it is placed in the transverse direction across longitudinal joints.

- All deviations exceeding the specified tolerances above shall be corrected by the contractor, to the satisfaction of the Engineer.

8.0			Method of Measurement:

(A)		Asphaltic Concrete:

Asphaltic concrete will be measured by the ton for the asphaltic concrete actually used, which will include the weight of mineral aggregate, asphalt cement, and mineral admixture.  Measurement will include any quantity used in construction of intersections, turnouts, or other miscellaneous items or surfaces.

(B)		Stabilizing additives:

Stabilizing additives (Cellulose or Mineral fibers) will be measured by the ton.

(C)		Asphalt Cement:

Asphalt cement will be measured by the ton on the basis of the asphalt cement content determined in accordance with Subsections 7.04(B) of this specification for each lot of asphaltic concrete accepted.  The average asphalt cement content will be multiplied by the number of tons of asphaltic concrete in that lot to determine the amount of asphalt cement.  If the contractor has requested referee testing, the average asphalt cement content will come from the independent testing laboratory results. At the discretion of the Engineer, asphalt cement may be measured by invoice quantities, adjusted as necessary for waste.  Waste generated from startup of the asphalt plant will be considered to have a binder content of 5.0 percent.  In no case shall the measured amount of asphalt cement for payment be greater than the total of the invoice quantities, adjusted for waste.

9.0			Basis of Payment:

The accepted quantities of asphaltic concrete, measured as provided above, will be paid for at the contract unit price adjusted by the appropriate pay factors as hereinafter provided.

When Warm Mix Asphalt (WMA) technologies are used in the mixture, no separate payment will be made for WMA additives or technologies, necessary hot plant modifications, or other associated costs.

For the purpose of determining acceptability and appropriate pay factors, each unit of asphaltic concrete will be included in three separate lots: a “spread lot,” a “mixture properties lot,” and a “compaction lot.”  The total unit price for any unit of accepted asphaltic concrete will be the contract unit price, adjusted by the applicable spread lot pay factor, mixture properties lot pay factor, and compaction lot pay factor.

The contractor may request to place the first lot of each mix type as a test strip.  Requests to place a test strip shall be made in writing and acknowledged by the Engineer prior to start of production.  A test strip shall be limited to 1,000 tons and may only be placed on shoulders, ramps, cross roads, or other areas approved by the Engineer.  A test strip shall be excluded from the mixture properties lot pay factor and the compaction lot pay factor; however, all other provisions of Subsection 9.0 specified herein shall still apply to such areas.

The Engineer may exclude asphaltic concrete from the spread lot and from the spread lot pay factor calculations if the Engineer determines that the proposed use of the material or the existing surface conditions are not conducive to the use of spread lots.

The Engineer may exclude certain locations from the mixture properties lot and/or the compaction lot and from the random sampling used in determining the mixture properties lot pay factor and/or the compaction lot pay factor should the Engineer determine that the location of the work precludes normal construction operations.

(A)		Spread Lot Pay Factor:

The spread lot pay factor will be determined in accordance with Subsection 7.03 of this specification.  If the quantity in a spread lot is found to vary by more than + 5.0 percent from the required quantity, no payment will be made for the material which exceeds + 5.0 percent, including asphalt cement and mineral admixture.  If the quantity is found to vary by more than - 12.0 percent from the required quantity, the spread lot will be rejected.

(B)		Mixture Properties Lot Pay Factor:

The mixture properties lot pay factor shall be determined in accordance with the following procedure:

- The individual PT values and pay factors for Gradation, Asphalt Cement Content, and Effective Voids shall be determined as set forth in Subsection 7.04 of this specification.

- A single pay factor shall be determined for Gradation and Asphalt Cement Content.  That pay factor shall be the lowest pay factor for the individual measured characteristics for Gradation and Asphalt Cement Content.

- If no individual PT value in (1) above is less than 50, the mixture properties lot pay factor shall be the sum of the pay factor determined in (2) above and the Effective Voids pay factor.  The negative pay factor for mixture properties shall not exceed $3.00 per ton.  If any individual PT value is less than 50, the lot is in reject and the provisions in Subsection 9(E) of this specification shall apply.

(C)		Compaction Lot Pay Factor:

The compaction lot pay factor shall be determined as set forth in Subsection 7.05 of this specification.

(D)			Determination of Lot Pay Factors on Contracts Involving Multiple Projects:

When more than one project is included in a single contract, placement during a shift or half shift of production may encompass more than one project.  In such case, the applicable spread lot pay factor, mixture properties lot pay factor, and compaction lot pay factor for each project shall be determined as follows:

Spread lot pay factors will be determined separately for each project utilizing the procedure set forth in Subsection 7.03 of this specification.

- The individual PT values and pay factors for Gradation, Asphalt Cement Content, and Effective Voids will be determined from the results of the random samples taken and tested in accordance with Subsection 7.04 of this specification, regardless of which project(s) the samples fall within.

- PT values and pay factors for compaction, for those areas subject to Subsection 7.05(B) of this specification, shall be determined from separate sets of core samples for each project utilizing the procedure set forth in that Subsection.

- The mixture properties lot pay factor shall be determined separately for each project in accordance with Subsection 9(B) specified herein, utilizing the individual pay factors determined in (B) above.

- The compaction lot pay factor shall be determined separately for each project in accordance with Subsection 9(C) specified herein, utilizing the pay factor determined in (C) above.

(E)		Acceptability:

Asphaltic concrete included in any mixture properties lot possessing an individual PT value lower than 50 for Gradation, Asphalt Cement Content, or Effective Voids will be rejected.  Asphaltic concrete included in any compaction lot possessing a PT value lower than 50 will be rejected.

The contractor may request that a sample with a failing test result(s) on gradation and/or asphalt cement content be allowed to remain in place without the completion of an engineering analysis if the application of a self-directed target value change as outlined in section 4.0 of this specification would have brought the failing test result(s) to within the specified tolerances. This proposal shall be made to the Engineer in writing with justification. Once accepted, the material will be allowed to remain in place at the maximum negative pay factor(s). Maximum negative are defined as a minus $3.00 per ton for mixture properties lots in reject for gradation only, minus $5.00 per ton for mixture properties lots in reject for asphalt cement content and/or effective voids only, and minus $5.00 per ton for mixture properties lots in reject for asphalt cement content and/or effective voids and also gradation.

Within 25 days after receiving notice that a spread lot, mixture properties lot, or compaction lot of asphaltic concrete has been rejected by the Engineer, the contractor may submit a written proposal to accept the material in place at the applicable maximum negative pay factor(s).  Maximum negative pay factors are defined as a minus $1.00 per ton for spread lots, minus $5.00 per ton for compaction lots, minus $3.00 per ton for mixture properties lots in reject for gradation only, minus $5.00 per ton for mixture properties lots in reject for asphalt cement content and/or effective voids only, and minus $5.00 per ton for mixture properties lots in reject for asphalt cement content and/or effective voids and also gradation.  Positive mixture properties lot pay factors become zero when the compaction lot is in reject and the material is allowed to be left in place.

The proposal shall contain an engineering analysis of the anticipated performance of the asphaltic concrete if left in place.  The engineering analysis shall also detail any proposed corrective action, and the anticipated effect of such corrective action on the performance.  The engineering analysis shall be performed by an independent professional engineer experienced in asphaltic concrete testing and the development of asphaltic concrete mix designs.  If a rejected mixture properties lot or a rejected compaction lot is submitted for referee testing by the contractor, the 25 days allowed to prepare an engineering analysis will begin upon notification of referee test results.

Within three working days, the Engineer will determine whether or not to accept the contractor’s proposal.  If the proposal is not accepted, the asphaltic concrete shall be removed at no additional cost to the Department and replaced with asphaltic concrete meeting the requirements of these specifications.  If the proposal is accepted, the asphaltic concrete shall remain in place at the applicable maximum negative pay factor(s), and any necessary corrective action shall be performed at no additional cost to the Department.

The Department reserves the right to suspend the work should any of the following conditions occur:

- The occurrence of two or more rejected lots within any 10 consecutive production lots.

- The occurrence of three consecutive negative mixture properties lot pay factors or three consecutive negative compaction lot pay factors.

- The occurrence of five or more pay factors that are negative either for a mixture properties lot or for a compaction lot within any 10 consecutive production lots.

If the Department elects to suspend the work for any of these conditions, the contractor shall either submit a revised mix design in accordance with Subsection 4, or submit for the Engineer’s approval a written engineering analysis.  The engineering analysis shall detail the course of action necessary to correct deficiencies in the contractor’s present production methods such that further production can be accomplished without excessive amounts of asphaltic concrete in penalty or rejection.  If approved by the Engineer, the revised mix design or the course of action proposed in the engineering analysis, shall be implemented and the work may continue.  Costs or delays due to the provisions of this subsection are not compensable.

(F)			Asphalt Cement:

The accepted quantity of the asphalt binder, measured as provided above, will be paid for under the respective contract item for asphalt binder shown on the bidding schedule at the contract unit price per ton, which price shall be full compensation for the work, complete in place, as specified herein.  Adjustments in payment will be made in accordance with the requirements of Subsection 1005-3.01 of the specifications.

(G)			Mineral Admixture:

No separate measurement or payment will be made for mineral admixture, the cost being considered as included in the cost of the asphaltic concrete.

(H)			Smoothness:

When required in the Special Provisions, payment for smoothness will be made in accordance with the requirements of Subsection 109.13 of the specifications.

(I)			Statistical Acceptance:

The “Total Percentage of Lot within UL and LL (PT)” will be determined in accordance with Subsection 109.11 of the specifications.

Pay Factors (PF) will be determined by entering Table 3 with PT.

| TABLE 3 PAY FACTORS |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Material Spread |  | Mixture Properties and Compaction |  |  |  |
| Negative Variance % | Pay Factor (Dollars per Ton) | PT | Pay Factors (Dollars per Ton) |  |  |
|  |  |  | Gradation and Asphalt Cement Content | Effective Voids | Compaction |
| 2.1 - 3.0 | - 0.10 | 100 | 0.00 | + 2.00 | + 2.00 |
| 3.1 - 4.0 | - 0.20 | 95 - 99 | 0.00 | + 0.50 | + 0.50 |
| 4.1 - 5.0 | - 0.30 | 90 - 94 | 0.00 | 0.00 | 0.00 |
| 5.1 - 6.0 | - 0.40 | 85 - 89 | 0.00 | - 0.25 | - 0.25 |
| 6.1 - 7.0 | - 0.50 | 80 - 84 | - 0.25 | - 0.50 | - 0.50 |
| 7.1 - 8.0 | - 0.60 | 75 - 79 | - 0.50 | - 0.75 | - 0.75 |
| 8.1 - 9.0 | - 0.70 | 70 - 74 | - 0.75 | - 1.00 | - 1.00 |
| 9.1 - 10.0 | - 0.80 | 65 - 69 | - 1.00 | - 1.25 | - 1.25 |
| 10.1 - 11.0 | - 0.90 | 60 - 64 | - 1.50 | - 1.50 | - 1.75 |
| 11.1 - 12.0 | - 1.00 | 55 - 59 | - 2.00 | - 2.00 | - 2.25 |
| More than 12.0 | Reject | 50 - 54 | - 2.50 | - 2.50 | - 3.00 |
|  |  | Less than 50 | Reject-See Subsection 9 (E) |  |  |
| See Subsections 9 (A) and (E) |  |  |  |  |  |

(J)			Referee Testing:

(1)		Referee Testing Performed for Mixture Properties Only:

Within 15 days after written notification to the contractor of test results for a particular mixture properties lot, the contractor may make a written request for referee testing.  The referee testing shall be performed by an independent approved laboratory designated by the Department.  The testing of the samples will be performed by the independent testing laboratory without knowledge of the specific project conditions such as the identity of the contractor or mix design laboratory, the test results by the Department, or the mix design targets for gradation and effective voids.  The asphaltic concrete samples previously saved will be tested for the following properties:

| Test Property | Test Method |  |
| --- | --- | --- |
| Asphalt Cement Content (See Note 1 Below) | AASHTO T 308 |  |
| Gradation |  |  |
| Gyratory Density | AASHTO T 312 (See Note 2 Below) |  |
| Maximum Theoretical Density | AASHTO T 209 |  |
| Effective Voids | AASHTO T 269 |  |
| Notes: (1) Correction to the asphalt cement content by ignition furnace testing is made in accordance with Subsection 7.04(B) of this specification. (2) Except compaction shall be performed to the number of gyrations specified in Table 1. |  |  |

The results of the referee testing will be binding on both the contractor and the Department.

Using the referee testing results, the Engineer will determine new PT’s for all characteristics.

When referee testing is performed on a mixture properties lot, the referee test result for the average maximum theoretical density will be used to determine a new PT for compaction.

The Department will pay for the referee testing; however, if the combined pay factor of the lot (Mixture Properties plus Compaction) does not improve or is reduced, or if either the mixture properties lot or compaction lot remains in reject or is placed in reject, payment to the contractor for asphaltic concrete shall be reduced by the amount of the cost of the referee testing for the mixture properties of that particular lot.

(2)		Referee Testing Performed for Compaction Only:

Within 15 days after written notification to the contractor of test results for a particular compaction lot, the contractor may make a written request for referee testing.  The bulk density of each of the cores previously saved will be determined in accordance with the requirements of AASHTO T 166 by an independent testing laboratory designated by the Department.  The testing of the cores will be performed by the independent testing laboratory without knowledge of the specific project conditions, such as the identity of the contractor or mix design laboratory, or the test results by the Department.  The percent air voids will be determined in accordance with AASHTO T 269.  The maximum theoretical density used in the determination of air voids will be the average of the four maximum theoretical densities determined for the lot in Subsection 7.04 of this specification.

The results of the referee testing will be binding on both the contractor and the Department.

When referee testing is performed on a compaction lot, the Engineer will determine a new PT for compaction using the referee testing results.

The Department will pay for the referee testing; however, if the pay factor of the compaction lot does not improve or is reduced, or the compaction lot remains in reject or is placed in reject, payment to the contractor for asphaltic concrete will be reduced by the amount of the cost of referee testing for the compaction of that particular lot.

(3)		Referee Testing Performed for Both Mixture Properties and Compaction:

When referee testing is performed, as described above, for both the mixture properties lot and the compaction lot, the Engineer will use the referee test results to determine new PT’s as specified herein in Subsections 9(J)(1) and 9(J)(2).

The Department will pay for the referee testing; however, if the combined pay factor of the lot (Mixture Properties plus Compaction) does not improve or is reduced, or if either the mixture properties lot or compaction lot remains in reject or is placed in reject, payment to the contractor for asphaltic concrete will be reduced by the amount of the cost of the referee testing for the mixture properties and compaction of that particular lot.

(K)			Stabilizing Additives:

The accepted quantity of the stabilizing additives, measured as provided above, will be paid for at the contract unit price per ton, which price shall be full compensation for the work, complete in place, as specified herein.