** USE IF SPECIFIED IN THE MATERIALS DESIGN REPORT **

# *	     USE IN CONJUNCTION WITH STORED SPECIFICATIONS:  1001MATL            *

# *											        104ENVIR            *

(401RCC, 05/15/25)

ITEM 4010021 – ROLLER-COMPACTED CONCRETE:

ROLLER-COMPACTED CONCRETE:

- Description:

The work under this item consists of furnishing all labor, equipment and materials to construct Roller-Compacted Concrete (RCC) pavement at the locations in accordance with the details shown on the project plans and the requirements specified herein.

The contractor shall proportion, mix, place, finish, and cure RCC in accordance with the requirements specified herein.

- RCC Mix Design Criteria:

The mix design shall have at least 425 pounds of cementitious material per cubic yard. Concrete test cylinders shall be fabricated in accordance with either ASTM C1435 or ASTM C1176 and cured in accordance with ASTM C192. At least one set of four cylinders shall be produced and tested for compressive strength in accordance with ASTM C39. Two cylinders shall be tested at 28 days and shall have a minimum allowable compressive strength of 4000 psi.

Changes in a mix design, other than those allowed by the Department, shall require a new mix design.

## 3.0	Materials:

## Materials shall conform to the requirements of Section 1006 of the specifications for cementitious material, hydraulic cement, water, chemical admixtures, and additives.

## 3.01	Aggregates:

A blend of fine and coarse aggregate fractions that in combination shall conform to Table 1, or unless approved by the Engineer in accordance with AASHTO T 11 and AASHTO T 27. The aggregate and sand shall be furnished in two or more stockpiles. The contractor shall provide aggregate sources in accordance with the requirements of Section 1001 of the specifications.  Coarse aggregate shall have a fractured face of 50% in accordance with AASHTO T 335, and a LA Abrasion shall not exceed 40 at 500 revolutions in accordance with AASHTO T 96. Aggregates with plasticity index exceeding 5 per AASHTO T 89 and T 90, shall not be used.

| TABLE 1 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Sieve Size | 1/2 inch |  | 3/4 inch |  | 1 inch |  |
|  | LL | UL | LL | UL | LL | UL |
| 1.5 in. |  |  |  |  | 100.0 | 100.0 |
| 1 in. |  |  | 100.0 | 100.0 | 82.0 | 100.0 |
| 3/4 in. | 100.0 | 100.0 | 95.0 | 100.0 | 72.0 | 95.0 |
| 1/2 in. | 81.0 | 100.0 | 70.0 | 95.0 | 61.0 | 81.0 |
| 3/8 in. | 71.0 | 91.0 | 60.0 | 85.0 | 50.0 | 71.0 |
| No. 4 | 49.0 | 70.0 | 40.0 | 60.0 | 36.0 | 55.0 |
| No. 8 | 33.0 | 54.0 | 30.0 | 50.0 | 25.0 | 43.0 |
| No. 16 | 24.0 | 40.0 | 20.0 | 40.0 | 15.0 | 32.0 |
| No. 30 | 15.0 | 30.0 | 15.0 | 30.0 | 10.0 | 26.0 |
| No. 50 | 10.0 | 25.0 | 10.0 | 25.0 | 5.0 | 19.0 |
| No. 100 | 2.0 | 16.0 | 2.0 | 16.0 | 2.0 | 16.0 |
| No. 200 | 0.0 | 8.0 | 0.0 | 8.0 | 0.0 | 8.0 |

## 3.02	Chemical Admixtures:

## If the contractor intends to use chemical admixtures, the contractor shall submit it as part of the proposed mix design to the Engineer for review and approval. Chemical admixtures shall be conforming to the requirements of Subsection 1006 of the specifications.

## If chemical admixtures are part of the proposed mix design, they shall also be used during production.

## 3.03	Curing Compounds:

Liquid membrane curing compound shall conform to the requirements of Subsection 1006-6.01(C) of the specifications.

## 4.0	Construction Requirements:

## 4.01	General:

## At least 15 calendar days prior to beginning of the project, the contractor shall submit a proposed mix design to the Engineer for review and approval. The mix design shall include the aggregate gradation, cementitious materials, admixtures, compressive strength, and required moisture and density to be achieved. If the proposed mix design meets the required parameters, the mix design will be given conditional approval. Final approval of the mix design will be based on the evaluation of the Test Section. Production shall not begin until an approved mix design has been obtained. A new mix design shall be submitted for approval if any variation is made from the approved mix design.

## 4.02	Quality Management Plan for RCC Pavement Installation:

## At least 30 calendar day prior to paving, the contractor shall provide a Quality Management (QM) plan for RCC pavement installation to the Engineer for review and approval. Construction of RCC shall not begin until the QM plan is accepted as being complete and has been distributed for inspection of the construction work. As a minimum, the contractor shall include the following information in the QM plan:

- Organizational chart that identifies the key individuals assigned to production and placement operations. As applicable, include a project manager, RCC consultant, project superintendent, RCC production supervisor, and quality control manager, and/or other positions as appropriate gives the application, include all appropriate contact data and the chain of command for decision making.

- List of subcontractors, including proposed job site personnel, for RCC construction operations.

- Construction schedule for all RCC work

- Proposal for:

- Direction of paving operation.

- Paving width and staging plan.

- Daily production targets, including trucking, placement, and production rates.

- Planned longitudinal and transversal cold joints.

- Curing methods and pattern.

- Outline of procedures and methods for cold weather protection (less than 40 degrees F).

- Outline of procedures and methods for hot weather protection (more than 40 degrees F).

- List of equipment proposed to use including:

- Manufacturer’s name.

- Technical specification sheet for:

- Mixing plant.

- Hauling equipment.

- Placing equipment.

- Spreading and compaction equipment.

- Layout and operation of mixing plant:

- Proposed mixing cycle.

- Location of each cementitious material bin.

- Location of each aggregate storage.

- Chemical admixture storage.

- Water supply on or off site.

- Mixing equipment (pugmill).

## 4.03	Equipment:

- Effectiveness of RCC Production Equipment:

## RCC shall be constructed with any combination of equipment to produce a completed pavement meeting the requirements for mixing, transporting, placing, compacting, finishing, and curing in accordance with the requirements specified herein.

- Equipment for Preparing and Curing Test Specimens:

## Cylinder production shall be in accordance with ASTM C1435, ASTM C1176, curing in accordance with ASTM C31, and tested in accordance with ASTM C39.

## All of the equipment furnished by the contractor for preparing and curing test cylinders shall be approved by the Engineer prior to the commencement of RCC placement.

- Mixing Plant:

## The mixing plant shall be located within a 30-minute haul time from the point of RCC placement. The plant shall be capable of producing a RCC pavement mixture in the proportions defined by the final approved mix design.

| ## MATERIAL | ## TOLERANCE |
| --- | --- |
| ## Cementitious Materials | ## ± 2.0% |
| ## Water | ## ± 3.0% |
| ## Aggregates | ## ± 4.0% |
| ## Chemical Admixtures | ## ± 3.0% |

## The capacity of the plant shall be sufficient, but not less than 100 cubic yard per hour, to produce a uniform mixture at a rate compatible with the placement equipment. If the plant is unable to produce material at a rate adequate to prevent unnecessary cold joints and frequent paver stoppages, the Engineer may stop production until such time that a plant of appropriate capacity is used.

## The mixing plant shall be a central plant with a twin-shaft pugmill mixer, capable of batch or continuous mixing. The mixer shall be equipped with synchronized metering devices and feeders to maintain the correct proportions of aggregate, cement, mineral and chemical admixtures, and water. Other mixing plant requirements are as follows:

- Aggregate Storage:

Aggregate storage shall be provided by separate stockpiles of each size group delivered. Aggregate bins shall have a feed rate controlled by a variable speed belt or an operable gate calibrated to accurately deliver any specified quantity of material. The feed rate from each bin shall be readily adjustable to change aggregate proportions when required. Feed rate controls shall maintain the established proportions of aggregate from each stockpile bin when the combined aggregate delivery is increased or decreased.

- Cementitious Material Feed Unit:

## Satisfactory means of dispensing cementitious materials, volumetrically or by weight, shall be provided to ensure that a uniform and accurate quantity of cementitious material enters the mixer.

- Water and Chemical Admixture Control Unit:

## Required amounts of water and chemical admixtures shall be measured by weight or volume. The mixer shall be equipped with an accurate metering device that will accurately measure the amount of water needed in the RCC mix. The rate of water added shall be adjustable to keep the RCC mixture at the targeted moisture content. The mixer shall also be equipped with an approved admixture dispensing system capable to consistently dispense the approved dosage rate to the RCC mix.

- Gob Hopper:

## For continuous operation pugmills, a gob hopper shall be provided and shall be attached to the end of the final discharger belt to temporarily hold the RCC discharge to allow the plant to operate continuously.

- Paver:

## RCC shall be placed with a high-density paver approved by the Engineer. The paver shall be capable of producing an RCC pavement with a minimum of 90 percent of the maximum density in accordance with AASHTO T 180, Method D. The paver shall be of suitable weight and stability to spread and finish the RCC material, without segregation, to the required thickness, smoothness, surface texture, cross-section, and grade.

## The contractor shall submit the type, model, and specifications of the paver to the Engineer for approval. The contractor shall deliver this submittal to the Engineer at least 14 calendar days prior to the use of the paver.

- Compactors:

## Self-propelled dual steel drum vibratory rollers shall be used for the primary compaction. For final compaction a steel drum roller operated in a static mode shall be utilized. Walk-behind vibratory rollers or plate tampers shall only be used for compacting areas inaccessible to large rollers.

- Haul Trucks:

Trucks for hauling the RCC material from the plant to the paver shall have covers available to protect the material from rain and to reduce excessive evaporation losses. The number of trucks used shall be sufficient to ensure an adequate and continuous supply of RCC material to the paver.

Trucks used shall have clean and smooth beds without buildup of partially hardened material in the corners or edges.

## 4.04	Preparation of Subgrade:

The subgrade shall be prepared in accordance with the details shown on the plans and specifications, and to the satisfaction of the Engineer before the placement of the RCC pavement begins.

## 4.05	Test Section:

- General:

## Prior to commencement of RCC production, the contractor shall construct a pavement test section using the conditionally approved mix design. The equipment, materials, and techniques used to construct the test section shall be those which will be used to construct the RCC pavement. The test section is to evaluate the mixing plant capabilities, equipment, methods of construction, curing process, and surface conditions of the completed test pavement. The contractor shall demonstrate joint construction in transverse and longitudinal directions and the ability to achieve a smooth, hard, uniform surface free of excessive tears, ridges, spalls, and loose material.

- Size and Location Required for the Construction of a Test Section:

The test section shall be at least 75 feet long and more than one lane to establish longitudinal and transverse joint finishing techniques based on the size, length and thickness shown on the plans. The contractor shall construct the test section at a location mutually agreeable to the contractor and the Engineer. If the test area is constructed on site and meets all the applicable requirements, it may be incorporated into the final work and measured and paid for at the appropriate payment item. However, if the test section is not acceptable to the Engineer, removal and replacement of the test area shall be done at no additional cost to the Department. Subsequent test sections shall be constructed at no additional cost to the Department if the contractor fails to properly place and compact the RCC mix. Satisfactory performance of the test section shall be completed prior to commencing any production of RCC.

- Moisture Content and Density:

Prior to construction of the test section, the contractor shall test, in a laboratory qualified by the Department, the proposed job materials to obtain the moisture/density relationship in accordance with AASHTO T 180, Method D. Optimum moisture content, maximum dry density, and maximum wet densities shall be recorded. All test results shall be submitted to the Engineer for evaluation. The testing to determine field density shall be performed by the contractor under observation by the Engineer.

During the test section placement, the contractor shall calibrate nuclear density gauges in accordance with ASTM C1040, Test Method A – Direct Transmission, with a sample of the test section mix. Moisture reading of the gauge shall be calibrated using oven dry samples of plant-mixed RCC.

## 4.06	Mixing Process:

- General:

The same mixture shall be used for the entire project unless otherwise approved by the Engineer.

- Mixing Time:

Mixing time shall be adequate to ensure a thorough and complete mixing of all materials.

- Plant Calibration:

Prior to commencement of RCC production, the contractor shall carry out a complete and comprehensive calibration of the plant in accordance with the manufacturer's recommendations. The contractor shall provide all scales, containers, and other items necessary to complete the calibration.

The contractor shall submit daily plant records of production and quantities of material used each day to the Engineer.

## 4.07	Transportation of RCC:

The transportation of the RCC material from the plant to the areas to be paved shall be in dump trucks fitted and equipped, when necessary, with retractable protective covers for protection from rain or excessive evaporation. The loads of trucks shall be dumped entirely with no excess RCC material left behind. The dump trucks shall deposit the RCC material directly into the paver hopper or into a secondary material distribution system which deposits the material into the paver hopper. Dump truck delivery shall be timed and scheduled so that RCC material is spread and compacted within the specified time limits.

## 4.08	Weather:

- Cold Weather Operations:

RCC shall not be placed when the ambient air temperature is below 40 degrees F without written permission from the Engineer. When the contractor is permitted to place RCC at temperatures below 40 degrees F, the aggregates and/or mixing water shall be heated as necessary to keep the temperature of the RCC above 50 degrees F from the time of placement to the time of initial set (500 psi, as indicated by a penetrometer in accordance with the requirements specified in AASHTO T 197, but not less than one hour after placement); however, in no case shall the materials be heated in excess of 150 degrees F, nor shall aggregates from frozen stockpiles be incorporated into the mix. Materials entering the mixer shall be free from ice, snow, or frozen lumps. Salts, chemicals, and other materials shall not be incorporated in the RCC to prevent freezing.

If there are indications there will be temperatures below 40 degrees F during the first three days after placement of concrete, the RCC shall be protected from cold temperatures by keeping the RCC surface at a temperature above 50 degrees F for the first 72 hours after placement and above 32 degrees F for an additional 72 hours. However, the protective covering shall be retained in place until the temperature inside the protective covering reaches that of the surrounding atmosphere. Chemical admixtures for accelerated curing and control of temperatures shall not be used.

The contractor shall assume all risk and added cost connected with mixing, placing, and protecting of RCC during cold weather. Permission given by the Engineer to place RCC during such time will in no way relieve the contractor of responsibility for satisfactory results. Should it be determined at any time that RCC placed under such conditions is found to be unsatisfactory, it shall be removed and replaced with satisfactory RCC by the contractor at no additional cost to the Department.

- Hot Weather Operations:

Hot weather operation practices shall be followed in accordance with requirements of ACI 305 for all RCC work done when the temperature of the RCC exceeds 95 degrees F.

During periods of hot weather or windy conditions, special precautions shall be taken to minimize moisture loss due to evaporation. Cooling of aggregate stockpiles by shading or the use of a fine mist may be required. Protective covers shall be required on dump trucks.

- Rain:

Placement of the RCC shall not be done while it is raining hard enough to be detrimental to the finished product. Placement may continue during light rain or mists provided the surface of the RCC pavement is not eroded or damaged in any way.

## 4.09	Paver Operations:

The quantity of RCC material in the paver shall not be allowed to approach empty between loads. The material shall be maintained above the auger at all times during paving.

The paver shall proceed in a steady, continuous operation with minimal starts and stops. Maximum paver speed during laydown shall not exceed 10 feet per minute. Higher paver speeds may be allowed at the discretion of the Engineer.

## 4.10	Inaccessible Areas:

All areas inaccessible to either the roller or paver shall be paved with fresh material meeting the approved mix design specifications.

The loose material shall be spread in a manner that does not promote segregation or a significant change in moisture content. RCC may be placed by hand and compacted to project specifications with a hand tamper or mechanically with a roller, plate tamper, or other method after demonstration that such hand placed areas can reliably achieve the specified density and finished uniformly and consistently with the contiguous pavement.

## 4.11	Adjacent Lane Pavement:

When fresh longitudinal joints are approved by the Engineer, adjacent paving lanes shall be placed within 30 minutes.  The contractor shall keep the fresh edge (fresh vertical joint) from drying out until the adjacent lane is placed either by increasing productivity with tandem paving, spraying the joint surface with a light water mist, applying wet burlap cover, or by using a set-retarding admixture in the RCC mixture with approval by the Engineer.

If more than 30 minutes elapse between placements of adjacent lanes, the vertical cold joint shall require treatment in accordance with the requirements of Subsection 4.15(B) specified herein.

## 4.12	Broadcast Spreading:

Broadcasting or fanning the RCC material across areas being compacted will not be allowed. Such additions of materials may only be done immediately behind the paver and before any compaction has taken place.

## 4.13	Segregation:

If segregation occurs in the RCC during paving operations, placement shall cease until the cause is determined and corrected to the satisfaction of the Engineer. If the Engineer determines that segregation is too severe, the segregated area shall be removed and replaced at the contractor’s expense.

## 4.14	Compaction:

Compaction shall begin with the placement process and shall be completed within 60 minutes of the start of the mixing at the plant. This time may be increased or decreased at the discretion of the Engineer depending on ambient conditions of temperature and humidity. The contractor shall plan operations and supply sufficient equipment to ensure that these criteria are met.

Place RCC in lifts between 4 in. and 10 in. thick.  The Engineer may approve placing lifts at thicknesses at 10 in. or greater if the density testing using direct transmission test method ASTM C1040 (with a probe) at multiple locations throughout the entire lift thickness range, meet the specification requirements.

The contractor shall determine the sequence and number of passes by vibratory and non- vibratory rollers to obtain the specified density and surface finish. Rollers shall only be operated in the vibratory mode while in motion during primary compaction. Rollers shall only be operated in the static mode during final compaction. Rubber-tired rollers may be used for final compaction. Additional rollers shall be used if specific density requirements are not obtained or if placing operations get ahead of the rolling operations.

The roller shall not operate within 2 feet of the edge of a freshly placed lane until the adjacent lane is placed. After the placement of the adjacent lane, both edges of the two lanes shall be rolled together within the allowable time. If a cold joint is planned, the complete lane shall be rolled and procedures for the construction of a cold joint shall be followed.

Areas inaccessible to large rollers shall be thoroughly compacted with walk-behind vibratory rollers or plate tampers.

## 4.15	Joints:

- Fresh Vertical Joints:

A joint is considered a fresh joint when an adjacent RCC lane is placed within 30 minutes of placing the previous lane or as specified by the Engineer based on ambient conditions. Fresh joints do not require special treatment

- Vertical Cold Joints:

Any planned or unplanned construction joints that do not qualify as fresh joints are considered cold joints. The vertical joint face shall be wetted and in a moist condition immediately prior to placement of the adjacent RCC. For uncompact surfaces or slopes more than 10 degrees from the vertical, joints shall be cut vertically for the full depth of the pavement. Within 2 hours of final compaction, the edge of a cold joint shall be cut with approved mechanical equipment. For joints cut after 2 hours, the joint shall be saw cut to the full depth to create a sound vertical face. Raveling or tearing of the surface of a cold joint shall not be allowed. Cold joints exhibiting spalling or deterioration shall be saw cut for the full depth a minimum of 6 inches behind the spalling to create a new cold vertical joint. The joint shall then be thoroughly cleaned of loose or foreign material.

- RCC Pavement Joints at Structures:

RCC pavement joints at structures such as manholes, valves, mainline concrete pavement or concrete curb and gutter shall be sealed with preformed joint material conforming to the requirements of either ASTM D995 or ASTM D1752, or to the details shown in the plans.

- Transverse Control Joints:

Concrete transverse control joints shall be constructed at 24 times the thickness in inches or a maximum of 15 foot intervals in the RCC pavement to induce cracking at pre-selected locations, unless otherwise shown on the plans or as directed by the Engineer. At the option of the contractor, soft-cut or green-cut saws set to the manufacturer's recommendations shall be utilized as soon as possible behind the rolling operation. Conventional cut saws shall be used as soon as the sawing operation will not result in raveling or other damage to the RCC pavement, and shall be completed in the same day. All joints shall be cut to 1/4 the depth of the RCC pavement to a single saw blade width and sealed with Hot Applied Joint Sealant conforming to the requirements of Subsection 1011-3 of the specifications for joint and crack sealants or in accordance with the details shown on the plans. Joint spacing may be reduced for the joints, when paving near an intersection or pavement terminus, to a minimum of 10 feet to ensure that the final transverse joint is at least 10 feet from the obstruction.

## 4.16	Finishing:

The finished surface of the RCC pavement, when tested with a 10-foot straightedge or crown surface template, shall not vary from the straightedge or template by more than 1/4-inch at any one point and shall be within 1/4-inch of the specified finished grade. When surface irregularities are outside these tolerances, the contractor shall grind the surface to meet the tolerance at no additional cost to the Department.

The final surface texture after rolling and curing shall be smooth and uniform over the entire area of pavement and shall reasonably match the surface condition of the test strip without significant rips, tears, cracking, segregation, rock pockets, or areas of loose aggregate.  Paste shall be consistently distributed around the larger aggregate materials. The surface area shall be free of tears greater than 1/4-inch depth and 1/4-inch width as measured in the longitudinal direction of paving.

Troweling of the RCC shall be utilized to improve the overall aesthetic appearance of the RCC surface, provided all requirements of the specifications are met.

The contractor shall use self-propelled machine trowels. Determine the number of machine trowels required to perform the work at a rate equal to the concrete delivery rate. Self-propelled trowels shall be equipped with devices that adjust the underside to a true flat surface. The contractor shall perform texturing that produces striations parallel or perpendicular to the centerline in accordance with the details shown in the project plans, or as directed by the Engineer. Self-propelled troweling shall be demonstrated in the test section.

Admixtures may be used to facilitate troweling of the RCC and shall be used in accordance with manufacturer’s recommendations.

## 4.17	Curing:

RCC shall be cured in accordance with the requirements specified in Subsection 401-3.04(G) of the specifications.

## 4.18	Traffic:

The contractor shall protect the RCC from vehicular traffic during the curing period. Completed portions of the RCC pavement may be opened to light construction traffic (small pick-up trucks and cars) when the compressive strength of the RCC reaches 2500 psi but not earlier than 24 hours. Traffic shall not be parked on the pavement during the curing period and any moisture removed by the traffic tires shall be replaced immediately. The pavement may be opened to unrestricted traffic after 48 hours if 80 percent of the 28-day compressive strength has been achieved. If the temperature drops below 40 degrees F, the period of time that the temperature is below 40 degrees F will be added to the minimum time to opening. Any part of the pavement damaged by traffic or other causes prior to its final acceptance shall be repaired or replaced at no additional cost to the Department in a manner acceptable to the Engineer.

## 4.19	Density:

The contractor shall conduct field density tests in accordance with ASTM C1040, Test Method A – Direct Transmission, as soon as possible, but no later than 30 minutes after the completion of the rolling. Wet density shall be used for evaluation.

The required density shall be a minimum of 98 percent of the maximum laboratory density obtained according to AASHTO T 180, Method D, on a moving average of five consecutive tests with no individual test falling below 96 percent. (A moving average is the latest test and the preceding four tests. A single density measurement is used in five separate calculations of average density as appropriate for the progress of construction.) At least 5 tests shall be performed for each 250 cubic yards of RCC, with at least one of these 5 tests within 12 inches of a properly prepared and compacted joint. If the moving average density falls below 97 percent, the contractor shall stop the placing operation and perform the necessary adjustment to bring the density to or above 97 percent. The in-place density and moisture content shall be determined with a nuclear moisture-density gauge. The gauge or gauges shall be calibrated for moisture content of the RCC at the beginning of the work and at any time during the work.

## 5.0	Acceptance:

## 5.01	Pavement Thickness:

RCC shall be evaluated for thickness by the lot. A lot shall consist of each day’s production, up to 4000 square yards. In the event a day’s production is less than 4000 square yards, multiple days may be combined to form a lot.

To determine the acceptability for thickness of each lot of RCC, the following procedures shall be followed:

- An initial core shall be drilled in each lot and, if the thickness of the core is not deficient by more than 0.25 inches, the thickness of the RCC in that lot will be considered acceptable;

- If the thickness of the initial core is deficient by more than 0.25 inches, but less than or equal to 0.75 inches, two additional cores shall be drilled within that lot and the thickness of the three cores will be averaged. The average of the three cores will be used to determine acceptability, and the unit price paid for the RCC in that lot will be adjusted as specified in Subsection 7.0 of the specifications; and

- If any core is deficient by more than 0.75 inches, additional cores shall be drilled at intervals not to exceed 10 feet in each direction from the deficient core, parallel to the roadway center line, until one core is obtained in each direction which is not deficient by more than 0.75 inches. The RCC between these two cores will be evaluated separately from the balance of the RCC in that lot, and unless otherwise directed by Engineer, shall be removed and replaced with RCC of the specified thickness at no additional cost to the Department.

At all locations where cores have been drilled, the resulting holes shall be filled with RCC or other similar material as approved by the Engineer.

The contractor may submit a written proposal to the Engineer to accept the RCC lot for thickness based on alternative technology to coring. The Engineer will make the final decision as to whether the proposed technology is acceptable.

## 5.02	Compressive Strength:

- General:

RCC shall be evaluated for compressive strength by the lot. A lot shall consist of each day’s production, up to 4000 square yards. The contractor shall sample four random locations for each lot under observation of the Engineer and prepare a set of 2 test cylinders with nominal dimensions of 6 inches in diameter and 12 inches in length for each location in accordance with ASTM C1435. In the event a day’s production is less than 4000 square yards, multiple days may be combined to form a lot. When a lot consists of production from more than one day, the following conditions apply: at least one sample shall be taken each day, and no mix design changes shall be made within the lot. If changes are made in the mix design, new lots will be established.

## The minimum average compressive strength of RCC shall be 4000 psi for each lot at twenty eight days. Each lot shall be represented by four random samples.  A compressive strength test will consist of the average strength of two cylinders prepared with material taken from a single load of RCC. If any cylinder should show obvious evidence of improper sampling, molding, or testing, it will be discarded and the strength test will consist of the strength of the remaining cylinder.  All test cylinders will be prepared in accordance with the requirements of ASTM C1435. Testing for compressive strength will be performed in accordance with the requirements of ASTM C39.  The mean value of the four compressive strength tests will be reported to the nearest 10 pound per square inch.  The unit price paid for the RCC in that lot will be adjusted in accordance with the provisions of Subsection 7.0 of the specifications.

## The contractor shall perform compressive strength testing in a laboratory qualified by the Department under observation of the Engineer.

## Extra cylinders may be cast and tested at the contractor’s expense to monitor strength at different ages or for early opening to traffic.

- In-Place Compressive Strength:

If the mean value of compressive strength of the RCC indicated by the testing of concrete cylinders is less than the required strength, cores shall be taken and tested to determine the in-place compressive strength. Concrete coring and testing shall be completed within 48 calendar days after the placement of the RCC.

The contractor shall extract three cores at random locations in the suspect area.  Removal, handling, and testing of the compressive strength of the cores shall be performed in accordance with ASTM C42.

For single lift pavements, outside core barrel diameter shall be 4 inches resulting in an extracted core diameter of approximately 3.7 inches. Cores shall be trimmed to provide a flat surface on the top and bottom portions that are perpendicular to the longitudinal axis.  To ensure that a representative portion of the RCC core is tested for compressive strength, approximately equal amounts of material shall be removed from the top and bottom portions of the RCC core where possible.  Unequal amounts may be needed depending on the core thickness and bottom deviation / aggregate size and requirement to maintain L/D > 1.0.  The minimum amount of material to be removed from the top and bottom sides of the core shall be 1/4 inch.

When testing dual lift RCC cores, the top and bottom lifts shall be tested independently. The outside core barrel diameter shall be 4 inches resulting in an extracted core diameter of approximately 3.7 inches.  The final overall RCC strength of the dual lift RCC core shall be the average compressive strength of the top and bottom cores.  When sizing RCC dual lift RCC cores, the horizontal bonded joint shall be clearly identified prior to sizing.  The minimum amount of trimming for dual lift RCC cores shall be increased to 3/8 inch above and below this joint.  This section of the core shall be removed to ensure that the horizontal joint has not been included in either the top or bottom lift cores after sizing.

RCC Cores shall be moisture conditioned in accordance with ASTM C42

RCC cores shall be capped with bonded caps.  Prior to capping, the core surfaces at both ends shall be dried sufficiently to ensure the cap bonds to the core.

The in-place compressive strength verification shall consist of three cores. If the average of the three cores exceeds the minimum specified compressive strength in Subsection 5.02(A), the RCC in the lot is acceptable and is subject to full payment. If the average strength of the three cores is less than the specified compressive strength in Subsection 5.02(A), the RCC is acceptable at a reduced value through a unit price adjustment as shown in Table 2.

## 6.0	Method of Measurement:

The RCC pavement will be measured by the square yard, complete in place, and accepted by the Engineer. RCC constructed outside the areas and locations designated on the plans will not be measured for payment.

## 7.0	Basis of Payment:

## The accepted quantities of RCC, measured as provided above, will be paid for at the contract unit price, complete in place, except that an adjustment to the nearest cent in the contract unit price will be made in accordance with Table 2 and Table 3, when either the quality of concrete represented by the mean value of the four compressive strength tests is less than the specified seven day compressive strength or when the average lengths of cores indicates deficiencies in thickness by more than 0.25 inches, but less than or equal to 0.75 inches.

No separate measurement or payment will be made for testing or joints, the cost being considered as included in the cost of this contract item.

## Where a deficiency exists in both the average length of cores and the average compressive strength, the amount of the contract unit price adjustment will be the appropriate percentage of contract unit price allowed from Table 2 less the unit price adjustment from Table 3.

| TABLE 2 ADJUSTMENT IN CONTRACT UNIT PRICE FOR DEFICIENCY IN STRENGTH OF RCC |  |
| --- | --- |
| Percentage of Design Strength | Unit Price Allowed; Percent of Contract |
| ≥100 | 1.00 |
| 90 – 99 | 0.95 |
| 80 – 89 | 0.80 |
| 75 – 79 | 0.65 |
| Note: When the in-place compressive strength verification is less than 75 percent of design strength, the RCC pavement shall be removed and replaced at no additional cost to the Department. |  |

| TABLE 3 ADJUSTEMENT IN CONTRACT UNIT PRICE FOR DEFICIENCY IN THICKNESS OF RCC |  |
| --- | --- |
| Average Core Length, Less Than Specified Thickness: Inches | Unit Price Allowed: Percent of Contract |
| 0.00 to 0.25 | 100 |
| 0.26 to 0.35 | 93 |
| 0.36 to 0.45 | 85 |
| 0.46 to 0.55 | 75 |
| 0.56 to 0.75 | 50 |
| Greater than 0.75* | 25 |
| Note: *Material represented by cores deficient by more than 0.75 inches in thickness will be evaluated as to acceptance. The Engineer will determine if the material can be left in place. RCC allowed to remain in place will be subject to the unit price adjustments presented in Tables 2 and 3. RCC not permitted to remain in place shall be removed and replaced at no additional cost to the Department. |  |