* 	USE THIS STORED SPECIFICATION ON PROJECTS INVOLVING CAST-IN PLACE BRIDGE DECK CONCRETE      *

(601BDCFA, 02/19/26)

SECTION 601 	CONCRETE STRUCTURES:

601-2.01		General: of the Standard Specifications is modified to add:

For cast-in place concrete used in bridge deck placement, fiber additives shall be incorporated into the concrete mix for plastic shrinkage control. Fiber additive shall be Polyolefin, conforming to the requirements of ASTM D7508/D7508M and applicable requirements of Section 1006 of the specifications. The specific type, size, and quantity of fiber additive shall be determined by the mix designer. The contractor shall submit the results from ASTM C1579, along with the proposed concrete mix design, to the Engineer for review and approval. Fiber additive shall be composed of 100 percent virgin materials and shall be non-corrosive, non-magnetic, and entirely alkali-free.

601-6	Basis of Payment: of the Standard Specifications is modified to add:

No separate measurement or payment will be made for fiber additive, the cost being considered as included in the cost of the Class S or Class B concrete.