(604STHSF, 02/19/26)

SECTION 604 	STEEL STRUCTURES:

604-2.03		High-Strength Bolts, Nuts and Washers: the first and the second paragraphs of the Standard Specifications are revised to read:

High Strength Bolts shall conform to ASTM F3125 Grade A325 except as may be modified herein.

The maximum hardness for ASTM F3125 Grade A325 bolts shall be 33 HRC for diameters 1 inch and smaller, and 30 HRC for diameters greater than 1 inch.

604-3.02	Fabrication: the second paragraph of the Standard Specifications is revised to read:

The structural steel fabrication plant shall be certified under the AISC Quality Certification program to the standard and supplement requirements for the type of work being performed. The following categories are defined under the AISC Quality Certification program:

Certified Bridge Fabricator – Simple (SBR)

Certified Bridge Fabricator – Intermediate (IBR)

Certified Bridge Fabricator – Advanced ( ABR)