*	          USE WHEN SPECIFIED IN THE MATERIALS DESIGN REPORT		    *

*                           USE STORED SPECIFICATION 109PAVSM WHEN AN                           *

*              INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE               *

*                                 PAVEMENT SMOOTHNESS IS SPECIFIED IN                                   *

*                                         THE MATERIALS DESIGN REPORT                                           *

*	USE IN CONJUNCTION WITH THE FOLLOWING:					    *

*		BID ITEM:							9240170			    *

*		STORED SPECIFICATIONS:			924CQC			    *

*									        1001MATL			    *

*	FILL IN THE FOLLOWING (SHOWN IN RED TEXT):					    *

*		416-3			UNIT WEIGHTS				(As Needed)		    *

*

*		416-3.03(B)	TYPE OF ASPHALT BINDER		(1 place)		    *

(416ROLL, 06/19/25)

SECTION 416		ASPHALTIC CONCRETE – END PRODUCT: of the Standard Specifications is revised to read:

## 416-1	Description:

The work under this section shall consist of constructing Asphaltic Concrete-End Product, hereinafter asphaltic concrete, by furnishing all materials, mixing at a plant, hauling and placing a mixture of aggregate materials, mineral admixture, and bituminous material (asphalt cement) to form a pavement course or to be used for other specified purposes, in accordance with the details shown on the project plans and the requirements of the specifications.

Reclaimed asphalt pavement (RAP), as defined in Subsection 416-3.04 of the specifications, may be used in the mixture provided all requirements of the specifications are met.  References to the use of RAP in this section apply only if RAP is utilized as part of the mixture.  ADOT Materials Practice and Procedure Directive No. 20, “Guidance on the Use of Reclaimed Asphalt Pavement (RAP) in Asphaltic Concrete”, shall be used in conjunction with the requirements of the specifications.

The contractor shall acquire and make all arrangements for a source or sources of material, furnish a mix design which will meet the design criteria specified hereinafter, and provide all the equipment, materials, and labor necessary to complete the work.

## 416-2	Asphaltic Concrete Mix Design Criteria:

Mix designs shall be developed utilizing a minimum ratio of three (3) for the lift thickness to nominal maximum aggregate size.

Mix designs shall be developed by the contractor on the basis of the following criteria and tested in accordance with the requirements of the following test methods:

| Criteria |  |  | Requirements |  |  |  | Arizona Test/AASHTO |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1/2” Mix |  | 3/4” Mix | Base Mix | Method |
| 1. Voids in Mineral Aggregate: %, Range |  |  | 15.5 - 18.5 |  | 15.0 - 18.0 | 14.5 - 17.0 | Note (2) |
| 2. Effective Voids: %, Range |  |  | 4.0 ± 0.2 |  | 4.0 ± 0.2 | 4.0 ± 0.2 | Note (2) |
| 3. Absorbed Asphalt: %, Range |  |  | 0 - 1.0 |  | 0 - 1.0 | 0 - 1.0 | Note (2) |
| 4. Index of Retained Strength: %, Minimum |  |  | 60 (Note 1) |  | 60 (Note 1) | 60 (Note 1) | Note (3) |
| 5. Wet Strength: psi, Minimum |  |  | 150 |  | 150 | 150 | Note (3) |
| 6. Stability: pounds, Minimum |  |  | 2,000 |  | 2,000 | 3,000 | Note (2) |
| 7. Flow: 0.01-inch, Range |  |  | 8 - 16 |  | 8 - 16 | 8 - 16 | Note (2) |
| 8. Mix Design Grading Limits |  |  |  |  |  |  | AASHTO T 11, T 27 |
|  | Percent Passing |  |  |  |  |  |  |
| Sieve Size | 1/2 inch Mix |  |  | 3/4 inch Mix |  | Base Mix |  |
|  | Without Admix. | With Admix. |  | Without Admix. | With Admix. | Without Admix. | With Admix. |
| 1-1/4 inch |  |  |  |  |  | 100 | 100 |
| 1 inch |  |  |  | 100 | 100 | 90 -100 | 90 - 100 |
| 3/4 inch | 100 | 100 |  | 90 - 100 | 90 - 100 | 85 - 95 | 85 - 95 |
| 1/2 inch | 90 - 100 | 90 - 100 |  | --- | --- | --- | --- |
| 3/8 inch | 67 - 82 | 67 - 82 |  | 62 - 77 | 62 - 77 | 57 - 72 | 57 - 72 |
| No. 8 | 40 - 48 | 41 - 49 |  | 37 - 46 | 38 - 47 | 32 - 42 | 33 - 43 |
| No. 40 | 10 - 18 | 11 - 19 |  | 10 - 18 | 11 - 19 | 8 - 16 | 9 - 17 |
| No. 200 | 1.5 - 4.5 | 2.5 - 6.0 |  | 1.5 - 4.5 | 2.5 - 6.0 | 1.5 - 3.5 | 2.5 - 5.0 |
| Notes: If the average elevation of the project is above 3,500 feet, the index of retained strength shall be a minimum of 70 percent. For mixes without RAP, Arizona Test Method 815. For mixes with RAP, Arizona Test Method 833. For mixes without RAP, Arizona Test Method 802 (as modified by Arizona Test Method 815). For mixes with RAP, Arizona Test Method 802 (as modified by Arizona Test Method 833). |  |  |  |  |  |  |  |

The ratio of the mix design composite gradation target for the No. 200 sieve, including mineral admixture, to the effective asphalt content shall be within the range 0.7 to 1.3.

## 416-3	Materials:

For comparative purposes, quantities shown in the bidding schedule have been calculated based on the following data:

(In the following table, use only the columns called for

in the Materials Design Report.)

| Standard Mixes | 1/2” Mix | 3/4” Mix | Base Mix |
| --- | --- | --- | --- |
| Unit Weight (lb./cu. ft.) | XXX | XXX | XXX |

### 416-3.01	Mineral Aggregate:

- General:

Mineral aggregate shall consist of virgin aggregate, or a combination of virgin aggregate and aggregate from RAP (RAP aggregate).  When the terms “mineral aggregate” or “aggregate” are used without being further described as “virgin” or “RAP”, the intended meaning is the total aggregate material used in the mixture.

No individual stockpile or hot bin usage of either virgin aggregate or RAP aggregate shall be less than 3 percent of the total mineral aggregate.

Virgin Mineral Aggregate:

The contractor shall provide a source in accordance with the requirements of Section 1001 of the specifications.

Coarse virgin mineral aggregate shall consist of crushed gravel, crushed rock, or other approved inert material with similar characteristics, or a combination thereof, conforming to the requirements of these specifications.

Fine virgin mineral aggregate shall consist of natural sand or of sand prepared from rock, or other approved inert materials, or a combination thereof, conforming to the requirements of these specifications.

RAP Mineral Aggregate:

RAP aggregate shall conform with Materials Practice and Procedure Directive No. 20, “Guidance on the Use of Reclaimed Asphalt Pavement (RAP) in Asphaltic Concrete”,

Mineral Aggregate Characteristics:

Aggregates shall be free of deleterious materials, clay balls, and adhering films or other material that prevent the thorough coating with the asphalt cement.

Mineral aggregate shall conform to the following requirements when tested in accordance with the applicable test methods.

| Mineral Aggregate Characteristics | Test Method | Requirement |
| --- | --- | --- |
| Combined Bulk Oven Dry Specific Gravity (1) | Arizona Test Method 251 | 2.350 - 2.850 |
| Combined Water Absorption (1) | Arizona Test Method 251 | 0 – 3.0% |
| Sand Equivalent (1) | AASHTO T 176 (After thoroughly sieving the sample, no additional cleaning of the fines from the plus No. 4 material is required.) | Minimum 55 |
| Abrasion (2) | AASHTO T 96 | 100 Rev., Max. 9% 500 Rev., Max. 40% |
| Fractured Coarse Aggregate Particles (3) | AASHTO T 335 | Minimum 70% (at least one fractured face, determined on plus No. 4 material) |
| Carbonates (3) and (4) | Arizona Test Method 238 | Maximum 20% |
| Notes: When the mix design contains RAP, the requirements shall be for the virgin aggregate portion only. Abrasion shall be performed separately on materials from each source of mineral aggregate, including RAP aggregate. All sources shall meet the requirements for abrasion. When the mix design contains RAP, the requirements shall be for the composite of virgin and RAP aggregate. Testing for carbonates only applies if either of the following conditions exist: The asphaltic concrete is the designed final pavement surface normally used by traffic. The asphaltic concrete, temporary or otherwise, will be subject to traffic for more than 60 days. |  |  |

Tests on aggregates outlined above, except for abrasion, shall be performed on materials furnished for mix design purposes and composited to the mix design gradation.  When RAP is used in the mixture, RAP aggregates for testing shall be obtained from the RAP material using Method A of AASHTO T 164, prior to combining with the virgin aggregate.

### 416-3.02	Mineral Admixture:

Mineral admixture will be required.  The amount used shall be 1.0 percent, by weight of the mineral aggregate, unless testing demonstrates that additional admixture is required in order to meet the mix design criteria for Wet Strength and Index of Retained Strength.  A maximum of 2.0 percent admixture will be permitted.  The exact amount of admixture required shall be specified in the mix design.  Mineral admixture shall be either Portland cement, blended hydraulic cement or hydrated lime conforming to the following requirements.

| Material | Requirement |
| --- | --- |
| Portland Cement, Type I, or Type II | ASTM C150 |
| Blended Hydraulic Cement, Type IP or IL | ASTM C595 |
| Hydrated Lime | ASTM C1097 |

The certification and acceptance of Portland cement, blended hydraulic cement, and hydrated lime shall be in accordance with ADOT Materials Practice and Procedure Directive No. 13, "Certification and Acceptance of Hydraulic Cement, Fly Ash, Natural Pozzolan, Silica Fume, and Lime".

### 416-3.03	Bituminous Material:

- General:

Bituminous material shall consist of performance grade (PG) asphalt binder (virgin binder), or a combination of virgin binder and binder from RAP (RAP binder).  When the terms “bituminous material”, “asphalt cement”, “asphalt binder”, or “binder” are used without being further described as “virgin” or “RAP”, the intended meaning is the total bituminous material used in the mixture.

The percent of asphalt cement used shall be based on the weight of total mix (asphalt cement, mineral aggregate, and mineral admixture).

Virgin Bituminous Material:

Virgin asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005 of the specifications.  The type of virgin asphalt binder shall be PG XXXXX or, if RAP is used in the mixture, the virgin asphalt binder shall be as required to meet the blending requirements in Subsection 416-3.03(C) of the specifications and Arizona Test Method 833.

The contractor shall provide the laboratory mixing and compaction temperature ranges to the mix design laboratory for each PG asphalt binder used for mix design purposes.  The laboratory mixing temperature range is defined as the range of temperatures where the un-aged virgin asphalt binder has a rotational viscosity of 0.17  0.02 Pascal·seconds, measured in accordance with AASHTO T 316.  The laboratory compaction temperature range is defined as the range of temperatures where the un-aged virgin asphalt binder has a rotational viscosity of 0.28  0.03 Pascal·seconds, measured in accordance with AASHTO T 316.  The testing required in AASHTO T 316 shall be performed at 275 degrees F and 350 degrees F, and a viscosity-temperature curve developed in accordance with ASTM D2493.  The viscosity-temperature curve shall be included in the mix design report.  For PG asphalt binders that have a maximum laboratory mixing temperature exceeding 325 degrees F or a maximum laboratory compaction temperature exceeding 300 degrees F, the laboratory mixing and compaction temperature ranges shall be specified in writing by the virgin asphalt binder supplier.  A viscosity-temperature curve will meet this requirement for written documentation if the viscosity-temperature curve is developed and submitted by the binder supplier and includes language that the recommended laboratory mixing and compaction temperatures are within acceptable ranges, and the submittal includes a statement indicating the maximum laboratory mixing temperature to which the binder can be heated without damage.  The laboratory mixing and compaction temperature ranges, as well as the actual laboratory mixing and compaction temperatures used, shall be reported on the mix design.  The contractor shall ensure that the asphalt binder supplier information required in this paragraph is provided to all appropriate parties in a timely manner, and that copies are included in the mix design report.  The laboratory mixing and compaction temperatures are for mix design purposes only.  Field mixing and compaction temperatures are specified in Subsections 416-6 and 416-7 of the specifications.

RAP Bituminous Material:

RAP binder content shall be determined by AASHTO T 308.  RAP binder shall consist of the asphalt binder portion of the reclaimed asphaltic pavement.  A maximum of 30 percent RAP binder, by weight of total binder in the mix, may be used in mixes placed in a lower lift (minimum 2 inches below finished surface).  A maximum of 24 percent RAP binder, by weight of total binder in the mix, may be used at all other locations.

When less than or equal to 17 percent RAP binder is used, by weight of total binder in the mix, no testing is required on the RAP binder.  When greater than 17 percent RAP binder is used, by weight of total binder in the mix, the RAP binder shall be extracted, recovered, and tested in accordance with the requirements of Arizona Test Method 833.  The virgin binder grade shall be modified if necessary to ensure the blend of virgin and RAP binder meets the PG grade specified in the Subsection 416-3.03(B) of the specifications.  However, a change of only one virgin PG binder grade (6 degrees C on either or both the high and low temperatures) will be allowed from that shown in Subsection 416-3.03(B) of the specifications.

### 416-3.04	Reclaimed Asphalt Pavement (RAP):

RAP shall consist of salvaged, milled, pulverized, broken, or crushed asphalt pavement.  If RAP is generated by milling, the minimum removal depth shall be 1-1/2 inches.  The source of RAP may be from ADOT or other projects.  The contractor shall be responsible for determining the suitability of the RAP for use in the mixture, regardless of its source.

RAP material shall pass the 1-1/4 inch sieve.  For asphaltic concrete containing greater than 17 percent RAP aggregate, the RAP material shall be processed into uniform coarse and fine stockpiles such that there will be a minimum amount of fines.

RAP shall be stockpiled so that segregation is minimized.  When two RAP stockpiles are used, acceptable methods to prevent intermingling of stockpiles shall be provided.

The Engineer reserves the right to reject obviously defective salvaged material or salvaged material that is not representative of the material used in the mix design.

## 416-4	Mix Design:

Utilizing mineral aggregate and RAP which has been crushed, processed, separated and stockpiled, a mix design shall be formulated and submitted by the contractor to the Engineer.  The mineral aggregate and RAP samples used for mix design purposes shall be representative of materials to be used during production.

The mix design shall be based on the mix design criteria and other requirements hereinbefore specified, utilizing asphalt cement and mineral admixture of the type and from the sources proposed for use in the production of asphaltic concrete.

The mix design shall be prepared by or under the direct supervision of a professional engineer experienced in the development of mix designs and mix design testing.  The mix design engineer shall meet the requirements given in ADOT Materials Practice and Procedure Directive No. 4, “Asphaltic Concrete Mix Design Proposals and Submittals”.  The mix design shall be provided in a format that clearly indicates all the mix design requirements and shall be sealed, signed, and dated by the mix design engineer.

The mix design shall be prepared by a mix design laboratory that has met the requirements of ADOT Materials Practice and Procedure Directive No. 19, “ADOT System for the Evaluation of Testing Laboratories”.

The contactor may propose the use of a mix design that has been developed for a previous project that is less than a year old with no additional requirements.  The proposed mix design shall meet the requirements of these specifications.  If the proposed mix design is greater than one year old but less than two years old, the contractor shall provide evidence that the type and source of bituminous material, the type of mineral admixture, and the source and methods of producing virgin mineral aggregate and RAP have not changed since the formulation of the previous mix design.  The contractor shall also provide current test results for all specified characteristics of the mineral aggregate and RAP proposed for use.  The Engineer will determine if the previously used mix design is suitable for the intended use and if the previous use of the mix design was satisfactory to the Department.  The Engineer will either approve or disapprove the proposed mix design.  Should the Engineer disapprove the use of the previously used mix design, the contractor shall prepare and submit a new mix design proposal in accordance with the requirements of these specifications.

A previously used mix design older than two years from the date it was formulated, sealed, signed, and dated shall not be allowed for use.  Once approved for use on a project, a mix design may be used for the duration of that project.

The mix design shall contain as a minimum:

(A)	The name and address of the testing organization and the person responsible for the mix design testing;

(B)	The specific location(s) of the source(s) of mineral aggregate;

(C)	The supplier, refinery, type of asphalt cement and any modifiers including polymers.  The source and type of mineral admixture.  The percentage of asphalt cement and mineral admixture to be used;

(D)	The anticipated mineral aggregate gradation in each stockpile;

(E)	Mix design gradation.  The mix design shall contain the mineral aggregate gradation, and also the gradation with mineral admixture;

(F)	The results of all testing, determinations, etc., such as: specific gravity of each component, water absorption, sand equivalent, loss on abrasion, fractured coarse aggregate particles, percent carbonates (if required), immersion compression results (Index of Retained Strength, wet and dry strengths), Marshall stability and flow, asphalt absorption, percent air voids, voids in mineral aggregate, and bulk density; and

(G)	Viscosity-temperature curve along with the laboratory mixing and compaction temperature ranges, as well as the actual laboratory mixing and compaction temperatures used.

When RAP is used in the mixture, the following additional information shall be included in the mix design:

(A)	The specific location(s) of the source(s) of RAP;

(B)	The anticipated RAP gradation, RAP aggregate gradation, and RAP binder content in each stockpile;

(C)	If greater than 17 percent RAP binder is used in the mixture, the results of all tests on the recovered RAP binder, as well as all tests on the blend of virgin binder and recovered RAP binder;

(D)	The percent RAP binder, virgin binder, and total binder in the mixture;

(E)	The composite gradation of virgin and RAP aggregates, with and without mineral admixture.  The composite gradation of the virgin aggregate and RAP, with and without mineral admixture.

(F)	The results of all testing, determinations, etc., for the RAP, virgin aggregate, RAP aggregate, and composite of virgin and RAP aggregates as required, such as: specific gravity, water absorption, sand equivalent, loss on abrasion, fractured coarse aggregate particles, and percent carbonates.

(G)	The viscosity-temperature curve along with the laboratory mixing and compaction temperature ranges for the blended binder, if greater than 17 percent RAP binder is used in the mixture, as well as the actual laboratory mixing and compaction temperatures used.

Test results used in the formulation of the mix design shall be from testing performed no earlier than 45 days prior to the date the mix design is signed by the mix design engineer.  Historical abrasion values may be supplied on sources provided the testing was conducted within the past two years.

The mix design shall be submitted to the Engineer under a cover letter signed by an authorized representative of the contractor.

A copy of the mix design and representative samples of the materials used in the mix design shall be submitted to the Engineer for calibration of the ignition furnace, and for the determination of sand equivalent and fractured coarse aggregate particles.  Approximately 300 pounds of virgin mineral aggregate (proportional to the mix design gradation), 3 gallons of asphalt cement, and 1 gallon of mineral admixture shall be submitted.  When RAP is used, a minimum of 40 pounds of representative RAP material and a minimum of 10 pounds of solvent-extracted RAP aggregate, per AASHTO T 164, Method A, shall be submitted.  If RAP is fractionated, the RAP and RAP aggregate from each stockpile shall be kept separate.  The Engineer shall witness the sampling of the virgin mineral aggregate and RAP.  The mix design and samples shall be submitted to the Engineer at least five working days prior to the start of asphaltic concrete production.

The sand equivalent and fractured coarse aggregate particles shall meet the requirements specified in Subsection 416-3.01 of the specifications.

If the mineral aggregate fails to meet the requirements specified herein, asphaltic concrete production shall not commence, and the contractor shall either submit a revised mix design which is representative of the materials produced or correct the deficiencies in the aggregate stockpiles.

The Engineer will review the mix design to assure that it contains all required information.  If it does not, it will be returned within two working days of receipt of all samples and mix design information, for further action and resubmission by the contractor.

If the contractor elects to change its source(s) of mineral aggregate or RAP, or adds or deletes the use of a stockpile(s) regardless of source, the contractor shall furnish the Engineer with a new mix design which meets the requirements specified hereinbefore.

If changes are made in the source or type of bituminous material, or the type of mineral admixture, the contractor shall provide verification testing results.  Verification testing shall be performed at the original mix design asphalt content using the original mineral aggregate and RAP (if used), the proposed bituminous material, and/or the proposed mineral admixture.  Three specimens shall be fabricated and tested for bulk density, maximum theoretical density, and effective voids.  The percent effective voids shall be within  0.2 of the percent effective voids in the original design and also be within the current effective voids mix design specification limits.  Verification testing results shall not replace target values shown in the original mix design.  All target values from the original design shall be used in future production with the exception of any self-directed target value changes that are requested.  The verification process does not ensure that the contractor can meet the target values during production.

In addition to the verification testing specified above, verification testing for immersion compression may also be required.  If there is a change in the type of mineral admixture, immersion compression testing is required.  If there is a change in the source or type of bituminous material, immersion compression testing is required if the Index of Retained Strength of the original mix design is less than 10 percentage points greater than the specified minimum, or if the Wet Strength is less than 100 pounds per square inch greater than the specified minimum.

The contractor may make self-directed target changes to the approved mix design within the limits shown below.  Requests for self-directed target changes shall be made in writing and acknowledged by the Engineer prior to start of production for a lot.  Self-directed target changes shall meet contract requirements for mix design criteria and grading limits.

| MEASURED CHARACTERISTICS | ALLOWABLE SELF-DIRECTED TARGET CHANGES |
| --- | --- |
| Gradation (sieve size): 3/8 inch No. 8 No. 40 | ±4% from mix design target value ±4% from mix design target value ±2% from mix design target value |
| Asphalt Cement Content | Within range of +0.4% to -0.2% from mix design target value |
| Effective Voids | None |

The contractor may propose target changes to the approved mix design for the Engineer’s approval.  The Engineer will determine if the proposed target change will result in mix production that meets the contract requirements for mix design criteria and grading limits. For acceptance purposes, target changes will not be retroactive.

In no case shall the approval of mix design changes relieve the contractor of the responsibility for the results obtained by the use of such approved changes.

Should a mix design prove unsatisfactory to the contractor during production, the contractor shall furnish the Engineer with a revised mix design.  For acceptance purposes, the revised mix design will not be retroactive.

The contractor shall not change its methods of crushing, screening, washing, or stockpiling from those used during production of material used for mix design purposes without approval of the Engineer or without preparing a new mix design.

## 416-5	Contractor Quality Control:

The contractor shall perform the quality control measures described in Subsection 106.04(C) of the specifications.  At the weekly meeting, the contractor shall be prepared to explain and discuss how the following processes will be employed:

- Aggregate production, including crusher methods, pit extraction, and washing;

RAP production, including milling, crushing, screening, and handling methods;

Stockpile management, including stacking methods, separation technique, plant feed technique, stockpile pad thickness, and segregation prevention;

Proportioning and plant control, including plant scale calibration, mix temperature control, storing method, and addition of admixture;

Transporting and placing, including hauling distance and temperature control, segregation and non-uniform placement control, and joint placement and technique; and

Compaction, including types and weight of rollers, establishing and monitoring of roller patterns, and temperature controls.

The contractor shall obtain samples and perform the tests specified in the following table:

| CONTRACTOR QUALITY CONTROL TESTING REQUIREMENTS |  |  |  |
| --- | --- | --- | --- |
| Type of Test | Test Method | Sampling Point | Minimum Testing Frequency |
| Virgin Mineral Aggregate |  |  |  |
| Gradation | AASHTO T 27 | Crusher Belt or Stockpile | 1 per stockpile per day |
| Sand Equivalent | AASHTO T 176 |  | 1 per 2000 Tons of total virgin aggregate (1) |
| Fractured Coarse Aggregate Particles | AASHTO T 335 |  |  |
| Reclaimed Asphalt Pavement |  |  |  |
| Gradation, Moisture Content, and Binder Content | AASHTO T 308 (Appendix A) | Crusher Belt or Stockpile | 1 per stockpile per day |
| RAP Aggregate |  |  |  |
| Gradation | AASHTO T 27 | Crusher Belt or Stockpile | 1 per stockpile per day |
| Fractured Coarse Aggregate Particles | AASHTO T 335 |  | 1 per stockpile every other day |
| Asphaltic Concrete |  |  |  |
| Gradation | AASHTO T 27 or T 308 (for both Non-RAP and RAP mixes) | Cold Feed, Hot Bins, Roadway, or Plant | 1 per 1000 Tons |
| Asphalt Content | AASHTO T 287, T 308 (for both Non-RAP and RAP mixes),or other approved methods | Roadway or Plant | 1 per 1000 Tons |
| Voids | AASHTO R 68, T 166, T 209, T 269 |  | 1 per 1000 Tons each day. Maximum of 4 per day. |
| Compaction | AASHTO T 355 | Roadway | 1 per 300 tons |
| Notes: (1) Prior to the completion of the mix design, quality control tests on mineral aggregate shall be performed based on the anticipated percent use of each stockpile. Samples taken from individual stockpiles may be composited prior to performing the required tests, or testing may be performed on material from each stockpile and the composite test result for each required test determined mathematically. |  |  |  |

## 416-6	Construction Requirements:

The contractor shall be responsible for the proportioning of all materials, for the hauling, placing, loading, spreading, and finishing of asphaltic concrete and for the applying of bituminous material, such as tack coats, prime coats, and provisional seals, all in accordance with the appropriate portions of the specifications.

The asphaltic concrete hot plant shall conform to the requirements of Section 403 of the specifications.

During production, the percent RAP aggregate and percent RAP binder shall not exceed the maximum allowed in Subsections 416-3.01(C), 416-3.03(C), and 416-3.04 of the specifications.  In addition, the percent RAP material shall be maintained to within plus 2 percent and minus 5 percent of the mix design value(s).  When two RAP stockpiles are used, this tolerance shall apply to the total percent RAP material in the mixture, as well as the percent RAP material from each stockpile.

The temperature of asphaltic concrete or mineral aggregate upon discharge from the drier shall not exceed 325 degrees F unless a higher temperature is recommended in writing by the asphalt binder supplier and approved by the Engineer.

All courses of asphaltic concrete shall be placed and finished by means of self-propelled paving machines except under certain conditions or at certain locations where the Engineer deems the use of self-propelled paving machines impractical.

Self-propelled paving machines shall spread the mixture within the specified tolerances, without segregation or tearing, true to the line, grade, and crown indicated on the project plans.  Pavers shall be equipped with hoppers and augers which shall distribute the mixture uniformly in front of adjustable screeds.

Pavers shall be equipped with a screed for the full width being paved, heated if necessary, and capable of spreading and finishing all courses of asphaltic concrete.

Pavers shall be equipped with automatic screed controls with sensors for either or both sides of the paver, capable of sensing grade from an outside reference line, sensing the transverse slope of the screed, and providing the automatic signals which operate the screed to maintain the desired grade and transverse slope.

Failure of the control system to function properly shall be cause for the suspension of the placing of asphaltic concrete.

The base or subgrade upon which asphaltic concrete is to be placed shall be prepared and maintained in a firm condition until asphaltic concrete is placed.  It shall not be frozen or excessively wet.

At any time, the Engineer may require that the work cease or that the work day be reduced in the event that weather conditions, either existing or expected, are anticipated to have an adverse effect upon the asphaltic concrete.

All wheels and tires of compactors shall be wetted with water, or if necessary soapy water, or a release agent in order to prevent the sticking of asphaltic concrete. All other equipment surfaces shall be treated when necessary with a release agent. Only release agents evaluated through AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) are acceptable for use. The results from AASHTO Product Evaluation & Audit Solutions (formerly NTPEP) testing, when tested in accordance with AASHTO TP 102, shall conform to the requirements shown in the table below:

| RELEASE AGENT TEST | REQUIREMENT |
| --- | --- |
| Asphalt Stripping Test Diluted Non-Diluted (Full Strength) | No Stripping No Stripping |
| Asphalt Performance Test | Less than or equal to 10.0% after the third cycle |

Release agents which degrade, dissolve, or in any way damage the bituminous material shall not be used.  Diesel fuel shall not be used as a release agent.

Longitudinal joints of each course shall be staggered a minimum of 1 foot with relation to the longitudinal joint of any immediate underlying course.

When surfacing courses are placed on 10 foot or wider shoulders which are to receive rumble strips, the contractor shall place any longitudinal joints approximately 1 foot away from the travel lane side of the rumble strip.

Longitudinal joints shall be located within 1 foot of the center of a lane or within 1 foot of the centerline between two adjacent lanes.  Joints shall be formed by a slope shoe or hot-lapped, and shall result in an even, uniform surface.

Before a surface course is placed in contact with a cold transverse construction joint, the cold existing asphaltic concrete shall be trimmed to a vertical face by cutting the existing asphaltic concrete back for its full depth of the lift and exposing a fresh face.  After placement and finishing of the new asphaltic concrete, both sides of the joint shall be dense and the joint shall be well sealed.  The surface in the area of the joint shall conform to the requirements hereinafter specified for surface tolerances when tested with the straightedge placed across the joint.

All locations where plate samples are taken from the roadway shall be immediately repaired by the contractor utilizing hot asphaltic concrete.  All holes where cores are taken shall be repaired within 48 hours after coring using a material approved by the Engineer.  All holes shall be in a dry condition prior to repair.  The patching material shall be thoroughly compacted in the holes by the contractor.

The handling of asphaltic concrete shall at all times be such as to minimize segregation.  Any asphaltic concrete which displays segregation shall be removed and replaced.

Before asphaltic concrete is placed, the surface to be paved shall be cleaned of all objectionable material and tacked in accordance with the requirements of Section 404 of the specifications.  The cleaning of the surface, the tacking of the surface, and the type of bituminous material used shall be acceptable to the Engineer.  The amount of bituminous material used shall be as directed by the Engineer.

A light coat of bituminous material shall be applied to edges or vertical surfaces against which asphaltic concrete is to be placed.

The contractor shall schedule its paving operations to minimize exposed longitudinal edges.  Unless otherwise approved by the Engineer, the contractor shall limit the placement of asphaltic concrete courses, in advance of adjacent courses, to one shift of asphaltic concrete production.  The contractor shall schedule its paving operations in such a manner to eliminate exposed longitudinal edges over weekends or holidays.

The moisture content of the asphaltic concrete immediately behind the paver shall not exceed 0.5 percent.  The moisture content will be determined in accordance with AASHTO T 329.

## 416-7	Acceptance:

### 416-7.01	General:

In addition to the random acceptance samples taken from each lot, the Engineer may sample and reject material which appears to be defective.  Such rejected material shall not be used in the work.  The results of tests run on rejected material will not be included with the lot acceptance tests.

Acceptance will be on the basis of the following:

- Sand equivalent;

Fractured coarse aggregate particles;

Uncompacted void content (for Special Mix);

Material spread;

Gradation;

Asphalt cement content;

Effective voids;

Stability;

Compaction; and

Smoothness

### 416-7.02	Sand Equivalent and Fractured Coarse Aggregate Particles of Mineral Aggregate:

During asphaltic concrete production, the Engineer shall obtain and test samples of material for the determination of the sand equivalent and fractured coarse aggregate particles.  When RAP is used in the mixture, the sand equivalent shall be determined on the composite of virgin aggregates only.  Samples shall be obtained from the cold feed belt prior to the addition of mineral admixture, or from the stockpiles when sampling from the cold feed belt is not possible.

When RAP is used in the mixture, the material for determining the fractured coarse aggregate particles shall come from an asphaltic concrete sample taken and tested in accordance with AASHTO T 308, as specified in Subsection 416-7.04(A).  However, if the Engineer determines that excessive breakdown of the aggregate has occurred due to the use of the ignition furnace, the fractured coarse aggregate particles testing shall be performed on the combination of RAP aggregate, as obtained in accordance with AASHTO T 308, and virgin mineral aggregate.

Virgin mineral aggregate will be acceptable for sand equivalent if it meets the minimum requirements specified in Subsection 416-3.01 of the specifications.

The fractured coarse aggregate particles shall meet the minimum requirements specified in Subsection 416-3.01 of the specifications.

If the mineral aggregate fails to meet the requirements specified herein, operations shall cease and the contractor shall have the option of submitting a revised mix design conforming to the requirements of Subsection 416-4 of the specifications or correcting deficiencies in the aggregate stockpiles.

### 416-7.03	Material Spread:

A spread lot shall be considered to be one-half shift of production.  Lots encompassing more than one project shall be separated in accordance with Subsection 416-9(D) of the specifications.

The contractor shall record information pertaining to each spread lot on forms provided by the Engineer.  Information shall include the project number, date and period of time that each spread lot was placed, the spread lot number, beginning and ending station, the plans thickness, and tons placed in each lot.  Completed spread lot forms shall be signed by the contractor and given to the Engineer at the end of each shift.

The Engineer will calculate the quantity required in each spread lot using the mix design bulk density unless a request is made by the contractor to use a production bulk density.  If a request is made to use production bulk density, the first three non-rejected lots following the test lot will be used to determine the average production bulk density.  All lots placed prior to establishing the average production bulk density shall be calculated using the mix design bulk density.  For each new mix design used on the project, a new production bulk density may be requested by the contractor.  In addition, if conditions warrant during asphalt production, the contractor may request establishment of a new average production bulk density.  All requests to use a production bulk density shall be made in writing and approved by the Engineer prior to use.  The same procedure will be used for determining average production bulk density in all cases.  Changes to the bulk density for calculating spread quantities will not be retroactive.

The calculated quantity required in each spread lot will be compared to the actual quantity placed.  A lot will be considered to be acceptable, with a zero pay factor, if the actual quantity placed varies by no more than -2.0 to +5.0 percent from the required quantity.

If the quantity in a lot is found to vary from the required quantity by -2.1 to -12.0 percent, the appropriate pay factor will be determined in accordance with Table 416-1.  This pay factor will be utilized in determining the pay adjustment as outlined in Subsection 416-9 of the specifications.

### 416-7.04	Gradation, Asphalt Cement Content, Effective Voids and Stability:

- General:

A mixture properties lot shall be considered to be one shift's production.  In the event a shift’s production is less than 1,200 tons, multiple shifts may be combined to form a lot.  When a lot consists of production from more than one shift, the following conditions apply:  at least one sample shall be taken each shift, at least one sample shall be taken every 500 tons, and no mix design or target value changes shall be made within the lot.  If changes are made in the mix design or target values, new lots will be established.

Four samples of the asphaltic concrete shall be taken for each lot by the contractor, under the observation of the Engineer, at random locations designated by the Engineer.  Samples will be taken in accordance with the requirements of AASHTO R 97 Plate Method and delivered to the Engineer immediately after being taken.  The minimum weight of the sample shall be 75 pounds.  The Engineer will split the sample and save one-half for 15 days after written notification to the contractor of test results for that lot has been made.  The material will be tested by the Engineer for the following properties:

| Test Property | Test Method |
| --- | --- |
| Asphalt Cement Content | AASHTO T 308 (for both Non-RAP and RAP mixes) (See Notes 1 and 2 below) |
| Gradation |  |
| Marshall Density and Stability | AASHTO R 68, T 245 |
| Maximum Theoretical Density | AASHTO T 209 |
| Effective Voids | AASHTO T 269 |
| Notes: A new calibration of the ignition furnace shall be performed for each mix design, and at any other time the Engineer directs. Ignition furnace results will be corrected for asphalt cement content in accordance with Subsection 416-7.04(B) as required. |  |

Acceptance testing results will be furnished to the contractor within four working days of receipt of samples by the Engineer.

A mixture properties lot placed with an average stability below 2,500 pounds for base mixes, or 1,750 pounds for 1/2 inch or 3/4 inch mixes shall be rejected, and shall be subject to an engineering analysis of anticipated performance in accordance with Subsection 416-9(E) of the specifications.  Production shall cease until the contractor proposes a corrective action the Engineer finds acceptable.  If the Engineer rejects the proposed corrective action, the contractor shall submit a revised mix design.

The target values for Gradation, Asphalt Cement Content, and Effective Voids are given in the contractor’s mix design.  The Upper Limits (UL) and Lower Limits (LL) of acceptable production of each of the measured characteristics are as follows:

| Measured Characteristics | LL (Note 1) | UL (Note 1) |
| --- | --- | --- |
| Gradation (Sieve size): 3/8 inch | TV - 8.0 | TV + 8.0 |
| No. 8 No. 40 No. 200 | TV - 8.0 TV - 5.0 TV - 2.0 | TV + 8.0 TV + 5.0 TV + 2.0 |
| Asphalt Cement Content | TV - 0.50 | TV + 0.50 |
| Effective Voids | TV - 2.0 | TV + 2.0 |
| Notes: - The limits are used in the statistical calculations for Quality Index. Acceptance is controlled by the variability of the produced material and every effort should be made to strive for the applicable target value (TV). |  |  |

The Engineer will determine the PT for each measured characteristic in accordance with Subsection 416-9(H) of the specifications, and utilizing Table 416-1 will determine the pay factor for each measured characteristic.

In the event the contractor elects to question the mixture property test results, the contractor may request referee testing in accordance with Subsection 416-9(I) of the specifications.

Ignition Furnace Correction:

Ignition furnace testing results shall be corrected in accordance with ADOT Materials Practice and Procedure Directive No. 20, “Guidance on the Use of Reclaimed Asphalt Pavement (RAP) in Asphaltic Concrete”.

### 416-7.05	Compaction:

- All Courses Regardless of Thickness:

General Requirements:

Asphaltic concrete shall be placed only when the temperature of the surface on which the asphaltic concrete is to be placed is at least 65 degrees F and the ambient temperature at the beginning of placement is at least 65 degrees F and rising.  The placement shall be stopped when the ambient temperature is 70 degrees F or less and falling.

Asphaltic concrete immediately behind the laydown machine shall be a minimum of 275 degrees F.

All edges shall be rolled with a pneumatic tired compactor, or other methods approved by the Engineer, while the mixture is still hot.

Equipment:

Compacting and smoothing shall be accomplished by the use of self-propelled equipment.  Compactors shall be pneumatic-tired and/or steel wheel.

Compactors shall be operated in accordance with the manufacturer's recommendations.  Compactors shall be designed and properly maintained so that they are capable of accomplishing the required compaction.

Steel wheel compactors shall weigh not less than 8 tons.

Pneumatic-tired compactors shall be the oscillating type with at least seven pneumatic tires of equal size and diameter.  Wobble-wheel compactors will not be permitted.  The tires shall be spaced so that the gaps between adjacent tires will be covered by the following tires.  The tires shall be capable of being inflated to 90 pounds per square inch and maintained so that the air pressure will not vary more than 5 pounds per square inch from the designated pressure.  Pneumatic-tired compactors shall be constructed so that the total weight of the compactor will be varied to produce an operating weight per tire of not less than 5,000 pounds.  Pneumatic-tired compactors shall be equipped with skirt-type devices mounted around the tires so that the temperature of the tires will be maintained during the compaction process.

Rolling Method Procedure:

Compaction shall consist of an established sequence of coverage using specified types of compactors.  A pass shall be defined as one movement of a compactor in either direction.  Coverage shall be the number of passes as are necessary to cover the entire width being paved.

The rolling sequence, the type of compactor to be used, and the number of coverages required shall be as follows:

| Rolling Sequence | Type of Compactor |  | No. of Coverages |  |
| --- | --- | --- | --- | --- |
|  | Option No. 1 | Option No. 2 | Option No.1 | Option No. 2 |
| Initial | Static Steel | Vibrating Steel | 1 | 1 |
| Intermediate | Pneumatic Tired | Vibrating Steel | 4 | 2-4* |
| Finish | Static Steel | Static Steel | 1-3 | 1-3 |
| Note: * Based on the roller pattern which exhibits the best performance. |  |  |  |  |

The Engineer shall select the option for compaction and, when pneumatic-tired compactors are used, will designate the tire pressure.

One pneumatic-tired roller shall be furnished for each 300 tons of asphaltic concrete per hour.

Steel wheel compactors shall not be used in the vibratory mode for courses of 1 inch or less in thickness nor when the temperature of the asphaltic concrete falls below 180 degrees F.

Initial and intermediate compaction shall be accomplished before the temperature of the asphaltic concrete falls below 200 degrees F.

Compaction will be deemed to be acceptable on the condition that the asphaltic concrete is compacted using the type of compactors specified, ballasted and operated as specified, and with the number of coverages of the compactors as specified.

### 416-7.06	Smoothness and Surface Tolerances:

Asphaltic concrete shall be compacted as required, smooth and true to the required lines, grades, and dimensions.

The Special Provisions may require the smoothness of the final pavement surface to be tested in accordance with Subsection 109.13 of the specifications.

Regardless of whether testing in accordance with Subsection 109.13 of the specifications is specified or not, the following requirements shall be met:

- The surface of any lift of asphaltic concrete placed under this section of the specifications, shall be tested and shall not vary by more than 1/4 inch from the lower edge of a 10-foot straightedge when it is placed in the longitudinal direction (including across transverse joints), and when it is placed in the transverse direction across longitudinal joints; and

All deviations exceeding the specified tolerances above shall be corrected by the contractor, to the satisfaction of the Engineer.

## 416-8	Method of Measurement:

Asphaltic concrete will be measured by the ton for the asphaltic concrete actually used, which will include the weight of mineral aggregate, asphalt cement, and mineral admixture.  Measurement will include any quantity used in construction of intersections, turnouts, or other miscellaneous items or surfaces.

No separate measurement or payment will be made for mineral admixture, the cost being considered as included in the cost of the asphaltic concrete.

## 416-9	Basis of Payment:

The accepted quantities of asphaltic concrete, measured as provided above, will be paid for at the contract unit price adjusted by the appropriate pay factors as hereinafter provided.

For the purpose of determining acceptability and appropriate pay factors, each unit of asphaltic concrete will be included in two separate lots: a “spread lot” and a “mixture properties lot.”  The total unit price for any unit of accepted asphaltic concrete will be the contract unit price, adjusted by the applicable spread lot pay factor and mixture properties lot pay factor.

The contractor may request to place the first lot of each mix type as a test strip.  Requests to place a test strip shall be made in writing and acknowledged by the Engineer prior to start of production.  A test strip shall be limited to 1,000 tons and may only be placed on shoulders, ramps, cross roads, or other areas approved by the Engineer.  A test strip shall be excluded from the mixture properties lot pay factor and the compaction lot pay factor; however, all other provisions of Subsection 416-9 of the specifications shall still apply to such areas.

The Engineer may exclude asphaltic concrete from the spread lot and from the spread lot pay factor calculations if the Engineer determines that the proposed use of the material or the existing surface conditions are not conducive to the use of spread lots.

The Engineer may exclude certain locations from the mixture properties lot and from the random sampling used in determining the mixture properties lot pay factor should the Engineer determine that the location of the work precludes normal construction operations.

- Spread Lot Pay Factor:

The spread lot pay factor will be determined in accordance with Subsection 416-7.03 of the specifications.  If the quantity in a spread lot is found to vary by more than +5.0 percent from the required quantity, no payment will be made for the material which exceeds +5.0 percent, including asphalt cement and mineral admixture.  If the quantity is found to vary by more than -12.0 percent from the required quantity, the spread lot will be rejected.

Mixture Properties Lot Pay Factor:

The mixture properties lot pay factor shall be determined in accordance with the following procedure:

The individual PT values and pay factors for Gradation, Asphalt Cement Content, and Effective Voids shall be determined as set forth in Subsection 416-7.04 of the specifications.

A single pay factor shall be determined for Gradation and Asphalt Cement Content.  That pay factor shall be the lowest pay factor for the individual measured characteristics for Gradation and Asphalt Cement Content.

If no individual PT value in (1) above is less than 50, the mixture properties lot pay factor shall be the sum of the pay factor determined in (2) above and the Effective Voids pay factor.  The negative pay factor for mixture properties shall not exceed $3.00 per ton.  If any individual PT value is less than 50, the lot is in reject and the provisions in Subsection 416-9(E) of the specifications shall apply.

Blank:

Determination of Lot Pay Factors on Contracts Involving Multiple Projects:

When more than one project is included in a single contract, placement during a shift or half shift of production may encompass more than one project.  In such case, the applicable spread lot pay factor and mixture properties lot pay factor for each project shall be determined as follows:

Spread lot pay factors will be determined separately for each project utilizing the procedure set forth in Subsection 416-7.03.

The individual PT values and pay factors for Gradation, Asphalt Cement Content, and Effective Voids will be determined from the results of the random samples taken and tested in accordance with Subsection 416-7.04 of the specifications, regardless of which project(s) the samples fall within.

The mixture properties lot pay factor shall be determined separately for each project in accordance with Subsection 416-9(B) of the specifications, utilizing the individual pay factors determined in (2) above.

Acceptability:

Asphaltic concrete included in any mixture properties lot possessing an individual PT value lower than 50 for Gradation, Asphalt Cement Content, or Effective Voids will be rejected.

Within 25 days, or as agreed upon by the Engineer, after receiving notice that a spread lot or mixture properties lot of asphaltic concrete has been rejected by the Engineer, the contractor may submit a written proposal to accept the material in place at the applicable maximum negative pay factor(s).  Maximum negative pay factors are defined as a minus $1.00 per ton for spread lots, minus $3.00 per ton for mixture properties lots in reject for gradation only, minus $5.00 per ton for mixture properties lots in reject for Asphalt Cement Content and/or Effective Voids only, and minus $5.00 per ton for mixture properties lots in reject for Asphalt Cement Content and/or Effective Voids and also Gradation.  In addition, for any mixture properties lot that is in reject due to Asphalt Cement Content but allowed to remain in place, payment shall not be made for asphalt cement quantities in excess of the upper limit (UL) as determined in Subsection 416-7.04(A) of the specifications.

The proposal shall contain an engineering analysis of the anticipated performance (i.e., reduction in serviceability in years) of the asphaltic concrete if left in place.  The engineering analysis shall also detail the potential root cause of the problem, any proposed corrective action, and the anticipated effect of such corrective action on the performance.  The engineering analysis shall only include acceptance or referee test results, as applicable to the standard specifications. The engineering analysis shall include the expected additional cost to the Department (over original performance life) to maintain the pavement at an acceptable condition. The engineering analysis shall include supporting information such as pictures of the area, control charts, plant and field records, etc. The engineering analysis shall be performed by an independent professional engineer experienced in asphaltic concrete testing and the development of asphaltic concrete mix designs.  If a rejected mixture properties lot is submitted for referee testing by the contractor, the 25 days allowed to prepare an engineering analysis will begin upon notification of referee test results.

The contractor may submit a written proposal without an engineering analysis for Engineer’s evaluation and approval, that a mixture properties lot with a PT value lower than 50 on Gradation and/or Asphalt Cement Content be allowed to remain in place if the application of a Self-Directed Target Change as outlined in Subsection 416-4 of the specifications would bring the PT value to 50 or greater. This written request shall also include the proposed revised PT calculations. Upon Engineer’s verification and approval of the request, the material shall remain in place at the maximum negative pay factor(s) specified in this Subsection for the mixture properties lot in reject.

Within three working days, the Engineer will determine whether or not to accept the contractor's proposal.  If the proposal is not accepted, the asphaltic concrete shall be removed at no additional cost to the Department and replaced with asphaltic concrete meeting the requirements of these specifications.  If the proposal is accepted, the asphaltic concrete shall remain in place at the applicable maximum negative pay factor(s), and any necessary corrective action shall be performed at no additional cost to the Department.

The Department reserves the right to suspend the work should any of the following conditions occur:

The occurrence of two or more rejected lots within any 10 consecutive production lots;

The occurrence of three consecutive negative mixture properties lot pay factors.

The occurrence of five or more pay factors that are negative for a mixture properties lot within any 10 consecutive production lots.

If the Department elects to suspend the work for any of these conditions, the contractor shall either submit a revised mix design in accordance with Subsection 416-4 of the specifications, or submit for the Engineer's approval a written engineering analysis.  The engineering analysis shall detail the course of action necessary to correct deficiencies in the contractor’s present production methods such that further production can be accomplished without excessive amounts of asphaltic concrete in penalty or rejection.  If approved by the Engineer, the revised mix design, or the course of action proposed in the engineering analysis, shall be implemented, and the work may continue.  Costs or delays due to the provisions of this subsection are not compensable.

Asphalt Cement:

No separate measurement or payment will be made for asphalt cement (bituminous material), the cost being considered as included in the cost of the asphaltic concrete.

A reduction in payment to the contractor for asphaltic concrete will be made for quantities of asphalt cement (bituminous material) that do not meet the requirements of Section 1005 as determined by corresponding test results.  Adjustments in payment will be made in accordance with the requirements of Section 1005 of the specifications.

Smoothness:

When required in the Special Provisions, payment for smoothness shall be made in accordance with the requirements of Subsection 109.13 of the specifications.

Statistical Acceptance:

The “Total Percentage of Lot within UL and LL (PT)” shall be determined in accordance with Subsection 109.11 of the specifications.

Pay Factors (PF) shall be determined by entering Table 416-1 with PT.

| TABLE 416-1 PAY FACTORS |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Material Spread |  |  | Mixture Properties |  |  |
| Negative Variance (%) |  | Pay Factor (Dollars per Ton) | PT | Pay Factors (Dollars per Ton) |  |
|  |  |  |  | Gradation & Asphalt Cement Content | Effective Voids |
| 2.1 - 3.0 | - 0.10 | 100 | 0.00 | + 2.00 |
| 3.1 - 4.0 |  | - 0.20 | 95 - 99 | 0.00 | + 1.00 |
| 4.1 - 5.0 |  | - 0.30 | 90 - 94 | 0.00 | 0.00 |
| 5.1 - 6.0 |  | - 0.40 | 85 - 89 | 0.00 | - 0.25 |
| 6.1 - 7.0 |  | - 0.50 | 80 - 84 | - 0.25 | - 0.50 |
| 7.1 - 8.0 |  | - 0.60 | 75 - 79 | - 0.50 | - 0.75 |
| 8.1 - 9.0 |  | - 0.70 | 70 - 74 | - 0.75 | - 1.00 |
| 9.1 - 10.0 |  | - 0.80 | 65 - 69 | - 1.00 | - 1.25 |
| 10.1 - 11.0 |  | - 0.90 | 60 - 64 | - 1.50 | - 1.50 |
| 11.1 - 12.0 |  | - 1.00 | 55 - 59 | - 2.00 | - 2.00 |
| More than 12.0 |  | Reject | 50 - 54 | - 2.50 | - 2.50 |
|  |  |  | Less than 50 | Reject – See Subsection 416-9 (E) |  |
| See Subsections 416-9 (A) and (E) |  |  |  |  |  |

Mixture Properties Lot Referee Testing:

Within 15 days after written notification to the contractor of test results for a particular mixture properties lot, the contractor may make a written request for referee testing.  The referee testing shall be performed by an independent approved laboratory designated by the Department.  The testing of the samples will be performed by the independent testing laboratory without knowledge of the specific project conditions such as the identity of the contractor or mix design laboratory, the test results by the Department, or the mix design targets for Gradation and Effective Voids.  The asphaltic concrete samples previously saved will be tested for the following properties:

| Test Property | Test Method |
| --- | --- |
| Asphalt Cement Content | AASHTO T 308 (for both Non-RAP and RAP mixes) |
| Gradation |  |
| Marshall Density and Stability | AASHTO R 68, T 245 |
| Maximum Theoretical Density | AASHTO T 209 |
| Effective Voids | AASHTO T 269 |

The results of the referee testing will be binding on both the contractor and the Department.

Using the referee testing results, the Engineer will determine new PT’s for all characteristics, with the exception of Asphalt Cement Content if a correction to the ignition furnace value was made as specified in Subsection 416-7.04(B) of the specifications, or if RAP is used in the mixture.

When referee testing is performed on a mixture properties lot, the referee test result for the average maximum theoretical density will be used to determine a new PT for compaction.

The Department will pay for the referee testing; however, if the combined pay factor of the lot (mixture properties plus compaction) does not improve or is reduced, or if either the mixture properties lot or compaction lot remains in reject or is placed in reject, payment to the contractor for asphaltic concrete shall be reduced by the amount of the cost of the referee testing for the mixture properties of that particular lot.