(610PNT, 8/21/25)

SECTION 610 	PAINTING:

610-3.02 (A)(2)		Steam Cleaning: the first paragraph of the Standard Specifications is revised to read:

All dirt, grease, loose chalky paint, and other foreign material which has accumulated on previously painted surfaces shall be removed with a steam cleaning apparatus prior to all other phases of cleaning. It is not intended that sound paint be removed by this process. After steam cleaning, any paint which has become loose, curled, lifted, or loses its bond to the preceding coat or coats shall be removed to sound paint or metal surface by the contractor a t no additional cost to the Department.

610-3.02 (A)(3)  	Hand Cleaning: of the Standard Specification is revised to read:

Manual or powered wire brushes, hand scraping tools, power grinders, or sandpaper shall be used to remove all dirt, loose rust, mill scale, and paint which is not firmly bonded to the surfaces.

610-3.05 (A)(1)	General: the second paragraph of the Standard Specifications is revised to read:

All paints used shall be appropriately chosen from among the types described in Subsection 1002-2 of the specifications and shall conform to the requirements given therein.

610-3.05 (B)      Concrete Surfaces: the first paragraph of the Standard Specifications is revised to read:

When painting is specified on the plans or in the special provisions, paint conforming to the

requirements of Subsection 1002-2.03 of the specifications, shall be applied to the exposed concrete surfaces tabulated below, except that sidewalks, appurtenant curbs, downdrains, and bridge deck surfaces shall be excluded.