(708 PTVCT, 07/17/25)

SECTION 708	WATERBORNE PAVEMENT MARKINGS:

708-2.01(D)	Quantitative Requirements of Mixed Paints: the viscosity row of the Table 708-1 of the Standard Specifications is revised to read:

| Table 708-1 |  |  |
| --- | --- | --- |
|  | White | Yellow |
| Viscosity: Krebs Units at 77 ± 1˚ F, ASTM D562 | 70 - 95 | 70 - 95 |