*	         USE ON ALL PROJECTS INVOLVING BITUMINOUS MATERIALS		     *

(1005PG, 12/17/20)

SECTION 1005	BITUMINOUS MATERIALS:

1005-3		Bituminous Material Requirements:

1005-3.01		Asphalt Cement: of the Standard Specifications is revised to read:

Asphalt cement shall be a performance grade (PG) asphalt binder conforming to the requirements of AASHTO M 320.  Air blown/oxidized asphalt and recycled engine oil bottom (REOB) will not be accepted.  Polyphosphoric acid (PPA) modification shall be limited to a maximum of 0.50 percent.  The pressure aging temperature for all binders, including Terminal Blend rubberized binder and Polymer modified asphalt binder shall be as specified below:

| PG Asphalt Binder | Pressure Aging Temperature |
| --- | --- |
| PG 70-XX and above | 110 ºC |
| PG 64-XX and below | 100 ºC |

If Terminal Blend rubberized binder (XX-XXTR+) is used, it shall conform to the requirements of Table 1005-1 and 1005-1a.

If Polymer modified asphalt binder (XX-XXPM) is used, it shall conform to the requirements of Table 1005-1 and 1005-1b.

If, during asphaltic concrete production, it is determined by testing that asphalt cement fails to meet the requirements for the specified grade, the asphaltic concrete represented by the corresponding test results shall be evaluated for acceptance.  Should the asphaltic concrete be allowed to remain in place, the contract unit price for asphalt cement will be adjusted by the percentage shown in Table 1005-1.  Should the asphalt cement be in reject status, the contractor may, within 15 days of receiving notice of the reject status, supply an engineering analysis of the expected performance of the asphaltic concrete in which the asphalt cement is incorporated.  The engineering analysis shall detail any proposed corrective action and the anticipated effect of such corrective action on the performance.  Within three working days, the Engineer will determine whether or not to accept the contractor’s proposal.  If the proposal is rejected, the asphaltic concrete shall be removed and replaced with asphaltic concrete meeting the requirements of the specifications at no additional expense to the Department.  If the contractor’s proposal is accepted, the asphaltic concrete shall remain in place at the applicable percent of contract unit price allowed, and any necessary corrective action shall be performed at no additional cost to the Department.

1005-3.03		Emulsified Asphalt: the fourth paragraph of the Standard Specifications is revised to read:

Emulsified asphalts shall be homogeneous.  If emulsified asphalt has separated, it shall be thoroughly mixed to insure homogeneity. If emulsified asphalt has separated due to freezing, it shall not be used.  Emulsified asphalt shall not be used after 30 days from production.

1005-3.04		Emulsified Asphalt (Special Type): of the Standard Specifications is revised to read:

Emulsified asphalt (special type) shall consist of Type SS-1 or CSS-1 diluted with water to provide an asphalt content not less than 26 percent.  The water used shall be potable.  Potable water obtained from public utility distribution lines will be acceptable.  The water used shall be free of injurious amounts of oil, acid, alkali, clay, vegetable matter, silt, or other harmful matter.  The material shall not be diluted in the field.

1005-3.07		Other Requirements: the tables 1005-1a and 1005-1b of the Standard Specifications are revised to read:

| TABLE 1005-1a Terminal Blend rubberized binder (XX-XXTR+) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Test Property | Test Method | Requirement | Test Result | Percent of Contract Unit Price Allowed |
| Solubility, %, minimum | ASTM D7553 or ASTM 2042 | 98 | ----- | ----- |
| Elastic Recovery, @ 10 ºC, %, minimum | AASHTO T 301 | 75 | 75 70 - 74 < 70 | 100 80 65 (1) |
| - Reject Status: The pay adjustment applies if allowed to remain in place. |  |  |  |  |
| Notes: In case of dispute, ASTM D2042 shall be used to determine the Solubility. The asphalt binder shall contain a minimum of 8 percent crumb rubber and a minimum of 3 percent SBS (styrene-butadiene-styrene) polymer. The crumb rubber shall be derived from processing whole scrap tires or shredded tire materials. The tires from which the crumb rubber is produced shall be taken from automobiles, trucks, or other equipment owned and operated in the United States. The processing shall not produce, as a waste product, casings or other round tire material that can retain moisture when stored or disposed of above ground. Modified binders shall be blended at the source of supply and delivered as a homogenous mixture to the job site. Modified Binders stored at the asphalt concrete mixing plant for more than two weeks or beyond the supplier recommended shelf life, whichever is less, shall be sampled and tested. |  |  |  |  |

| TABLE 1005-1b Polymer Modified Asphalt Binder (XX-XXPM) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Test Property | Test Method | Requirement | Test Result | Percent of Contract Unit Price Allowed |
| Solubility, %, minimum | ASTM D7553 or ASTM D2042 | 98 | ----- | ------- |
| Elastic Recovery @ 10oC, %, minimum | AASHTO T 301 | 75 | ≥ 75 70 - 74 < 70 | 100 80 65 (1) |
| (1) Reject Status: The pay adjustment applies if allowed to remain in place. |  |  |  |  |
| Notes: In case of dispute, ASTM D2042 shall be used to determine the Solubility. Asphalt binder shall contain a minimum of 3 percent SBS (styrene-butadiene-styrene) polymer. Modified binders shall be blended at the source of supply and delivered as a homogenous mixture to the job site. Modified Binders stored at the asphalt concrete mixing plant for more than two weeks or beyond the supplier recommended shelf life, whichever is less, shall be sampled and tested. |  |  |  |  |

1005-3.07		Other Requirements: the table 1005-1c of the Standard Specifications is hereby deleted.

1005-3.07		Other Requirements: the table 1005-3 of the Standard Specifications is revised to read:

| TABLE 1005-3 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| EMULSIFIED ASPHALTS |  |  |  |  |  |  |  |
| Tests On Emulsion | Test Method | Requirement |  |  |  |  |  |
|  |  | RS-1 | CRS-1 | RS-2 | CRS-2 | SS-1 | CSS-1 |
| Viscosity: Saybolt Furol, seconds, range 77 F 122 F | AASHTO T 59 | 20-100 | 20-100 | 50-400 | 50-400 | 20-100 | 20-100 |
| Settlement: 5 days, %, maximum | AASHTO T 59 | 5 | 5 | 5 | 5 | 5 | 5 |
| Sieve: Retained on No. 20, %, | AASHTO T 59 (1) | 0.10 | 0.10 | 0.10 |  | 0.10 | 0.10 |
| maximum |  |  |  |  |  |  |  |
| Particle Charge | AASHTOT 59 |  | Pos. |  | Pos. |  | Pos. |
|  |  |  |  |  |  |  | (2) |
| Demulsiability: 35 mL, 0.02 N calcium chloride %, minimum | AASHTO T 59 | 60 |  | 60 |  |  |  |
| Classification: Uncoated particles, %, minimum | Arizona Test Method 502 |  |  |  | 55 |  |  |
| Residue: (3) |  | 55 | 60 | 63 | 65 | 57 | 57 |
| Residue, %, |  |  |  |  |  |  |  |
| minimum (4) |  |  |  |  |  |  |  |
| Notes: |  |  |  |  |  |  |  |
| - Distilled water shall be used. Two percent sodium oleate solution will not be accepted. |  |  |  |  |  |  |  |
| - If the Particle Charge Test result is inconclusive, material having a maximum PH value of 6.7 will be acceptable. |  |  |  |  |  |  |  |
| - Residue will be obtained in accordance with the requirements of Arizona Test Method 504 and shall conform to all the requirements of AASHTO M 320 for PG 64-16, except that for CRS-2 the dynamic shear (G*/Sin ) on the original residue shall be a minimum of 1.00 kPa and a maximum of 1.50 kPa. |  |  |  |  |  |  |  |
| - Residue by evaporation may be determined in accordance with the requirements of Arizona Test Method 512; however, in case of dispute, AASHTO T 59 will be used. |  |  |  |  |  |  |  |

1005-3.07		Other Requirements: the note (2) of Table 1005-3a of the Standard Specifications is revised to read:

- Testing shall be performed on residue by distillation. Testing on residue by oven evaporation will not be accepted.

1005-3.07		Other Requirements: the table 1005-5 of the Standard Specifications is revised to read:

| TABLE 1005-5 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| EMULSIFIED RECYCLING AGENTS |  |  |  |  |  |
| Tests on Emulsified Recycling Agent | Test Method | Requirement |  |  |  |
|  |  | ERA-1 | ERA-5 | ERA-25 | ERA-75 |
| Viscosity: Saybolt Furol, 77 F, seconds range | AASHTO T 59 | 15 - 40 | 15 - 100 | 15 - 100 | 15 - 100 |
| Miscibility | AASHTO T 59 | Passes | Passes | Passes | Passes |
| Sieve Test: %, maximum | AASHTO T 59 (1) | 0.10 | 0.10 | 0.10 | 0.10 |
| Particle Charge | AASHTO T 59 | Positive | Positive | Positive | Positive |
| Residue: (2) Residue, %, minimum | (3) | 60 | 60 | 60 | 60 |
| Notes: (1) Distilled water shall be used. Two percent sodium oleate solution will not be accepted. (2) Residue will be obtained in accordance with the requirements of Arizona Test Method 504 and shall conform to the requirements specified in Table 1005-4. |  |  |  |  |  |
| (3) Residue by evaporation may be determined in accordance with the requirements of Arizona Test Method 512; however, in case of dispute, AASHTO T 59 will be used. |  |  |  |  |  |

1005-3.07		Other Requirements: the Paving Asphalt row of the table 1005-6 of the Standard Specifications is modified to add:

| TABLE 1005-6 |  |  |  |  |
| --- | --- | --- | --- | --- |
| OTHER REQUIREMENTS |  |  |  |  |
| Grade of Asphalt Specification Designation | Range of Temperatures for Application by Spraying, F (Not applicable for Plant Mixing) | Range of Aggregate Temperatures for Plant Mixing, F |  | Basis of Conversion, Average Gallons Per Ton at 60 F |
| Paving Asphalt | 275 - 400 | ------ |  |  |
| PG 76-22 PM 229 PG 70-22 PM 230 PG 64-28 PM |  |  |  | 231 232 233 |