(1006PCC, 01/20/22)

SECTION 1006	PORTLAND CEMENT CONCRETE:

1006-2.01(A)	General: of the Standard Specifications is revised to read:

Cementitious material is defined as an inorganic material or a mixture of inorganic materials that sets and develops strength by chemical reaction with water by formation of hydrates and is capable of doing so under water.  In this specification, cementitious materials are defined as hydraulic cement (Portland cement, Portland-pozzolan cement or Portland-limestone cement) and supplementary cementitious materials (fly ash, natural pozzolan, or silica fume).

1006-2.01(B)	Hydraulic Cement: the first paragraph of the Standard Specifications is revised to read:

Hydraulic cement shall consist of Portland cement, Portland-pozzolan cement or Portland-limestone cement.

1006-2.01(B)	Hydraulic Cement: of the Standard Specifications is modified to add:

Portland-limestone cement shall conform to the requirements of ASTM C595 for blended hydraulic cement with moderate sulfate resistance, Type IL (MS).

1006-2.01(C)(2)	Flyash and Natural Pozzolan: of the Standard Specifications is revised to read:

Fly ash and natural pozzolan shall conform to the requirements of ASTM C618 for Class C, F, or N.

TABLE 1006-5	Design Criteria: the column heading of the third column of the Standard Specifications is revised to read:

|  |  | Cementitious Material Content: Lbs. per Cu Yd. Minimum - Maximum |  |  |
| --- | --- | --- | --- | --- |

1006-3.02(C)	Mix Design Submittal Requirements: the items (16) and (18) of the Standard Specifications are revised to read:

- Volume of each material measured to the nearest hundredth of a cubic foot;

- Total volume measured to the nearest hundredth of a cubic foot;