*		USE WHEN EITHER CLASS S OR CLASS P CONCRETE		*

*			         QUANTITY IS 300 CUBIC YARDS OR MORE			*

*	USE IN CONJUNCTION WITH THE FOLLOWING:					*

*		BID ITEM:						9240170				*

*		STORED SPECIFICATION:			924CQC				*

(1006QCPC, 07/12/05)

SECTION 1006	PORTLAND CEMENT CONCRETE:

1006-4.01		General Requirements:  of the Standard Specifications is modified to add:

1006-4.01(A)	Contractor Quality Control:

The contractor shall perform the quality control measures described in Subsection 
106.04(C).  At the weekly meeting, the contractor shall be prepared to explain and discuss how the following processes will be employed.

(a)	Aggregate Production, including crusher methods, pit extraction, and washing.

(b)	Stockpile Management, including stacking methods, separation technique, plant feed technique, stockpile pad thickness, and segregation prevention.

(c)	Mixing and Transport, including mixing time and revolutions, water and concrete temperature, integrity of mixing equipment, sight glass for water, slump meters, batch ticket, and travel time.

(d)	Proportioning, including scale calibration, water added, water meter moisture correction, and bin loading.

The contractor shall obtain samples and perform the tests specified in the following table:

| # CONTRACTOR QUALITY CONTROL TESTING REQUIREMENTS |  |  |  |
| --- | --- | --- | --- |
| TYPE OF TEST | TEST METHOD | SAMPLING POINT | MINIMUM TESTING FREQUENCY |
| Fine Aggregate for PCC (Class S or Class P) |  |  |  |
| Gradation | ARIZ 201 | Crusher Belt or Stockpile | 1 per 750 CY of Concrete |
| Sand Equivalent | AASHTO T 176 |  |  |
| Coarse Aggregate for PCC (Class S or Class P) |  |  |  |
| Gradation | ARIZ 201 | Crusher Belt or Stockpile | 1 per 750 CY of Concrete |
| Class S Portland Cement Concrete |  |  |  |
| Entrained Air | AASHTO T 152 | At Point of Discharge | 1 per 40 CY of Concrete |
| Slump | AASHTO T 119 |  |  |