*     USE IN CONJUNCTION WITH REINFORCED CONCRETE PIPE FLARED END SECTION PAY ITEMS      *

(1010PIPE, 03/16/23)

SECTION 1010	DRAINAGE PIPE:

1010-6	Reinforced Concrete Pipe: the sixth paragraph of the Standard Specifications is revised to read:

Precast, reinforced concrete flared end sections shall conform to the requirements of the previously cited specifications to the extent to which they apply.  The area of steel reinforcement per linear foot of the flared end section shall be at least equal to the minimum steel requirement for the reinforcement in that portion of the flared end section which abuts the pipe. Flared end sections may utilize in lieu of steel reinforcement a minimum of 5.0 pounds of macro fibers, conforming to ASTM C1116, per cubic yard of concrete mix.