*	  	USE WHEN TOTAL QUANTITY OF BORROW, EMBANKMENT, AND           *				STRUCTURAL BACKFILL ON THE PROJECT	*

*				IS 5000 CUBIC YARDS OR MORE	*

*	USE IN CONJUNCTION WITH THE FOLLOWING:		*

*			BID ITEM:				9240170		*

*			STORED SPECIFICATION:	924CQC	*

(203QCEW, 07/15/05)

SECTION 203	EARTHWORK:  of the Standard Specifications is modified to add:

203-2.02		Contractor Quality Control:

The contractor shall perform the quality control measures described in Subsection 106.04(C).  At the weekly meeting, the contractor shall be prepared to explain and discuss how the following processes will be employed:

(a)	Backfill production, including crusher methods, pit extraction, and washing.

(b)	Stockpile management, including stacking methods, separation techniques, stockpile pad thickness, and segregation prevention.

(c)	Transporting and placing, including transport technique, lift thickness, processing and mixing technique, and compaction methods.

(d)	Excavation and transporting, including method of excavation and transporting methods.

(e)	Embankment, including method of mixing, compaction methods, unsuitable material control, waste site, and lift thickness.

The contractor shall obtain samples and perform the tests specified in the following table:

| CONTRACTOR QUALITY CONTROL TESTING REQUIREMENTS |  |  |  |
| --- | --- | --- | --- |
| TYPE OF TEST | TEST METHOD | SAMPLING POINT | MINIMUM TESTING FREQUENCY |
| Structural Backfill |  |  |  |
| Gradation | ARIZ 201 | Stockpile | 1 per 500 CY per Source |
| PI | AASHTO T 89 AASHTO T 90 |  |  |
| ### Proctor Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | Stockpile | 1 per Source and as needed |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | In-place | 1 per 200 CY, minimum 1 per lift |
| Subgrade |  |  |  |
| Gradation | ARIZ 201 | Roadway | 1 per Soil Type |
| PI | AASHTO T 89 AASHTO T 90 |  |  |
| ### Proctor Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | Roadway | 1 per Soil Type |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | Roadway | 1 per 1,000 feet |
| Natural Ground for Embankment Less than 5 Feet |  |  |  |
| ### Proctor Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | In-place | 1 per Soil Type |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | In-place | 1 per 1,000 feet |
| Embankment |  |  |  |
| ### Proctor Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | In-place | 1 per Soil Type |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | In-place | 1 per 1,000 feet per lift |
| Borrow Within Three Feet of Finished Subgrade Elevation |  |  |  |
| Gradation | ARIZ 201 | In-place | 1 per 2,000 CY |
| PI | AASHTO T 89 AASHTO T 90 |  |  |