*	FILL IN THE FOLLOWING IN MATERIALS SUBSECTION:			*

PERCENT PASSING			(3 places)		*

PLASTICITY INDEX RANGE		(1 place)		*

*	USE IN CONJUNCTION WITH THE FOLLOWING:

BIDDING SCHEDULE:				2030113		*

* QUANTITY OF EXCAVATION FOR SHOULDER BUILDUP SHOWN ON PLANS	*

(203SHLEA, 04/16/20)

SECTION 203	EARTHWORK

203-11.02(A)	Earthen: the third and fourth paragraphs of the Standard Specifications are revised to read:

Borrow for shoulder build-up material shall conform to the requirements of Subsection 203-9.02 of the specifications and to the following gradation (Arizona Test Method 201):

| Sieve Size | Percent Passing |  |
| --- | --- | --- |
| 1-1/2 inch | # XXX |  |
| 1/2 inch | XX - XX |  |
| No. 200 | X.X – XX.X |  |

The plasticity index shall be XX to XX when tested in accordance with the requirements of AASHTO T 90.  The soluble salts, when tested in accordance with the requirements of Arizona Test Method 237, shall not exceed 3,000 parts per million unless the level of soluble salts in the in-place native soil exceeds 3,000 parts per million, in which case the shoulder build-up material may not exceed the level of soluble salts in the in-place native material.