*      USE IF THE PROJECT INCLUDES STRUCTURE BACKFILL      *

(203STRBKFL, 10/21/21)

SECTION 203	EARTHWORK:

203-5.03(B)(1) 	Structure Backfill: the first paragraph of the Standard Specifications is revised to read:

Structure backfill material shall be selected from excavation or from a source selected by the contractor. It shall not contain frozen lumps, chunks of clay, or other objectionable material. Backfill material shall not contain salvaged asphaltic concrete materials. Backfill material to be used for metal piles or similar items of metal shall have a value of resistivity not less than 2,000 ohm-centimeters or the value shown on the plans. Backfill material shall have a pH value between 6.0 and 10.0, inclusive, when placed against metal installations, except aluminum. Backfill material shall have a pH value between 6.0 and 9.0, inclusive, when placed against aluminum installations. Backfill material shall have a pH value between 6.0 and 12.0, inclusive, when placed against installations other than metal. Tests for pH and resistivity shall be in accordance with the requirements of Arizona Test Method 236.