*				USE WHEN TOTAL AGGREGATE BASE OR			*

*				SUBBASE IS 1,000 CUBIC YARDS OR MORE.			*

*	USE IN CONJUNCTION WITH THE FOLLOWING:					*

*			BID ITEM:				9240170				*

*			STORED SPECIFICATION:		924CQC				*

(303QCAB, 07/15/05)

SECTION 303	AGGREGATE SUBBASES AND AGGREGATE BASES:  of the Standard Specifications is modified to add:

303-3.04		Contractor Quality Control:

The contractor shall perform the quality control measures described in Subsection 106.04(C).  At the weekly meeting, the contractor shall be prepared to explain and discuss how the following processes will be employed:

(a)	Aggregate production, including crusher methods, pit extraction, and washing.

(b)	Stockpile management, including stacking methods, separation technique, stockpile pad thickness, and segregation prevention.

(c)	Transporting and placing, including transport technique, lift thickness, processing and mixing technique, and compaction methods.

The contractor shall obtain samples and perform the tests specified in the following table:

| CONTRACTOR QUALITY CONTROL TESTING REQUIREMENTS |  |  |  |
| --- | --- | --- | --- |
| TYPE OF TEST | TEST METHOD | SAMPLING POINT | MINIMUM TESTING FREQUENCY |
| Aggregate Base Class 1, 2, or 3 |  |  |  |
| Fractured Coarse Aggregate Particles | ARIZ 212 | Crusher belt or Stockpile | 1 per 1,200 CY |
| Gradation | ARIZ 201 | Crusher belt or Stockpile | 1 per 600 CY |
| PI | ### AASHTO T 89 AASHTO T 90 |  |  |
| ### Proctor Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | Crusher belt or Stockpile | 1 per Source and as needed |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | Roadway | 1 per 600 CY |
| Aggregate Subbase Class 4, 5, or 6 |  |  |  |
| Fractured Coarse Aggregate Particles (Class 4) | ARIZ 212 | Crusher Belt or Stockpile | 1 per 1,200 CY |
| Gradation | ARIZ 201 | Crusher Belt or Stockpile | 1 per 600 CY |
| PI | AASHTO T89 AASHTO T90 |  |  |
| ### Proctor Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | Crusher belt or Stockpile | 1 per Source and as needed |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | Roadway | 1 per 600 CY |