** FILL IN INFORMATION FROM THE MATERIALS REPORT IN THE FOLLOWING SUBSECTION (SHOWN IN RED TEXT) **

** 4040302-2.0	Material Requirements **

(404WDCRK, 05/20/21)

ITEM 4040302 -	WIDE CRACK AND JOINT REPAIR USING HOT APPLIED MASTIC:

1.0			Description:

The work under this item shall consist of furnishing all materials, personnel, and equipment to clean and repair cracks and joints 1-1/2 inches or wider in existing asphaltic concrete pavements.

2.0			Material Requirements:

Mastic material shall be a hot-applied, prepackaged, pourable, aggregate filled, polymer modified asphalt mastic conforming to the requirements of ASTM D8260, Type X.

Certificates of Compliance, conforming to the requirements of Subsection 106.05 of the specifications, shall be submitted.

3.0			Construction Requirements:

3.01	Preparation of Cracks:

Immediately prior to application of the mastic material, the contractor shall ensure that the cracks are thoroughly cleaned through the full depth of the crack or joint.  Loose particles, grass, grass roots, weeds, dust and other deleterious substances shall be removed by means of high velocity compressed air, or by other methods approved by the Engineer.  Compressed air equipment shall have traps or devices to prevent moisture and oil from contaminating the crack surfaces.

Cracks with juts shall be chiseled to provide a consistent surface for the mastic material to adhere, as approved by the Engineer.

3.02	Equipment:

The mastic material shall be heated in a melter approved by the material manufacturer.  The melter shall be capable of maintaining the application temperature.  The melter shall be equipped with positive temperature controls, and with mechanical horizontal agitation.  The melter shall be equipped with a thermometer that indicates the temperature of the mastic material in the hopper.

3.03	Application of Mastic Material:

Pavement temperature shall be 40 degrees F or higher and pavement shall be clean and dry.

The mastic material shall be mixed, heated, placed, and finished in accordance with the manufacturer’s instructions.  The material shall be applied in an overband configuration or as shown on the project plans.  The overband shall exceed the deteriorated area at least 2 inches on both sides to structurally sound pavement.

The finished installation shall be smooth and not exceed 1/8 inch thickness above the surrounding pavement surface.

To prevent tracking, traffic shall not be allowed on the repaired areas until the material has cooled to the surrounding pavement surface temperature.  Water may be applied to the material surface to expedite cooling, as approved by the Engineer.

4.0			Method of Measurement:

Wide crack and joint repair using hot-applied mastic will be measured by the pound.

5.0			Basis of Payment:

The accepted quantities of wide crack and joint repair using hot-applied mastic, measured as provided above, will be paid for at the contract unit price per pound, which price shall be full compensation for the work, complete in place, as described and specified herein, and as shown on the project plans.