*	FILL IN THE FOLLOWING:								*

*		SECTION 2	TYPE OF ASPHALT BINDER		(1 place)	*

(406ACMSP, 09/08/11)

ITEM 4060009 -	ASPHALTIC CONCRETE (MISCELLANEOUS PAVING):

Description:

The work under this item shall consist of constructing Asphaltic Concrete (Miscellaneous Paving), hereinafter asphaltic concrete, by furnishing all materials, mixing, hauling and placing a mixture of aggregate materials and bituminous material (asphalt cement) to form a pavement course or to be used for other specified purposes, in accordance with the details shown on the project plans, the requirements of the specifications, and as directed by the Engineer.

Asphaltic concrete shall be produced from commercial sources or from any source approved by the Engineer.

Materials:

Aggregate for asphaltic concrete shall have an abrasion of not more than nine percent loss at 100 revolutions when tested in accordance with AASHTO T 96.  The aggregate shall be crushed and processed to the following grading limits such that the sand equivalent is at least 55 when tested in accordance with AASHTO T 176.  The gradation will be determined in accordance with the requirements of Arizona Test Method 201.

| Sieve Size | Percent Passing |
| --- | --- |
| 3/4-inch | 100 |
| 1/4-inch | 55 - 75 |
| No. 8 | 40 - 55 |
| No. 200 | 0 - 6.0 |

Bituminous material shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005.  The type of asphalt binder shall be PG XXXXX.

(A)		Proportions:

The asphalt cement content will be specified by the Engineer and will be appropriate with the characteristics of the aggregates furnished from which the asphaltic concrete is to be produced.

The percent of asphalt cement used shall be based on the weight of total mix (asphalt cement and aggregate).

(B)		Sampling and Testing:

Sampling and testing the materials or mixture for quality control purposes shall be the contractor's responsibility.  The Engineer reserves the right to sample and test the materials and mixture as the Engineer deems necessary to determine that the materials and mixture reasonably conform to the requirements specified herein.

Construction Requirements:

Before asphaltic concrete is placed, the surface to be paved shall be cleaned of all objectionable material and tacked with bituminous material in accordance with the requirements of Section 404.

Just prior to being placed, the asphaltic concrete shall be in a thoroughly mixed condition, free of lumps and crusts and at such a temperature as to be in a free flowing, workable condition.

The asphaltic concrete shall be placed, using approved equipment and methods, to the lines and grades shown on the project plans or as directed by the Engineer.

The asphaltic concrete shall be compacted, using approved equipment and methods, to the satisfaction of the Engineer.

(A)		Acceptance:

Asphaltic concrete will be accepted complete in place, if, in the judgment of the Engineer, the asphaltic concrete reasonably conforms to the requirements specified herein.  Asphaltic concrete that is not acceptable and is rejected shall be replaced to the satisfaction of the Engineer and at no additional cost to the Department.

Method of Measurement:

Asphaltic Concrete (Miscellaneous Paving) will be measured by the ton for the mixture actually used, which will include the weight of aggregate and bituminous material.  Measurement will include any tonnage used in construction of intersections, turnouts, curbs, spillways and spillway inlets, ditches, catch basin entrances, median strips, sidewalks or other miscellaneous items or surfaces.

Basis of Payment:

The accepted quantities of Asphaltic Concrete (Miscellaneous Paving), measured as provided above, will be paid for at the contract unit price per ton for the bituminous mixture complete in place.

No direct payment will be made for the bituminous material in the asphaltic concrete, or the bituminous material for tack coat, or for the application of tack coat, the price being considered as included in the price paid for asphaltic concrete.

Asphaltic concrete may be measured by volume, upon the execution of a Supplemental Agreement which will specify the manner in which the volume is determined.  The volume will include the volume of aggregate and bituminous material.