*                    USE WHEN SPECIFIED IN THE MATERIALS DESIGN REPORT                  *

*                          USE STORED SPECIFICATION 109PAVSM WHEN AN                           *

*              INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE              *

*                                                      PAVEMENT SMOOTHNESS                                          *

*                                  IS SPECIFIED IN THE MATERIALS DESIGN REPORT.                   *

**               WHEN PAVEMENT SMOOTHNESS INCENTIVES/DISINCENTIVES               **

**                            ARE SPECIFIED IN THE MATERIALS DESIGN REPORT,                   **

**              EDIT THIS STORED SPECIFICATION TO INCLUDE THE REVISION               **

**                          TO SUBSECTION 409-3.01 (SECOND PARAGRAPH).                          **

*	FILL IN THE FOLLOWING (SHOWN IN RED TEXT):					    *

*		409-2		UNIT WEIGHT	(1 place)	    *

*		409-2.02		TYPE OF ASPHALT BINDER		(1 place)	    *

(409AGGR, 03/16/23)

SECTION 409	ASPHALTIC CONCRETE (MISCELLANEOUS STRUCTURAL):  the title of the Standard Specifications is revised to read:

SECTION 409	ASPHALTIC CONCRETE (MISCELLANEOUS STRUCTURAL-SPECIAL MIX):

409-1			Description:  the first paragraph of the Standard Specifications is revised to read:

The work under this section shall consist of constructing Asphaltic Concrete (Miscellaneous Structural-Special Mix), hereinafter asphaltic concrete, by furnishing all materials, mixing at a plant, hauling and placing a mixture of aggregate materials, reclaimed asphalt pavement (RAP) if used, mineral admixture, and bituminous material (asphalt cement) to form a pavement course or to be used for other specified purposes, in accordance with the details shown on the project plans and the requirements of the specifications, and as directed by the Engineer.

409-2			Materials:  of the Standard Specifications is modified to add:

The bidding schedule quantity of asphaltic concrete is based on an estimated unit weight of XXX pounds per cubic foot.

409-2.01		Mineral Aggregate:  of the Standard Specifications is revised to read:

Mineral aggregate shall conform to the following requirements when tested in accordance with the applicable test methods.

| Mineral Aggregate Characteristics | Test Method | Requirement |
| --- | --- | --- |
| Combined Bulk Oven Dry Specific Gravity | Arizona Test Method 251 | 2.350 - 2.850 |
| Combined Water Absorption | Arizona Test Method 251 | 0 - 2.5% |
| Abrasion | # AASHTO T 96 | 100 Rev., Max 9% 500 Rev., Max 40% |
| Sand Equivalent | AASHTO T 176 (After thoroughly sieving the sample, no additional cleaning of the fines from the plus No. 4 material is required.) | Minimum 55 |
| Fractured Coarse Aggregate Particles | Arizona Test Method 212 | Minimum 85% with at least two fractured faces and minimum 92% with at least one fractured face (plus No. 4 material) |
| Uncompacted Void Content | Arizona Test Method 247 | Minimum 45.0% |
| Carbonates (1) | Arizona Test Method 238 | Maximum 20% |
| (1): Testing for carbonates only applies if either of the following conditions exist: |  |  |
| (a) The asphaltic concrete is the designed final pavement surface normally used by traffic. (b) The asphaltic concrete, temporary or otherwise, will be subject to traffic for more than 60 days. |  |  |

The gradation will be determined in accordance with Arizona Test Method 201, and shall conform to the requirements given below.

| Mix Design Grading Limits |  |  |
| --- | --- | --- |
| Sieve Size | Percent Passing |  |
|  | Without Admix. | With Admix. |
| 1 Inch | 100 | 100 |
| 3/4 Inch | 90 – 100 | 90 - 100 |
| 3/8 Inch | 62 – 77 | 62 - 77 |
| No. 8 | 37 – 46 | 38 -47 |
| No. 40 | 10 – 18 | 11 - 19 |
| No. 200 | 1.5 - 4.5 | 2.5 – 6.0 |

Fine mineral aggregate shall be obtained from crushed gravel or crushed rock.  All uncrushed material passing the No. 4 sieve shall be removed prior to the crushing, screening, and washing operations necessary to produce the specified gradation.  The contractor shall notify the Engineer a minimum of 48 hours in advance of crushing the material to be used as mineral aggregate, so all crushing operations can be inspected.  Existing stockpile material which has not been inspected during crushing will not be permitted for use unless the contractor is able to document to the Engineer's satisfaction that the mineral aggregate has been crushed.  Any material inspected by the Department as crushed material for the project shall be separated from the contractor’s other stockpiles and reserved for use throughout the project duration.

The contractor may blend uncrushed fine aggregate up to a maximum of 15 percent of the total aggregate, provided that the composite of uncrushed fine aggregate and crushed fine aggregate meets the requirement for uncompacted void content.  The uncrushed fine aggregate shall be 100 percent passing the 1/4 inch and not contain more than 4.0 percent passing the No. 200 sieve.  Should the contractor modify the method of producing either the uncrushed or crushed fine aggregate, the Engineer shall be immediately notified and the materials sampled and tested for determination of uncompacted void content.

409-2.02		Bituminous Material:  the first paragraph of the Standard Specifications is revised to read:

Asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005 of the specifications.  The type of asphalt binder shall be PG XXXX.

409-2.03		Mineral Admixture:  the second paragraph of the Standard Specifications is revised to read:

The mineral admixture content shall be 2.0 percent, by weight, of the mineral aggregate.  However, a minimum of 1.0 percent mineral admixture may be used if the contractor submits test information showing a lowered percentage of mineral admixture produces mix design results for Index of Retained Strength of at least 60 percent (70 percent if the average elevation of the project is above 3,500 feet) and a Minimum Wet Strength of 150 psi when tested in accordance with Arizona Test Method 802.

409-2.04		Mix Design:  the third, fourth, and fifth paragraphs of the Standard Specifications are revised to read:

The mix design shall be prepared by or under the direct supervision of a professional engineer experienced in the development of mix designs and mix design testing.  Reclaimed asphalt pavement (RAP) may be used in the mixture if properly designed per Arizona Test Method 833; however, RAP will not be allowed in the mixture when asphalt cement type PG 76-22 TR+ or PG 70-22 TR+ is specified in Subsection 409-2.02 of the specifications.  Limits for the usage of RAP shall be in accordance with ADOT Materials Practice and Procedure Directive No. 20, “Guidance on the Use of Reclaimed Asphalt Pavement (RAP) in Asphaltic Concrete”.  The mix design engineer shall meet the requirements given in ADOT Materials Practice and Procedure Directive No. 4, “Asphaltic Concrete Mix Design Proposals and Submittals”.  The mix design shall be provided in a format that clearly indicates all the mix design requirements and shall be sealed, signed, and dated by the mix design engineer.

The mix design shall be prepared by a mix design laboratory that has met the requirements of ADOT Materials Practice and Procedure Directive No. 19, “ADOT System for the Evaluation of Testing Laboratories”.

If approved by the Engineer, as an alternative to meeting the mix design requirements specified herein, a mix design meeting the requirements of the specifications for a Section 416 Asphaltic Concrete (End Product) (3/4 inch Special Mix), Section 417 Asphaltic Concrete (SHRP) (End Product (1/2 inch Mix), or Section 417 Asphaltic Concrete (SHRP) (End Product) (3/4 inch Mix) may be substituted for use.  The type of asphalt binder used in the alternative mix design must be the same as that specified in Subsection 409-2.02 of the specifications.  The alternative mix design may include reclaimed asphalt pavement (RAP) if properly designed per Arizona Test Method 833.  If a mix design meeting the requirements of Section 417 is used, the number of gyrations for N-design used in the alternative mix design must be at least that which would be specified at the location where the Asphaltic Concrete (Miscellaneous Structural-Special Mix) is to be placed.  The lift thickness for the alternative mix design shall conform to the following table.

| Alternative Mix Design | Minimum Lift Thickness |
| --- | --- |
| Section 416 (3/4 inch Special Mix) | 2 inches |
| Section 417 (1/2 inch mix) | 2 inches |
| Section 417 (3/4 inch mix) | 2-1/2 inches |

409-2.04		Mix Design:  the last three paragraphs of the Standard Specifications are revised to read:

A copy of the mix design and representative samples of the mineral aggregate, mineral admixture, and asphalt cement used in the mix design shall be submitted to the Engineer for calibration of the ignition furnace, and for the determination of sand equivalent, fractured coarse aggregate particles, and uncompacted void content.  The Engineer shall witness the sampling of the mineral aggregate.  The mix design and samples shall be submitted to the Engineer at least five working days prior to the start of asphaltic concrete production.

The sand equivalent, fractured coarse aggregate particles, and uncompacted void content shall meet the requirements specified in Subsection 409-2.01 of the specifications.  Additional testing of the uncrushed and crushed fine aggregate for uncompacted void content will be required if the method of producing either fine aggregate is modified.

If the mineral aggregate fails to meet the requirements specified herein, asphaltic concrete production shall not commence, and the contractor shall either submit a revised mix design which is representative of the materials produced or correct the deficiencies in the aggregate stockpiles.

The mix design shall meet the following criteria when tested in accordance with the requirements of the following test methods:

| ## Criteria | ## Requirement | Arizona Test Method |
| --- | --- | --- |
| 1. Voids in Mineral Aggregate: %, Range | 15.0 – 18.0 | (See Note ) |
| 2. Effective Voids: %, Range | 5.3 – 5.7 | (See Note ) |
| 3. Absorbed Asphalt: %, Range | 0 – 1.0 | (See Note ) |
| Note: For mixes without RAP, Arizona Test Method 815. For mixes with RAP, Arizona Test Method 833. |  |  |

The contractor may make self-directed target changes to the approved mix design within the limits shown below.  Requests for self-directed target value changes shall be made in writing and acknowledged by the Engineer prior to start of production.  Self-directed target changes shall meet contract requirements for mix design criteria and grading limits.

| MEASURED CHARACTERISTICS | ALLOWABLE SELF-DIRECTED TARGET VALUE CHANGES |  |
| --- | --- | --- |
| Gradation (sieve size): |  |  |
| 3/8 inch No. 8 No. 40 No. 200 | 4% from mix design target value 4% from mix design target value 2% from mix design target value 0.5% from mix design target value |  |
| Asphalt Cement Content | +0.2% from mix design target value |  |
| Effective Voids | None |  |

The contractor may propose target value changes to the approved mix design for the Engineer’s approval.  The Engineer will determine if the proposed target value change will result in mix production that meets the contract requirements for mix design criteria and grading limits.  For acceptance purposes, target value changes will not be retroactive.

In no case shall the approval of mix design changes relieve the contractor of the responsibility for the results obtained by the use of such approved changes.

409-2.05		Sampling and Testing:  of the Standard Specifications is revised to read:

Sampling and testing the materials and mixture for quality control purposes shall be the contractor's responsibility.  The contractor shall perform sufficient testing to assure that mineral aggregate and asphaltic concrete are produced which meet all specified requirements.

For acceptance purposes, samples of the asphaltic concrete shall be taken by the contractor, under the observation of the Engineer, at random locations designated by the Engineer.  A minimum of one sample shall be taken for each 500 tons of asphaltic concrete.  Samples shall be taken in accordance with the requirements of Section 2 or Section 3 of Arizona Test Method 104.  The Engineer will immediately take custody of the samples.  The material will be tested by the Engineer for the following properties:

| Test Property | Test Method |
| --- | --- |
| Asphalt Cement Content | Arizona Test Method 427 (428 for RAP mixes) (See Note) |
| Gradation |  |
| Marshall Density | Arizona Test Method 410 |
| Maximum Theoretical Density | Arizona Test Method 417 |
| Effective Voids | Arizona Test Method 424 |
| Note: A new calibration of the ignition furnace shall be performed for each mix design, and at any other time the Engineer directs. |  |

(When pavement smoothness incentives/disincentives are

specified in the Materials Design Report, use the following

revision to the second paragraph of Subsection 409-3.01 and change to black text;

otherwise delete this revision of the second

paragraph from this stored specification.)

409-3.01		General:  the first sentence of the second paragraph of the Standard Specifications is revised to read:

Smoothness of the final pavement surface shall be tested, and payment for smoothness made, in accordance with Subsection 109.13 of the specifications.  In addition to the requirements of Subsection 109.13 of the specifications, the following requirements shall also be met:

409-3.01		General:  the fourth paragraph of the Standard Specifications is hereby deleted:

409-3.03		Acceptance:  of the Standard Specifications is revised to read:

Asphaltic concrete will be accepted complete in place unless the result of any test varies from the contractor’s mix design target value (TV) as follows:

| Test Property | Allowable Variation from Target Value |  |
| --- | --- | --- |
| Gradation (Sieve sizes) |  |  |
| 3/8 inch | TV –10.0 | TV + 10.0 |
| No. 8 | TV – 8.0 | TV + 8.0 |
| No. 40 | TV – 6.0 | TV + 6.0 |
| No. 200 | TV – 2.5 | TV + 2.5 |
| Asphalt Cement Content | TV – 0.60 | TV + 0.70 |
| Effective Voids | TV –2.5 | TV + 2.0 |

Within 15 days after receiving notice of any failing test result(s), the contractor may submit a written proposal to accept the material represented by the failing test result(s), in place, at a reduction in cost.  If the failing test result(s) are only on asphalt cement content and/or effective voids, the reduction in cost will be $5.00 per ton.  If the failing test result(s) are only on gradation, the reduction in cost will be $3.00 per ton.  If the failing test result(s) are on asphalt cement content and/or effective voids, and also on gradation, the reduction in cost will be $5.00 per ton.  The proposal shall contain an engineering analysis of the anticipated performance of the asphaltic concrete if left in place.  The engineering analysis shall also detail any proposed corrective action, and the anticipated effect of such corrective action on the performance.  The engineering analysis shall be performed by an independent professional engineer, who is not an employee of the contractor or materials supplier, experienced in asphaltic concrete testing and the development of asphaltic concrete mix designs.

Within three working days, the Engineer will determine whether or not to accept the contractor’s proposal.  If the proposal is accepted, the asphaltic concrete shall remain in place, at a reduction in cost per ton, as described above, and any necessary corrective action shall be performed at no additional cost to the Department.  If the proposal is not accepted, the asphaltic concrete shall be removed at no additional cost to the Department and replaced with asphaltic concrete meeting the requirements of these specifications.

The contractor may request that a sample with a failing test result(s) on gradation and/or asphalt cement content be allowed to remain in place without the completion of an engineering analysis if the application of a self-directed target value change as outlined in section 409-2.04 would have brought the failing test result(s) to within the specified tolerances. This proposal must be made to the Engineer in writing with justification. Once accepted, the material will be allowed to remain in place at the maximum negative pay factor(s). Maximum negative are defined as a minus $3.00 per ton for mixture properties lots in reject for gradation only, minus $5.00 per ton for mixture properties lots in reject for asphalt cement content and/or effective voids only, and minus $5.00 per ton for mixture properties lots in reject for asphalt cement content and/or effective voids and also gradation.

If the asphaltic concrete, represented by failing test results, is used as temporary pavement which will be removed prior to, or after, the completion of construction, the Engineer reserves the right to waive the engineering analysis and accept the material in place, at a cost reduction described above, provided the temporary pavement maintains the functionality of the intended use for the duration of the project.