*                           USE STORED SPECIFICATION 109PAVSM WHEN AN                           *

*              INCENTIVE/DISINCENTIVE PAYMENT FOR ASPHALTIC CONCRETE               *

*                                 PAVEMENT SMOOTHNESS IS SPECIFIED IN                                   *

*                                          THE MATERIALS DESIGN REPORT                                          *

*	USE IN CONJUNCTION WITH THE FOLLOWING:					    *

*		BID ITEM:							9240170			    *

*		STORED SPECIFICATIONS:			924CQC			    *

*									        1001MATL			    *

*	FILL IN THE FOLLOWING (SHOWN IN RED TEXT):					    *

*		416-2			EFFECTIVE VOIDS				(As Needed)		    *

*					RATIO MINIMUM VALUE			(1 place)		    *

*		416-3			UNIT WEIGHTS				(As Needed)		    *

*					PERCENTAGES				(As Needed)		    *

*		416-3.03(B)	TYPE OF ASPHALT BINDER		(1 place)		    *

(416ACES, 12/16/21)

SECTION 416	ASPHALTIC CONCRETE – END PRODUCT

416-2			Asphaltic Concrete Mix Design Criteria: Item 2 “Effective Voids” of the Standard Specifications is revised to read, and the Note (1) is hereby deleted:

| Criteria | Requirements |  |  | Arizona Test Method |
| --- | --- | --- | --- | --- |
|  | 1/2” Mix | 3/4” Mix | Base Mix |  |
| 2. Effective Voids: %, Range | X.X 0.2 | X.X 0.2 | X.X 0.2 | Note (3) |

416-2			Asphaltic Concrete Mix Design Criteria: the last paragraph of the Standard Specifications is revised to read:

The ratio of the mix design composite gradation target for the No. 200 sieve including mineral admixture, to the effective asphalt content shall be within the range specified below:

X.X to 1.2

416-3			Materials: of the Standard Specifications is modified to add:

For comparative purposes, quantities shown in the bidding schedule have been calculated based on the following data:

(In the following two tables, use only the columns called for in the

Materials Design Report;  exclude all of either table if no

column is called for in the Materials Design Report.)

| Standard Mixes | 1/2” Mix | 3/4” Mix | Base Mix |
| --- | --- | --- | --- |
| Unit Weight, (lb./cu. ft.) | XXX | XXX | XXX |
| Asphalt Cement, % | X.X | X.X | X.X |
| Mineral Admixture, % | 1.0 | 1.0 | 1.0 |

| Special Mixes | 1/2” Mix | 3/4” Mix | Base Mix |
| --- | --- | --- | --- |
| Unit Weight, (lb./cu. ft.) | XXX | XXX | XXX |
| Asphalt Cement, % | X.X | X.X | X.X |
| Mineral Admixture, % | 1.0 | 1.0 | 1.0 |

416-3.03(B)	Virgin Bituminous Material: the first paragraph of the Standard Specifications is revised to read:

Virgin asphalt cement shall be a performance grade (PG) asphalt binder, conforming to the requirements of Section 1005.  The type of virgin asphalt binder shall be PG XXXXX or, if RAP is used in the mixture, the virgin asphalt binder shall be as required to meet the blending requirements in Subsection 416-3.03(C) and Arizona Test Method 833.

416-9(E)	Acceptability: of the Standard Specifications is modified to add:

The contractor may submit a written proposal without an engineering analysis for Engineer’s evaluation and approval, that a mixture properties lot with a PT value lower than 50 on gradation and/or asphalt cement content be allowed to remain in place if the application of a Self-Directed Target Change as outlined in Subsection 416-4 of the specifications would bring the PT value to 50 or greater. This written request shall also include the proposed revised PT calculations. Upon Engineer’s verification and approval of the request, the material shall remain in place at the maximum negative pay factor(s) specified in this Subsection for the mixture properties lot in reject.