*	USE WHENEVER THE PROJECT REQUIREMENTS APPLY FOR ANY OF 	*

*	THE FOLLOWING:										*

*     ANY PIPE ON THE PROJECT WITH A DESIGNATED 		*

DIAMETER OF 60 INCHES OR GREATER.

*     THE TOTAL LENGTH OF ALL PIPE ON THE PROJECT IS	*

IN EXCESS OF 600 FEET.

*     IF THERE IS ANY PIPE ON THE PROJECT AND STORED	*

SPECIFICATION 203QCEW IS BEING USED.

*	USE IN CONJUNCTION WITH THE FOLLOWING:

*		BID ITEM:						9240170				*

*		STORED SPECIFICATION:			924CQC				*

(501QCDRN, 07/15/05)

SECTION 501	PIPE CULVERT AND STORM DRAINS:

501-3			Construction Requirements:  of the Standard Specifications is modified to add:

501-3.01(A)	Contractor Quality Control:

The contractor shall perform the quality control measures described in Subsection 106.04(C).  At the weekly meeting, the contractor shall be prepared to explain and discuss how the following processes will be employed:

(a)	Bedding and backfill production, including crusher methods, pit extraction, and washing.

(b)	Stockpile management, including stacking methods, separation techniques, stockpile pad thickness, and segregation prevention.

(c)	Transporting and placing, including transport technique, lift thickness, processing and mixing technique, and compaction methods.

The contractor shall obtain samples and perform the tests specified in the following table:

| CONTRACTOR QUALITY CONTROL TESTING REQUIREMENTS |  |  |  |
| --- | --- | --- | --- |
| TYPE OF TEST | TEST METHOD | SAMPLING POINT | MINIMUM TESTING FREQUENCY |
| Backfill Material |  |  |  |
| Gradation | ARIZ 201 | ## Stockpile | 1 per 500 CY per Source |
| PI | AASHTO T 89 AASHTO T 90 |  |  |
| ### Proctor ### Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | Stockpile | 1 per Source and as needed |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | In-place | 1 per 200 CY, minimum 1 per lift |
| Bedding Material |  |  |  |
| Gradation | ARIZ 201 | ## Stockpile | 1 per 300 CY per Source |
| PI | AASHTO T 89 AASHTO T 90 |  |  |
| ### Proctor ### Density | ARIZ 225 #### ARIZ 226 ### ARIZ 245 | Stockpile | 1 per Source and as needed |
| ### Field ### Density | ARIZ 227 ARIZ 230 ### ARIZ 232 ARIZ 235 ### ARIZ 246 | In-place | 1 per 50 CY |