(703DTRMKR, 07/21/22)

SECTION 703	DELINEATORS AND MARKERS:

703-2.10		Flexible Delineator Posts: the fourth paragraph of the Standard Specifications is revised to read:

The flexible delineator posts shall be pigmented throughout the entire cross- section (or entire cross-section of the outer layer of multi-layered, multi-material units) so as to produce a uniform color which is an integral part of the material. The posts shall exhibit negligible color fading after 1,000 hours of Xenon Arc Exposure (ASTM G155). The posts shall be made of durable, ultraviolet-resistant, impact-resistant, non-warping, non-metallic, polymeric materials designed for a minimum of 120 months of outdoor service life.